EVALUATION OF CORROSION PROPERTY OF COPPER IN WASTE PLAM OIL AS BIOFUEL

BY

M.SUGANTHI

(09PCM17)

A DISSERTATION SUBMITTED TO

AVINASHILINGAM DEEMED UNIVERSITY FOR WOMEN

COIMBATORE-641 043

IN PARTIAL FULFILLMENT OF DEGREE OF

MASTER OF SCIENCE IN CHEMISTRY

MAY 2011

DEDICATED TO MY FAMILY AND MY GUIDE

ACKNOWLEDGEMENT

ACKNOWLEDGEMENT

I submit my reverential gratitude at the feet of the Lord Almighty, and I thank all those who helped me during this course of study,

I owe my heartfelt thanks to Mr.T.S.K.Meenakshi Sundaram, M.A,M.Phil,Chancellor, Avinashilingam Deemed University for women, Coimbatore for providing the opportunity to conduct this study.

My sincere thanks to Dr. (Tmt.) sheela Ramachandran, M.Sc., P.G Dip.,Ph.D (Avinashilingam), Vice Chancellor, Avinashilingam Deemed University for women, Coimbatore, for providing all the necessary facilities for the study.

My hearty thanks to Dr. (Mrs.) Gowri Ramakrishnan, M.Sc., (Madras), M.phil., Ph.D., (Avinashilingam), Registrar, Avinsahilingam Deemed University for Women, Coimbatore for providing adequate help required to carry out the work.

I express my sincere gratitude to Dr. (Tmt.) Saroja Prabhakaran, M.A., Dip.Ed., (Madras), Ph.D (Mother Teresa), The Director, Hall of residence,  Avinashilingam University for Women, Coimbatore, for all the amenities provided for the conduct of the study.

My thanks to Dr.(Mrs.) R.Parvatham. M.sc., Dip.Ed.,M.Phil.(Madras) Ph.D (Avinashilingam), Dean, Faculty of Science, Avinashilingm Deemed University for Women, Coimbatore her constant support for completion of my dissertation work.

I express my deep sense of gratitude to my guide Dr.(Mrs.).R.Shyamala M.Sc, Dip.Ed,(Madras), M.phil,(Bharathiar), Ph.D (Avinashilingam), Professor and Head, Department of Chemistry, Avinashilingm Deemed University for Women, Coimbatore for her valuable guidance, moral support, encouragement, constructive criticism, assertive advice, throughout my dissertation work.

I also thank all the staff members of the Department of chemistry Avinashilingm Deemed University for Women, Coimbatore for their help and encouragement.

I thank my sisters Mrs.H.N.Meenakshi, Miss.Anisha Anand, research scholars, Avinashilingm Deemed University for Women, Coimbatore for their co-operation patience, support and help for the successful completion of my study.

I also express my heartfelt thanks to my beloved parents and my friends for their whole hearted support and encouragement to carry out this work.

M.SUGANTHI

CONTENTS

CONTENTS

S.NO					TITLE					PAGE NO

LIST OF TABLES

LIST OF FIGURES

ABBREVIATIONS

1				INTRODUCTION					1

2				REVIEW OF LITERATURE			9

3				MATERIALS AND METHODS			19

4				RESULTS AND DISCUSSION			24

5				SUMMARY AND CONCLUSION			41

REFERENCES

LIST OF TABLES

| S.NO | PARTICLUARS | PAGE NO |
| --- | --- | --- |
| 1 | Standards on fuel properties of biodiesel | 5 |
| 2 | Composition of copper metal | 20 |
| 3 | Comparison of fuel properties of UPO with that of ASTMD6751standard values | 29 |
| 4 | Corrosion rate of copper coupons exposed to O100, O99, NaCl and their conductance (Mass loss method) | 30 |
| 5 | Corrosion rate of copper coupons exposed to O100, O99, NaCl and their conductance (LPR method) | 31 |
| 6 | Corrosion rate of copper coupons exposed to CD, O5, O10,O20,O100 and their conductance (Mass loss method) | 32 |
| 7 | Corrosion rate of copper coupons exposed to CD, O5, O10,O20,O100 and their conductance (LPR method) | 33 |

LIST OF FIGURES

LIST OF FIGURES

| S.NO | PARTICULARS | PAGE NO |
| --- | --- | --- |
| 1 | PALM OIL SEED AND TREE | 6-7 |
| 2 | SOLATRON 1280B | 23 |
| 3 | CONTACT ANGLE DIAGRAM | 27 |
| 4 | Corrosion Rate of Copper metal in O100, O99, NaCl, as Function of Time (LPR method) | 34 |
| 5 | Comparison of Corrosion Rate of Copper Metal as Determined by Mass Loss and LPR Method | 35 |
| 6 | Contact angle of UPO on copper metal | 36 |
| 7 | Corrosion Rate of Copper Metal in CD, O5, O10, O20 and O100 as Function of Time (LPR method) | 37 |
| 8 | Comparison of Corrosion Rate of Copper Metal in various UPO and CD blends as Determined by Mass Loss and LPR Method | 38 |
| 9 | Photomicrographs of polished copper and copper in O100,O99 and NaCl | 39 |
| 10 | Photomicrographs of Copper in UPO-CD Blends | 40 |

ABBREVIATIONS

mpy	:	mils per year

C.R	: 	Corrosion rate

t	:	Time

hrs	:	Hours

NaCl	:	Sodium chloride

W	:	Weight

D	:	Density

A	:	Area

UPO	:	Used palm oil

LPR    :	Linear Polarization Resistance

INTRODUCTION

1.INTRODUCTION

As civilization is growing, transport becomes essential part of human life; the energy needs are increasing which ultimately results in the decrease in supply of fossil fuels. Hence an alternative fuel source is very important to meet the demands on fossil energy. The development of new technologies for processing and using biofuels is steadily progressing

Biofuels production and consumption ensures that the natural carbon cycle to be 100% achieved which completely eliminates the continuous increase in carbon dioxide rates in the atmosphere which in turns will have the greatest effect on the environment and a way to end global warming.

Among all renewable energy resources, biomass is the only resource that can be converted in a relatively direct way into fuels. Bioenergy is energy derived from biofuels. Biofuels are fuels produced directly or indirectly from organic material – biomass – including plant materials and animal waste. Overall, bioenergy covers approximately 10% of the total world energy demand. Traditional unprocessed biomass such as fuelwood, charcoal and animal dung is the main source of energy for a large number of people in developing countries who use it mainly for cooking and heating.

Primary biofuels such as fuelwood, wood chips and pellets, organic materials are used in an unprocessed form, primarily for heating, cooking or electricity production. Secondary biofuels result from processing of biomass and include liquid biofuels such as ethanol and biodiesel that can be used in vehicles and industrial processes.

- Energy Security: Biofuels can readily displace petroleum fuels and in many countries, can provide a domestic rather than imported source of transport fuel

- Environment: Biofuels are generally more climate-friendly than petroleum fuels, with lower emissions of CO2 and other greenhouse gases

- Fuel quality: Refiners and car manufacturers have become very interested in the benefits of ethanol in order to boost fuel octane, especially where other potential octane enhancers such as MTBE are discouraged or prohibited More sustainability in transportation: biofuels are derived from renewable energy     .

1 BIOFUEL FEEDSTOCKS

1.2 BIOFUEL FROM WASTE COOKING OIL

There is a large variety of waste oils available for biofuel production. In general these waste oils are inexpensive and offer an additional environmental impact by using substances which would otherwise have to be disposed. The origin of the oil can be characterized by three types:

- Waste oil from households and restaurants

- Waste oil from food industry

- Waste oil from non-food industry

Rape, soybean, palm and coconut oils are the waste oils most frequently used in biodiesel production. The use of these waste vegetable oils (WVO) requires additional processing to filter out residues and to handle the acids produced by high temperatures.

A brief description of the use of waste oil from households and restaurants is given by MITTELBACH & REMSCHMIDT. They describe the success of recycled-frying oil for the use in bus fleets in Austria. There, recycled-frying oil methyl esters (RFO-ME) have been commercially produced since 1992. In the City of Graz about fifty buses are running without any problems on RFO-ME as this fuel only slightly differs from those of RME. The values of viscosity and carbon residue of RFO-ME tend to be slightly higher and cold temperature properties are poorer compared to RME.

There are many co-products in the food industry, which can be used for biofuel production as well. MITTELBACH & REMSCHMIDT  mention rice-bran oil, a highly acidic oil recovered from the waste material produced during rice dehulling. Also oil from palm fruit pulp is mentioned. Palm fruit pulp is the waste material left over after the removal of the palm seeds, which normally are dumped without further treatment.

During refinement steps of edible soybean oil production, soybean soapstock is produced.This co-product may be used for biodiesel production, too. Additionally highly acidic sulfur olive oil, a co-product of olive oil refining and whey, a waste product of the diaryindustry can serve for biodiesel production.     Besides the above mentioned sources of waste-oil, sometimes industrial waste oils can beused for biofuel production. An example is tall oil, a co-product of the manufacture of sulfate pulp from resinous woods, such as pine and spruce.

1.3 PROPERTIES OF BIODIESEL

A major benefit of biodiesel is that it can be used in diesel engines and fuel injection equipment with little to no impact on operating performance. In more than 50 million miles of in-field experience, a blend of 20% biodiesel and 80% petroleum diesel (B20) showed similar fuel consumption, horsepower, torque, and haulage rates compared with conventional diesel. Hundreds of truck fleets across the country are now using B20 in all types of vehicles and driving conditions.

LUBRICITY

All diesel fuel injection equipment has some reliance on the fuel itself as a lubricant, especially for the proper functioning of rotary and distributor type fuel injection pumps. In these pumps, moving parts are lubricated not by engine oil, but by the fuel as it moves through the pump. Other diesel fuel systems, including unit injectors, unit pumps, and in-line pumps are partially fuel lubricated.

CETANE INDEX

Cetane index measures the readiness of a fuel to auto-ignite after it has been injected into a diesel engine, and is comparable to the octane rating for gasoline. Higher cetane fuels have shorter ignition delay periods than lower cetane fuels. Fuels with a cetane rating lower than the engine’s minimum requirements can cause rough engine operation and may be more difficult to start, especially in cold weather or at high altitudes. In addition, low cetane fuels may increase engine deposits, resulting in more smoke, increased exhaust emissions, and greater engine wear.

ENERGY CONTENT

Study results of energy content in biodiesel and how it impacts performance have been varied and research into this area continues. Current consensus is that high level blends of biodiesel may contain a lower energy content than petroleum diesel. Depending on the load and driving conditions, the difference in energy content between biodiesel and petroleum diesel may be noticeable when using B99. As the biodiesel blend level is lowered, any effects due to reduced energy content diminish. For B20, the difference in power, torque, and fuel economy should be between 1% and 2%, depending on the diesel with which it is blended. Most users report little performance difference between B20 and 2 diesel. Blends of B5 or less do not cause noticeable differences in performance. Table 1 summarises the popular standards of fuel properties of biodiesel.

TABLE 1

STANDARDS ON FUEL PROPERTIES OF BIODIESEL

| Biodiesel Standards |  | EUROPE | GERMANY | USA | PETROLEUM DIESEL |
| --- | --- | --- | --- | --- | --- |
| Specification |  | EN 14214:2003 | DIN V 51606 | ASTM D 6751-07b | EN 590:1999 |
| Applies to |  | FAME | FAME | FAAE | Diesel |
| Density 15°C | g/cm³ | 0.86-0.90 | 0.875-0.90 |  | 0.82-0.845 |
| Viscosity 40°C | mm²/s | 3.5-5.0 | 3.5-5.0 | 1.9-6.0 | 2.0-4.5 |
| Distillation | % @ °C |  |  | 90%,360°C | 85%,350°C - 95%,360°C |
| Flashpoint (Fp) | °C | 120 min | 110 min | 93 min | 55 min |
| Cloud point | °C |  |  | * report |  |
| Sulphur | mg/kg | 10 max | 10 max | 15 max | 350 max |
| Carbon residue (10%dist.residue) | %mass | 0.3 max | 0.3 max |  | 0.3 max |
| Sulphated ash | %mass | 0.02 max | 0.03 max | 0.02 max |  |
| Oxid ash | %mass |  |  |  | 0.1 max |
| Water | mg/kg | 500 max | 300 max | 500 max | 200 max |
| Total contamination | mg/kg | 24 max | 20 max |  | 24 max |
| Cu corrosion max | 3h/50°C | 1 | 1 | 3 | 1 |
| Oxidation stability | hrs;110°C | 6 hours min |  | 3 hours min | N/A (25 g/m3) |

1.4 CONTAMINATION BY WATER

Biodiesel may contain small but problematic quantities of water. Although it is not miscible with water, it is, like ethanol, hygroscopic .One of the reasons biodiesel can absorb water is the persistence of mono and diglycerides left over from an incomplete reaction. These molecules can act as an emulsifier, allowing water to mix with the biodiesel. In addition, there may be water that is residual to processing or resulting from storage tank condensation. The presence of water is a problem because:Water reduces the heat of combustion of the bulk fuel. This means more smoke, harder starting, less power.Water causes corrosion of vital fuel system components: fuel pumps, injector pumps, fuel lines, etc.Water & microbes cause the paper element filters in the system to fail (rot), which in turn results in premature failure of the fuel pump due to ingestion of large particles.Water freezes to form ice crystals near 0 °C (32 °F). These crystals provide sites for nucleation and accelerate the gelling of the residual fuel. Water can cause pitting in the pistons on a diesel engine. The  present work is aimed to study the corrosion behaviour of copper on waste palm oil obtained from a restaurant.

PALM OIL

Figure 1(a)

Figure (b)

OBJECTIVES

- To compare the values of fuel properties of oil with ASTM D6751 standard.

- To find out the composition of metal.

- To conduct a systematic study to test the corrosivity of used palm oil on copper metal.

- To evaluate the corrosion rate of copper metal in 3% NaCl.

- To evaluate the corrosion rates of copper metal in UPO, O99, and blends for a period of 100hrs at room temperature by mass loss measurement.

- To determine the corrosion rate for various blends of commercial diesel and UPO.

- To measure the conductivity of the test solutions before and after exposure of the copper metal in the solutions.

- To carry out the linear polarization studies to evaluate the corrosion rate continuously for a period of 24 hours for copper metal in various test media.

- To compare the corrosion rate obtained in mass loss method with that obtained by linear polarization method.

- To determine the wettability of oil on copper metal using contact angle method

- To study the surface morphology of copper exposed to various test media.

REVIEW OF LITERATURE

# 2. REVIEW OF LITERATURE

# In this chapter Research and development works done in the field of biofuel by various Researches have been reviewed.

# Meenakshi H.N et al., (2011) have studied the corrosivity of Pongamia pinnata biodiesel and its blends with petro diesel on various metals in state  condition by mass loss and linear polarisation resistance methods. The result showed that the metals immersed in Pongamia pinnata biodiesel and its blends are higher than those immersed in commercial diesel.

# Anisha Anand et al., (2011)  have studied the corrosion aspect of Jatropha oil on various industrial metals by various techniques and the result obtained were compared with that of biodiesel from pongamia pinnata. Under most condition studied, the corrosivity of Jatropha oil is lower than that of biodiesel obtanined from Pongamia pinnata.

T.M. Loganathan et al.,2010 Investigation has been carried out following the frequent occurrences of shaft failures in a number of palm oil screw press machines in a Malaysia palm oil mill company. Visual inspection, chemical analysis on the shaft material, fatigue analyses by utilizing traditional method and microscopic examinations were performed to support the investigation. Overview on pitting corrosion problems is presented. Common locations of the failure are at around bottom edges of keyway and shoulder fillets of the shafts. The findings indicate that pitting corrosion is identified as the main root causes of the premature shaft failures.

Meenakshi H.N et al., 2010 have studied the corrosion rates of few metal in biodiesel obtained from Pongamia pinnata. The results showed that biodiesel is a suitable renewable alternative fuel that can be added to diesel derived from fossil fuel because their constituents match that of diesel. The corrosion rates of all metals in biodiesel are insignificant.

Deniz F Aktast et al., 2010 have studied that biodiesel metabolism accelerated the rate of both sulfate reduction and methanogenesis above biodiesel-unamended cont. Electrochemical/corrosion experiments showed that the anaerobic microbial metabolism of biodiesel in coastal seawater samples accelerated the rate of pitting corrosion in carbon steel. The susceptibility of biodiesel to anaerobic biodegradation and its propensity to stimulate bio corrosion suggest caution when integrating this alternate fuel with the existing infrastructure.

A.S.M.A. Haseeb et al., 2010 have studied the corrosion behavior of commercial pure copper and leaded bronze commonly encountered in the automotive fuel system in diesel engine. Static immersion tests in B0, B50 and B100 fuels were carried out at room temperature for 2640 h. Similar immersion tests in diesel, B100 and B100 (oxidized) fuels were also conducted at 60 °C for 840 h. At the end of the test, corrosion behavior was investigated by weight loss measurements and changes in surface morphology. Fuels were analyzed by using TAN analyzer, FTIR, MOA (multi-element oil analyzer) to investigate acid concentration, oxidation level with water content and corrosive impurities respectively. Results showed that under the experimental conditions, pure copper was more susceptible to corrosion in biodiesel as compared to leaded bronze.

Wei Wang et al, 2010. have studied the influence of water contamination and corrosion behavior of carbon steel in biodiesel using the wire beam electrode (WBE) technique. In situ local current distributions among the electrodes showed a distinct corrosion pattern, with the anodes formed in the area that was exposed to water, and the cathodes formed along the water–biodiesel interface. The anodic current distribution showed a positive correlation with the biodiesel concentration gradient in water.

Alexander Guzman et al.,2010 have studied the high cetane index renewable diesel can be obtained by hydro processing of palm oil using conventional hydro treating catalyst (NiMo/Al2O3).At 40-90 bar hydrogen pressure crude palm oil can be deeply converted into paraffin’s in the diesel range. At lower pressures hydro-deoxygenation cannot be fully reached and the appearance of intermediates as C16-C18 acids and esters were preliminary identified in the reaction product. Times of stream experiments have shown conventional hydro treating catalyst suffers of slight deactivation as the reaction proceeds.

Siddharth Jain et al.,2010 have reported the results of kinetics study of acid base catalyzed two step transesterification process of waste cooking oil, carried out at pre-determined optimum temperature of 65°C and 50°C for esterification and transesterifiation process  respectively under the optimum condition of methanol to oil ratio of 3:7 (v/v), catalyst concentration 1% (w/w) for H2SO4 and NaOH and 400 rpm of stirring. The optimum temperature was determined based on the yield of ME at different temperature. Simply the optimum concentration of H2SO4 and NaOH and determined with respect of ME yield. This is the first study of its kind which deals with simplified kinetics of two step acid-base catalyzed transesterification process carried under the above optimum conditions and took about 6h for  complete conversion of TG to ME with least amount of activation energy. Also various parameters related to experiments are optimized with respect to ME yield.

Nezahat Boz et al., 2009 synthesized biodiesel by using KF- impregnated nano partical of Al2O3 as heterogeneous catalysts for the trans esterification of vegetable oil with methanol for the synthesis of biodiesel. The ratio KF to nano Al2O3, calcinations temperature, molar ratio of methanol/oil, trans esterification reaction, temperature and time, and the concentration of the catalyst were used as the parameters of the study.

M.A. Fazal et al, 2009 have made a comparative study on corrosion behavior of aluminum, copper and stainless steel in both petroleum diesel and palm biodiesel. Immersion tests in biodiesel (B100) and diesel (B0) were carried out at 80 °C for 1200 h. Corrosion characteristic was investigated by weight loss measurements and changes on the exposed metal surface. Surface morphology was examined by optical microscope and scanning electron microscopy with energy dispersive X-ray analysis. Results show that the extent of corrosion and change in fuel properties upon exposure to metals are more in biodiesel than that in diesel. Copper and aluminum were susceptible to attack by biodiesel whereas stainless steel was not.

Jianwei Tan et al., 2009 have investigated the characteristics of carbonyl compounds emission on a direct injection, turbocharged diesel engine fueled with pure biodiesel derived from soybean oil. The gas-phase carbonyls were collected by 2,4-dinitrophenylhydrazome (DNPH)-coated silica cartridges from diluted exhaust and analyzed by HPLC with UV  detector. A commercial standard mixture including 14 carbonyl compounds was used for quantitative analysis.

L.M Geng et al., 2009 have prepared the biodiesel from soybean crude oil by a method of alkaline-catalyzed transesterification. The important properties of bio diesel were compared with those of diesel. Diesel and biodiesel used as fuels in the compression ignition engine were analyzed. The results showed that biodiesel exhibited the similar combustion stages to thet of diesel, however, biodiesel showed an earlier start of combustion.

Katherine M.Richard, 2009 have studied the impact of biodiesel on corrosion related performance. The effect of FAME biodiesel on lubricant corrosion control and the difference on performance due to FAME source were described. Mechanistic studies into the corrosive nature of RAME were reported. Novel lubricant technologies tailored to control the negative impact of FAME in the crankcase were demonstrated.

B.H.Hameed et al., 2009  have studied that transesterification of waste cooking palm oil using activated carbon supported potassium fluoride catalyst. A central composite rotatable design was used to optimize the effect of molar ratio of methanol to oil, reaction period catalyst loading and reaction temperature on the transesterification process. The reactor was pressurizes up to 10 bar using nitrogen gas. All the variables were found to affect significantly the methyl ester yield where the most effective factors being the among of catalyst and reaction temperature, followed by methanol to oil ratio. A quadratic polynomial equation was obtained for methyl ester yield by multiple regression analysis using response surface methodology. The experimental value was well within the estimated value of the model. The catalyst showed good performance with a high yield of methyl ester and the separation of the catalyst from the liquid mixture is easy.

L. Díaz-Ballote et al., 2008 have evaluated corrosion behaviour of Aluminium by conventional electrochemical techniques .Aluminium was exposed to biodiesel with different levels of contaminants and impurities, and its corrosion behaviour was evaluated. It was found that the corrosion behaviour of aluminium in biodiesel contaminated with alkalis is similar to the corrosion behaviour of aluminium in aqueous solutions. In addition, it was demonstrated that corrosion of aluminium can be used as a quantitative indication of the biodiesel purity.

Investigations have been carried out on regulated and unregulated emissions of a diesel engine fueled with ultra-low sulfur diesel fuel blended with bio diesel from waste cooking oil (Yage Di et al., 2008)

The effects of hydrocarbons and corrosion have been predicted based on type of emulsion (water-in-oil or oil-in-water), wet ability (oil wet, water of mixed wet), and corrosivity of brain in the presence of hydrocarbons, obtained from operating pipelines. S.Papavinasm et al 2008

Y.C.Sharma et al., 2008 have described that the biodiesel is an environmentally viable fuel. Direct use and blending, micro- emulsions, thermal cracking and trans esterification, most commonly used method is trans esterifucation of vegetable oils, fats, waste oils

Hanbey Hazar 2008 has studied the increase in engine power and decrease in specific fuel consumption as well as significant improvements on exhaust gas emissions and smoke density, for all test fuels used in the coated engine and compared with that of the uncoated engine.

Ana Maria de oliveira et al., 2007 have studied the increase in bio fuels consumption, mainly ethanol and biodiesel as well as their blends with diesel that reduced the cost impact of bio diesel while retaining some of the advantages of the biofuels. This increase was due to several factors like decreasing the dependence on imported petroleum; providing a market for the excess production of vegetable oils and animal fats; using renewable and biodegradable fuels; reducing global warming due to its closed carbon cycle by CO2 recycling

A.P.Roskily et al., 2007 investigated that the power output for both trial engines operating with biodiesel were comparable to that fuelled with fossil diesel, but with an increase in fuel consumptions. The NOx emission was found to be lower when the engines operated at higher loads using bio diesel. The CO emissions were found to be lower when the engines operated at higher loads using bio diesel.

Xiangmei Meng  et al., 2007  Investigation of biodiesel production from waste cooking oil on reaction conditions such as methanol/oil  molar ratio, alkaline catalyst amount, reaction time and reaction temperature which are deemed to have main impact on reaction conversion efficiency experiments have been performed to determine the optimum conditions for this transesterification process by orthogonal analysis lf parameters in a four factor and three level test. After the analysis main characteristics of biodiesel sample, the impact of biodiesel/diesel blend fuels on an YC6M220 turbo-charge diesel exhaust emissions was evaluated compared with 0 diesels. The testing results show without any modification  to diesel engine, under all conditions dynamical performance kept normal and the B20,B50 blend fuels led to unsatisfactory emissions whilst the B20 blend fuel reduced significantly particular, HC and CO etc, emission. For example CO,HC and particles were reduced by 18.6%,26%and20.58% respectively.

N. H. Jayadas et al., 2007 have studied the corrosion properties of vegetable oils as base oil for industrial lubricants by the copper strip corrosion test and rust prevention test An analysis of possible organic reaction mechanisms leading to corrosion of metals in the absence and presence of oxygen and moisture is presented, when vegetable oils are used as base oils. Control of moisture content and use of additives like ZDDP can be effective in controlling corrosion.

Zjemg-ji-Lu, 2006 have studied that the rice husk was fast pyrolysed at temperature between 420oc and 54. In a fluidized bed, and the main product of bio oil was obtained. The experimental result conformed that the highest bio oil yields of 56 weight percentage was obtained that 465oc for rice husk. Chemical composition of bio oil acquired was analyzed by GC-MS AND its heat value, stability, miscibility and corrosion characteristic were determined.

Savita kual al ., 2006 have investigated the corrosion behaviour of bio diesel from non-edible oils like Jatropha curcas, Pongamia glabra ,Madhuca indica and Salvadora oleoides.  Corrosion characteristics of bio diesel are important for long-term durability of engine parts, and very little information is available on this aspect. The studies were therefore taken up to assess the corrosion of synthesized biodiesel from the above-mentioned non edible oils.

Mangesh G.Kulkarni et al., 2006 reviewed methods for the trans esterification of waste cooking oil and the performance of biodiesel obtained from waste cooking oil in a commercial diesel engine .The basic chemistry involved during frying and the effects of the products formed in the frying process on biodiesel quality was also examined.

S.Murillo et al., 2006 investigated that the biodiesel alone or blended biodiesel can be used in compression ignition outboard engines, thereby providing a viable alternative to diesel. Special attention should be paid to the use of bio diesel in boats operating on lakes and rivers and in sheltered bays, which are more vulnerable to pollution.

Yung Chee Liang et al., 2005 have investigated the effect on the oxidative stability of distilled palm oil methyl esters. It was found that both types of antioxidant showed beneficial effects in inhibiting the oxidation of distilled palm oil methyl esters. Comparatively, the synthetic antioxidants were found to be more effective than the natural.

Sandun Fernando  et al 2005 have  evaluated the performance of fatty acid methyl ester with different proportions of unconverted triglycerides triglyceride of flash point, water and sediment, kinematic viscosity, sulphur content, sulphated ash, copper strip  corrosion, cetane number, cloud point, carbon residue, acid number, free glycerin, total glycerin, phosphorus content and distillation temperature.

W.Yuan et al., 2005 have analyzed the scmitivity of coconut and butterfat. Most of the methyl esters of the vegetable oils and animal fats had a normal boiling point in the range of 620-630 K. A sensitivity analysis indicated that the variation of fatty acid composition and the uncertainty of the normal boiling point of C18:2 were the main factors that affected the predicted normal boiling points of the biodiesel fuels.

D.Q.Peng et al., 2004 evaluated the aqueous corrosion resistance of implanted M5 alloy in 1 M suphuric acid solution by adopting potentiodinamic polarization technique. A significant improvement was achieved in the aqueous corrosion resistance of M5 alloy implanted with carbon ions. The higher the flounce, the better is the corrosion resistance. Finally, the mechanism of the corrosion behavior of carbon-implanted M5 alloy was discussed.

J. Kaminski et al., 2003 have studied that the corrosion resistance of stainless steel and carbon steel in diesel oil solution containing different amount of fatty acid methyl ester and microorganism. The corrosion resistance was examined by using impedance methods on samples expose for up to 26 weeks in an organic phase, water phase and inter face water-bio diesel. Correlation between the corrosion rate and bio component quantity was determined. The corrosion rate and the amount of bacteria the degraded fuel also reported.

Chaur jeng Wang et al., 2003 have studied both the higher temperature and the water vapor in the atmosphere promoted metal loss. The metal loss of SB450 in the atmosphere that contained water vapor, resulting from the burning of emulsified oil, was larger than obtained by burinig just the diesel oil. Moreover, water vapor contributed to higher SO2 concentrations is the gas produced. SB450 suffers sulfidation more seriously in an atmosphere that constrains water vapor than in one obtained by burning diesel oil; it thus deteriorates more rapidly.

S. S. Abd El Rehim, et al, 2002 have studied the electrochemical behaviour and corrosion of a commercial Egyptian 18-8 austenitic stainless steel in sulphuric acid and in sodium sulphate solutions using the potentiodynamic technique. In acid solution, the anodic polarization scans are characterized by the appearance of active, passive and transpassive transitions before oxygen evolution. The current densities corresponding to these three regions are increased by increasing either the acid concentration or the voltage scanning rate. The passive electrode does not regain its activity when subjected to cathodic treatment. Sensitization of the electrode enhances its susceptibility to intergranular corrosion. In sodium sulphate solution, the polarization scans are characterized by the disappearance of the active region. On sensitization, a second transpassive region appears before oxygen evolution

M.A.Maleque et al., 2002 discussed that the activity of palm oil methyl ester on the metal surface is quite remarkable when added to a mineral-based lubricant wear of piston ring and ball bearing materials took place by abrasive, corrosive and/or oxidative mechanisms with different concentrations of palm oil methyl ester in lubricants.

J.W.Goodrum, 2001 investigated the quality control of fuel-related properties of Biodiesel, such as volatility, which is needed to obtain consistent engine performance by fuel users. The vapor pressures and boiling points of selected methyl esters and vegetable oils were proposed as quality control metrics for Biodiesel.

M.A.Maleque et al., 2000 have studied the friction behavior of POME (palm oil methyl ester) as an additive in commercial lubricant indicates the prevalence of the boundary lubrication regime. The viscosity test results showed that 5% POME could improve the viscosity properties of mineral-based lubricant up to 500 N loads. In this investigation, corrosive wear and pits on the damaged surface were the dominant wear mode at higher temperature was more susceptible to corrosion in biodiesel as compared to leaded bronze.

H.H.Masjuki et al 2000 have evaluated the effect of anticorrosion additive in bio diesel on diesel engines, performance, and emission and wear characteristics. This bio diesel is defined as the methyleater palm oil also known as palm oil diesel. The results of this investigation will be of use to find a compatible lubricant for biodiesel engines.

Jan Cvengros et al., 1995 have investigated the production and treatment of rapeseed oil methyl esters as alternative fuels for diesel engines.

H.H.Masjuki et al., 1999 have studied tribiological and emission of palm oil and mineral oil based lubricants performance of the palm oil based lubrication oil exhibited better performance in terms of wears and that the mineral oil based lubricating oil exhibited better performance in terms of friction. The palm oil based lubricant was the more effective in reducing the emissions levels of CO and hydrocarbon.

MATERIALS AND METHODS

- MATERIALS AND METHODS

To determine the outcome of any research work, selection of method and materials are vitally important. Following are the material chosen and methodology adopted in the present work.

3.1 SELECTION OF SAMPLE

Copper occurs naturally with elements such as lead, nickel, silver and zinc. It is widely used in industry both as a pure metal and as an alloying material. The metal develops adherent protective coatings, initially of oxide, but subsequently thickening to give a familiar green patina on roofs and the dark brownish color of bronze statues. Because copper is largely unaffected by potable water, its is widely used for tubes carrying domestic and industrial water.

3.2 PREPARTATION OF SAMPLE

The sheet of cold rolled copper metal, which is commercially available in the market, was machined into coupons of area 33.94 cm2. Holes were drilled on the center of the one side of all the coupons for suspension. These coupons were degreased, cleaned with emery paper and washed with distilled water. The panels were stored in desiccators in the absence of moisture before their use for the investigation.

TABLE 2

COMPOSITION OF COPPER METAL

| S.NO | ELEMENT | % OF CHEMICAL COMPOSITIONSAMBLE |
| --- | --- | --- |
| 1 2 3 4 5 6 7 8 9 10 | COPPER LEAD TIN ZINC MANGANESE ALUMINIUM IRON NICKEL PHOSPHOROUS SILICON | 94.907 0.000 0.000 5.065 0.006 0.003 0.000 0.008 0.000 0.000 |

The elemental analysis of the copper metal sample has been carried out at Premier Instrument and Control Limited (PRICOL), testing laboratory Coimbatore by using Vacuum emission spectrometer DV-4. The composition of copper metal used in the investigation is given in table 2.

3.3   OIL CHARACTERIZATION PROCEDURE

Used palm oil was collected from a particular restaurant in Theni. The characterization of the oil was performed as per ASTM D6751 in IND-AG Inspection and Testing Laboratory Coimbatore.

3.4 CORROSION RATE MEASUREMENT

MASS LOSS METHOD:

Specimen were accurately weighed in an electronic balance (SHIMADZUAUW22OD) and fully immersed in 200 ml test media for a period of 100hrs.

TEST MEDIA

O100 → 100%oil

O99 → 1% of 3%NaCl+99%oil

NaCl → 3% NaCl

CD   → commercial diesel

O5   → 5ml oil+ 95 ml CD

O10 → 10ml oil+90ml CD

O20 → 20ml oil+80ml CD

Specimens were removed after the set intervals of time and dipped in sodium hydroxide solution for the removal of the excess oil. They were washed with distilled water dried and reweighed. The mass loss was determined in triplet in each test media. The corrosion rate was calculated from the following equation.

Corrosion rate (mpy) =           3.45xmoss. loss(grams)

Density (g/cm3) xArea (cm2) x time (hours)

3.5 CONDUCTIVITY MEASUREMENT

The conductivity of O100, O99, NaCl, O5, O10, O20,CD before and after exposure of coupons by a conductivity bridge.

3.6 LINEAR POLARISATION RESISTANCE METHOD:

LPR studies were conducted with the help of LPR study (SOLSTRON 1280B (Fig 2). The electrochemical cell was a glass beaker containing the aerated unstirred test solution with a platinum electrode as the counter electrode, saturated calomel electrode as the reference electrode and the metal specimen (with an exposed area of 1cm2) as the working electrode. The metal coupons (of same composition as in the mass loss method) were degreased, cleaned with fine quality emery sheet and washed with distilled water. The linear polarization measurements were carried out within the potential range of -0.02Vto +0.02V (scan ratio 0.1667m V/s) with respect to open circuit potential. The corrosion rate was measured every hour for 24hours. From the polarization resistance (Rp)  values, the corrosion rate was calculated.

Corrosion current Icorr =  1/Rp          _βa.βc_

2.303(ßa+ßc)

Where

βa	-	Anodic Tafel slope

βc		cathodic Tafel slope

Assuming value of 120vfor both βa and βc the above equation is reduced to

Icor =26/Rp

From the corrosion current, corrosion rate was calculated using the ASTM G5 standard.

Figure (2)

3.7 WETTABILITY

3.7.1CONTACT ANGLE METHOD

Metal samples were polished and cleaned first with distilled water and the with ethanol. The samples were then placed in a non- reflecting rectangular glass tank containing distilled water and the oil was injected through a syringe into the water so that it would adhere to the sample surface. The contact angle was measured through the water phase. The photograph of the oil droplet on the metal surface was taken. On a printed photograph a horizontal line was drawn at the base of the droplet with the metal surface two tangents were drawn. The two exterior angles between the base and the tangents are measured with a protractor.

3.8 SURFACE MORPHOLOGY

Changes in Surface Morphology of pure copper and copper strips exposed to various test media was characterized by Inverted metallurgical microscope KOZO optics model XJM 404T.

.

RESULTS AND DISCUSSION

RESULTS AND DISCUSSION

The environmental, social and economic advantages of biofuels including lower emissions of harmful pollutants decreased green house gas emissions, increased employment and energy security, decreased dependence of oil imparts and good fuel properties for vehicles have paved way for research in this field. Considering the above facts reused palm oil was chosen as biofuel and its corrosion properties on copper has been investigated.

4.1 ANALYSIS OF BIOFUEL AS PER ASTM STANDARD

The various parameters for used palm oil as biofuel was analysed as per ASTM D6751 and the data is presented in table (3). The data reveals that most of the properties of used palm oil are comparable with the ASTM standards. The higher viscosity may be attributed to the high molecular weight and large chemical structure of the vegetable oil. Used cooking oil is associated with water content in it. As the heating by cooking period increased, free fatty acid content also increases and hence the higher acid number.

4.2 CORROSION BEHAVIOUR OF COPPER METAL

Biodiesel induced corrosion in storage and transportation occurs by electrochemical mechanism (wet corrosion) costly due to the presence of entrained water. Entry of moist air and or accumulation of water in the tank create conditions for corrosion to occur. Hence the corrosion behaviour of copper was analysed in used palm oil and its blends with CD and NaCl, the various test media used is as follows:

- O100 – Used palm oil

- O99 – 1%of 3% NaCl +99% oil

- NaCl – 3% sodium chloride

- CD – Commercial diesel

- O5 – 5ml of oil+ 95ml CD

- O10 – 10MLof oil+ 90ml CD

- O20 – 20ml of oil+ 80ml CD.

The conductivities of the test solutions before and after the metal panels were exposed to the corrosion atmosphere were also measured.

4.2.1 MASS LOSS MEASUREMENTS

Mass loss measurements were taken for the copper metal statically immersed in various test media for a period of 100hrs. The mass change of the specimens was determined as the different between the final and initial weights. The corrosion rates were calculated from the mass changes. The moss loss changes measured and the corrosion rate calculated are summarized the table (4). As expected the corrosion rate is maximum in NaCl (mpy 3.739) which is ionic in nature.

The susceptibility of copper metal surface to corrosion oil the presence of water is controlled by three factors

    - The corrosivity of brine in the presence of oil

    - The emulsion of the oil and water

    - The wettability of metal surface

The low corrosion rates of copper metal in O100 may be attributed to the non-ionic nature of the palm oil. During storage of biodiesel in steel tanks and transportation through metal pipelines, the oil wets the metal surface since it is has a strong affinity and hence does not occur.

When 1ml of 3%NaCl is added to UPO, the corrosion rate increased. The addition NaCl represents the presence of water. At this low concentration of water, UPO forms water in oil emulsion where water is entrapped inside the oil. Thus the metal is still in contact with the oil and hence a non-corrosive stage prevails.

Since wet corrosion is electrochemical in nature, there is a direct correlation between the corrosivity of the medium and conductance. The highly corrosive brine solution has higher conductance.

The  higher conductance of NaCl solution after exposure of the copper than that before indicates the increased ionic content of the solution due to corrosion. The results of the mass loss studies reveal the fact that copper metal is compatible with the used palm oil.

4.2.2 LPR MEASUREMENTS

To support the mass loss measurements, the corrosion rate of copper metal in NaCl, O99 and O100 as a function of time was carried out by LPR method. Table (5) summarized the corrosion rate obtained by the LPR method. The same is shown in fig (3). Results shows that the corrosion rate is maximum in NaCl and minimum in O100 similar to that obtained from moss loss method.

A variation is the corrosion rate obtained by was loss method and LPR method and LPR method may be attributed to the damage in methodology moss loss method give the instantaneous corrosion.

4.3 WETTABILITY

The presence of free water on of oil/water emulsion does not necessarily lead to corrosion. Under this condition, wettability of the biodiesel on the metal determines the corrosion based on which oil may be classified into three categories.

- Oil wet surface: on an oil-wet surface, the, oil has a strong affinity to be in contact with metal. Oil-wet surface physically isolate the pipe from the corrosion does not occur.

- Water wet surface:  on an oil-wet surface, the oil does not have affinity to be in contact with metal and hence is highly susceptible to corrosion.

- Neutral-wet surface: on a neutral-wet surface, the oil does not has any preference to be in contact with metal. The oil may be in contact with the metal surface as long as there is no competing phase is present.

Figure 3

Wettability is characterized by measuring the contact angel. In the present study, was measured through the water phase. The surface is considered water-wet in which the contact angle is acute and oil-wet when the contact angle is obtuse as shown in figure (3). The contact angle for UPO as measured from figure (6) 140° and 137° the contact angle measurements further confirms that the UPO wets the copper metal surface making it non-corrosive.

4.4 CORROSION BEHAVIOUR OF COPPER IN REUSED PALM OIL-DIESEL BLENDS:

The corrosion rate of copper metal in reused palm oil and its blends namely O5, O10, O20 with commercials diesel and 100% commercial diesel were determined by mass loss and linear polarization resistance methods. The calculated corrosion rates are presented in table (6) and pictorially shown in figure (8)

The measured corrosion rates were very low and there is not much difference in the corrosion rates of copper metal in O100 and its blends with commercial diesel.

The comparison of corrosion rates obtained by mass loss and liner polarization method are shown in figure (8) the difference may be due to the methods adopted.

The increase in conductivities of O100, O5, O20 and commercial diesel may be due to degradation of oil and its blends with commercial diesel and the adsorption of moisture from their environments.

4.5 SURFACE MORPHOLOGY:

Figure (9) shows the photomicrographs of the polished copper sample and copper sample exposed to various test media. The polished copper sample shows  little scratches on the surface which may be due to the grinding of the sample with emery paper (9). Figure (10) also shows a similar pattern as that of the polished sample, which confirms that little corrosion has occurred on the copper surface in O100.

Visual aberration of copper in NaCl showed brown patches which are clear in the photomicrograph (9). From the figure it is evident that corrosion has taken place to a small extent. The pits observed for the metal sample in O99 figure (9) may be due to the presence of entrained water in the oil. The presence of a small amount of water enhances corrosion of the metal.

The photomicrographs of the coupons in commercial diesel and its various blends with UPO do not show signs of corrosion, except for the patches which may be formed due to cleaning of the sample with emery paper fig (10). Thus it may be concluded that used palm oil may be used as biofuel blending with commercial diesel without corrosion issues.

TABLE 3

Comparison of fuel properties of UPO with that of ASTM D6751 Values

| PARAMETERS | # STANDARD (ASTM D 6751) VALUES | # CHARACTERIZED VALUE | # UNITS |
| --- | --- | --- | --- |
| Flash point | 130.0mim | 164 | °c |
| Water and sediments | 0.050max | 0.05 | % |
| Kinematic viscosity | 1.9-6.0 | 27 | Mm2/sec |
| Sulfated ash | 0.020max | 0.91 | % |
| Sulfur content | 0.0015max(ppm) | 12 | Mg/kg |
| Copper strip corrosion | No 3max | NIL | - |
| Cetane | 47min | 29 | - |  |
| Carbon residue | 0.050max | 0.24 | % |
| Acid number | 0.80max | 1.4 | KOH/gm |
| Free glycerine | 0.020max | 0.01 | % |
| Total glycerine | 0.240max | 0.11 | % |
| Phosphorus content | 0.001max | 1.6 | % |
| Distillation temperature Atmospheric Equivalent temperature , 90% recovered | 360max | 284 | °c |

TABLE 4

Corrosion Rate of copper coupons exposed to O100, O99 & NaCl and their conductance (Mass Loss Method)

| Medium | Specimen number | Initial weight(gm) | Final weight(gm) | Mass loss(gm) | Corrosion rate (mpy) | Conductance(µΩ-1) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Initial | Final |  |
| O100 | 1 | 39.6394 | 39.62385 | 0.01555 | 1.767874 | 0.073 |  | 0.131 |
|  | 2 | 39.78211 | 39.76735 | 0.01476 | 1.678058 | 0.073 |  | 0.131 |
|  | 3 | 39.60668 | 39.5315 | 0.01353 | 1.58822 | 0.073 |  | 0.131 |
| O99 | 4 | 39.57266 | 39.55994 | 0.01272 | 1.44613 | 0.074 |  | 0.130 |
|  | 5 | 39.86679 | 39.85516 | 0.01163 | 1.32221 | 0.074 |  | 0.130 |
|  | 6 | 39.2975 | 39.28569 | 0.01181 | 1.34267 | 0.074 |  | 0.131 |
| NaCl | 7 | 39.71085 | 39.68219 | 0.02866 | 3.25834 | 0.051 |  | 0.714 |
|  | 8 | 39.41505 | 39.38258 | 0.0322 | 3.66080 | 0.051 |  | 0.717 |
|  | 9 | 39.62741 | 39.59733 | 0.03008 | 3.41978 | 0.051 |  | 0.714 |

TABLE 5

Corrosion Rate of copper coupons exposed to O100, O99 & NaCl, and their conductance (LPR Method)

| Time(hrs) | Corrosion rate(mpy) |  |  |
| --- | --- | --- | --- |
|  | NaCl | O99 | O100 |
| 1 | - | - | 0.000931 |
| 2 | - | - | 0.000398 |
| 3 | - | 0.21964 | 0.036212 |
| 4 | 0.48409 | - | 0.03596 |
| 5 | 14.288 | - | 0.047726 |
| 6 | - | 0.85133 | 0.000814 |
| 7 | 1.7853 | 0.00555 | 0.000216 |
| 8 | 2.8308 | - | 0.2084 |
| 9 | 0.19508 | 0.082917 | 0.17175 |
| 10 | 1.4115 | 0.07777 | 0.10934 |
| 11 | 10.801 | 0.1026 | 0.00023 |
| 12 | - | 0.38581 | 1.0778 |
| 13 | 0.97009 | 0.096815 | 0.000214 |
| 14 | 1.4043 | 0.043552 | 0.000467 |
| 15 | 0.11049 | - | 0.000949 |
| 16 | 0.44287 | 0.2699 | 0.097121 |
| 17 | 1.0535 | - | 0.000123 |
| 18 | - | 0.61293 | 0.41048 |
| 19 | 0.84048 | 0.27083 | - |
| 20 | 1.7263 | 0.13344 | 0.31455 |

TABLE 6

Corrosion Rate of copper coupons exposed to CD, O5, O10, O20, O100, and their conductance (Mass Loss Method)

| Medium | Specimen number | Initial weight(gm) | Final weight(gm) | Mass loss(gm) | Corrosion rate(mpy) | Conductance(µΩ-1) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Initial | Final |
| O100 | 1 | 39.63940 | 39.62385 | 0.01555 | 1.76787 | 0.073 | 0.031 |
|  | 2 | 39.78211 | 39.76735 | 0.01476 | 1.67805 | 0.073 | 0.031 |
|  | 3 | 39.60668 | 39.59315 | 0.01353 | 1.58822 | 0.073 | 0.031 |
| CD | 10 | 39.61845 | 39.60092 | 0.01753 | 1.98853 | 0.077 | 0.125 |
|  | 11 | 39.72972 | 39.71224 | 0.01748 | 1.98286 | 0.076 | 0.123 |
|  | 12 | 39.45790 | 39.44065 | 0.01725 | 1.95676 | 0.076 | 0.121 |
| O5 | 13 | 39.85905 | 39.84548 | 0.01357 | 1.53932 | 0.075 | 0.123 |
|  | 14 | 39.42480 | 39.40896 | 0.01584 | 1.7682 | 0.076 | 0.122 |
|  | 15 | 39.46984 | 39.45452 | 0.01532 | 1.73783 | 0.076 | 0.122 |
| O10 | 16 | 39.86207 | 39.85095 | 0.01112 | 1.26140 | 0.076 | 0.084 |
|  | 17 | 39.64761 | 39.63437 | 0.01324 | 1.50186 | 0.072 | 0.084 |
|  | 18 | 39.96637 | 39.95394 | 0.01243 | 1.41000 | 0.072 | 0.084 |
| O20 | 19 | 39.49940 | 39.48821 | 0.01119 | 1.26934 | 0.070 | 0.127 |
|  | 20 | 39.42958 | 39.41654 | 0.01304 | 1.47920 | 0.071 | 0.127 |
|  | 21 | 39.60265 | 39.58405 | 0.0186 | 2.10990 | 0.071 | 0.126 |

TABLE 7

Corrosion Rate of copper coupons exposed to CD, O5, O10, O20 and O100 (LPR Method)

| Time | Corrosion Rate (mpy) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | CD | O5 | O10 | O20 | O100 |
| 1 | 0.00011 | 0.00068 | 0.00502 | 0.00132 | 0.49786 |
| 2 | 0.00009 | 0.01635 | 0.24772 | 0.00151 | 0.07620 |
| 3 | 0.00022 | 0.00172 | 0.00578 | 0.00042 | 0.02177 |
| 4 | 0.00014 | 0.00118 | 0.11085 | 0.00461 | 0.81364 |
| 5 | 0.00014 | - | 0.04382 | 0.00046 | 0.59776 |
| 6 | 0.00014 | 0.00748 | 0.00053 | 0.01210 | 0.00563 |
| 7 | 0.00017 | 0.00855 | 0.00052 | 0.00169 | 0.03598 |
| 8 | 0.00882 | 0.05778 | 0.00212 | 0.00148 | 0.14281 |
| 9 | 0.00150 | 0.00455 | 0.00062 | 0.03092 | 0.28146 |
| 10 | 0.00013 | 0.01562 | 0.00074 | 0.00453 | 0.25276 |
| 11 | 0.00015 | 0.01246 | 0.00071 | 0.00079 | 0.11113 |
| 12 | 0.00016 | 0.04183 | 0.00085 | 0.00079 | 0.11177 |
| 13 | 0.00016 | 0.00354 | 0.00088 | 0.00157 | 1.10846 |
| 14 | 0.00015 | 0.00060 | 0.01409 | 0.00179 | 0.09384 |
| 15 | 0.01711 | 0.03747 | 0.00224 | 0.00164 | 0.09363 |
| 16 | 0.00156 | 0.00598 | 0.00173 | 0.18465 | 0.00147 |
| 17 | 0.00016 | 0.00193 | 0.00208 | 0.00130 | 0.12614 |
| 18 | 0.00016 | 0.00509 | 0.00041 | 0.06643 | 0.12614 |
| 19 | 0.00196 | 0.00079 | 0.00062 | 0.09671 | 0.00307 |
| 20 | 0.00089 | 0.00108 | 0.00568 | 0.09685 | 0.01101 |

FIGURE 4

CORROSION RATE OF COPPER METAL IN O100, O99, NaCl, AS FUNCTION OF TIME (LPR METHOD)

FIGURE 5

COMPARISON OF CORROSION RATE OF COPPER METAL AS DETERMINED BY MASS LOSS AND LPR METHOD

FIGURE 6

CONTACT ANGLE OF UPO ON COPPER METAL

FIGURE 7

CORROSION RATE OF COPPER METAL IN CD, O5, O10, O20 AND O100 AS FUNCTION OF TIME (LPR)

FIGURE 8

COMPARISON OF CORROSION RATE OF COPPER METAL AS DETERMINED BY MASS LOSS AND LPR METHOD

FIGURE 9

PHOTOMICROGRAPHS OF COPPER IN VARIOUS TEST MEDIA

9(a)   Polished Sample                                                         9(b)   Sample Immersed inO100

9(c) Sample Immersed inO99                                     9(d) Sample Immersed in NaCl

FIGURE 10

PHOTOMICROGRAPHS OF COPPER IN UPO-CD BLENDS

10(a)   Sample

Immersed in CD                         10(b)   Sample Immersed inO5                               10(c) Sample Immersed in010

10(d) Sample Immersed inO20                                                       10(e) Sample Immersed in O100

SUMMARY AND CONCLUSION

SUMMARY AND CONCLUSION

The compatibility of metals in biofuels is an advancing field and little is known on the corrosion behaviour of various metals in biofuels. Hence the present work has been carried out on the corrosion property of copper in used palm oil and the following conclusions were discussed.

- The UPO has been characterized as per ASTM D6751 and most of the properties were found to meet the standard.

- The corrosion behaviour of copper metal in UPO as biofuel was studied by mass loss method and LPR method.

- The corrosion rate of copper in 0100 was compared with that of O99 and NaCl.

- The corrosion rates of copper in UPO – commercial diesel blends have been reported.

- The corrosion behaviour of metals can be predicted based on the wettability. The measured contact angle for copper was found to be obtuse suggesting that the oil wets the metal surface and hence is less prove to corrosion.

A research in biofuel is essential in the present global energy crisis scenario the development of new techlologies for the use of biofuels in steadily progressing waste cooking oil is a promising altemative for biofuel production as it in a cheaper raw material.The study can be further extended into various other industrial metals which is very important to confidently use biofuel without corrosion problems.

BIBILIOGRAPHY

- REFERENCE

- Meenakshi H.N Paramesh, Anisha Anand, Shymala Krishnamoorthy, Saratha Mani, and Sankara Papavinasam, “Corrosivity of Pongamia pinnata Biodiesel-Diesel blends on a few industrial metals". NACE conference, CORROSION 2011:  paper no: 11142.

- Anisha Anand, Meeenaskhi H.N Paremesh, Shymala Krishnamoorthy, Saratha Mani, and Sankara Papavinasam, “Compatibility of metal in Jatropha oil". NACE conference, CORROSION 2011:  paper no: 11140.

- T.M.Loganathan, J.Purboladsono, J.Inaya Hussain, G.Muthaiyah, and N.Wahab (2010), “pitting corrosion of triggering initial fractures of palm oil screw press machines shafts”, Engineering Failure Analysis,vol. 239(1);1 117-128.

- Meenakshi H.N Paramesh, Anisha Anand, Shymala Krishnamoorthy, Saratha Mani, and Sankara Papavinasam “Corrosion of metals in biodiesel from Pongamia pinnata” NACE conference, CORROSION 2011:  paper no: 10076.

- Deniz F.Aktas,Jason S.Lee Brenda,Little,Richard.I.Ray,Irene      A.Davidova,Chrislopher N.Lyles,and Joseph,M.Sulftifa (2010)”, Anaerobic metabolism of Biodiesel and its Impact on metal corrosion”, Energy fuel, vol.(24); 2924-2928.

- A.S.M.A. Haseeb,  H.H. Masjuki and M.A. Fazal  (2010), “Corrosive characteristics of copper and leaded in palm biodiesel”, Fuel processing technology,vol.(91);329-334.

- Weiwang, Peter E.Jenkins and Zhiyong Ren (2010), “Heterogeneous corrosion behavior of carbon steel in water contaminated biodiesel”,Corrosion Science, vol.( 53); 845-849.

- Siddharth Jain, M.P.Sharma, Shalini and Rajvanshi (2010), “Acid base catalyzed transesterification kinetics of waste cooking oil”, Fuel Processing Technology, vol. (2); 32-38.

- Alexander Guzman, Juan E Torres, Laura P Prada, and Manuel L Nuñez (2009), “Hydro processing of palm oil at piolet plant scale” ,Catalysis today,vol. (156); 38-43.

- Nezahat Boz , Nebahat Degirmenbasi , and Dilhan  M. Kalyon (2009), “Transesterification of vegetable oil to biodiesel using KF loaded nano-γ-Al2O3 as catalyst”, Conversion of biomass to fuel,  vol.( 89); 590-596.

- M.A.Fazal, A.S.M.A. Haseeb, and H.H. Masjuki (2009), “comparative  corrosive characteristic of petroleum diesel and palm biodiesel for automotive material” ,Fuel processing Technology,vol.(91);1308-1315.

- Jianwei Tan, Chao He, Yunshan Ge Kewei You, Xunkun Han, Junfang Wang QiuwenYou and Asad Naeem Shah (2009), “Comparison of carbonyl compounds emissions from diesel engine fueled with biodiesel and diesel”, Atmospheric environment, vol.(43) 3657-3661.

- L.M. Geng D.H. Qi, H. Chen, Y.ZH. Bian, J. Liu and X.CH. Ren (2009), “Combustion and performance evaluation of a diesel engine fueled with biodiesel produced from soybean crude oil”, Renewable energy, vol. (34); 2706-2713.

- B.H.Hameed, C.S.Goh, and L.H.Chin (2009), “Process optimization for methyl ester production from waste cooking oil using activated carbon supported potassium fluoride”, Fuel Processing Technology, vol.(90); 1532-1537.

- Katherine M. Richard Stuart McTavish (2009), “Impact of Biodiesel on Lubricant Corrosion Performance”,Fuels and Lubricant, vol. 2(2);66-71.

- L. Díaz-Ballote, J.F. López-Sansores, L. Maldonado-López and L.F. Garfias-Mesias (2008), “Corrosion behavior of aluminum exposed to a biodiesel”, Corrosion Science, vol.(11); 41-44.

- Yoge Di, C.S.Cheung, and zuohu Huang, (2008), “Comparison of the effect of biodiesel-diesel and ethanol-diesel on the gaseous emission of a direct injection diesel engine”, Aerosol science and technology, vol. 43(5);455-465.

- S.Papavinasm, Alex Doiron, Tharani Panneerselvam and R. Winston Revie (2008), “Effect of hydrocarbons’ on the internal corrosion of oil and gas pipelines”Corrosion,vol.(47);635-644.

- Y.C.Sharma, B.Bosingh, and S.N.Upadhyay (2008), “Advancements in development and characterization of biodiesel”, Fuel, vol. (87);2355-2373.

- Hanbay Hazar (2008), “Effect of biodiesel on low heat loss diesel engine”, Renewable energy, vol. ( 34);1533-1537.

- Ana Maria de Oliveira, Rezende Michelle J. C, Serpa Da Cruz Rosenira Torres Ednildo A. DeAndeade Jailson B. (2007), “Comparative Study of the Effect of Biodiesel and Diesel Fuel on a Compression Ignition Engine’s Performance, Emissions, and Its Cycle by Cycle Variations”, Energy fuel, vol. 26(6);3627-3636.

- A.P. Roskilly, S.K. Nanda, Y.D. Wang and J. Chirkowski (2007), “The performance and the gaseous emissions of two small marine craft diesel engines fuelled with biodiesel”, Fuel Processing Technology, vol. (28); 872-880.

- Xiangmei Meng,(2007), “biodiesel production from waste cooking oil alkali catalyst and its engine test”, Fuel Processing Technology,vol.(89);851-857.

- N.H.Jayadas, K.Prabhakaran Nair.g, and K.Mohanan pillai (2007), “Evaluation of the oxidative properties of vegetable oil as base stocks for industrial lubricants using spectroscopic and the thermo gravimetric analysis”, Synthetic Lubrication, vol. ( 25); 105-113.

- Zheng ji-lu, (2006), “Bio-oil from fast pyrolysis of husk; Yield and related properties and improvement of the pyrolysis system”, Analytical and applied pyrolysis, vol 80(1); 30-35.

- Savita Kaul, R.C.Saxena, Ajaykumar, and  M.S Nigi, (2006), “Corrosion behavior of biodiesel from seed oils of Indian origin on diesel engine part”, Fuel processing Technology, vol.( 88); 303-307

- Mangesh G.Kulkarni, and Dalaiajay, (2006), “Waste cooking oil an economical source for biodiesel”, Industrial & Engineering Chemistry Research, vol. 45 (0888-5885); 2901-2913.

- S.Murillo, J.L.Miquez, J.Porterio, E Granada and J.C.Moran (2006), “Perfomance and exhaust emissions in the use of biodiesel in out board diesel engines”, Fuel Technology, vol. (86), 1765-1771.

- Yung chee Liang,(2005), “The effect of natural and synthetic antioxidant on oxidative stability of palm diesel”,Fuel,vol.(85);867-870.

- Sandum Fernando, Prasanth Kaera, Sarojkumar, Rafase and Hernanvez,(2005), “Effect of incompleted converted soy bean oil in biodiesel quality” , Energy ,vol. (32); 844-851.

- W.Yuan , A.C.Hansen, and Q.Zhang (2005), “Vapour pressure and normal boiling point predictions for pure methyl esters and biodiesel fuels”, Fuel Technology vol.( 84);943-950.

- D.Q.peng , X.D.Bai, F Pan, H.Sun and B.S. Chen(2004), “Corrosion behavior of carbon implanted  M5 alloy in 1M H2SO4”, Mettalography , vol.23 (1) ; 21-26.

- J. Kaminski R. Sitek Marcin Pisarek, Hubert Matysiak, Krzysztof and J. Kurzydłowski, (2003), “Comparative corrosive characteristics of petroleum diesel and palm biodiesel for automotive materials”, Fuel Processing Technology, vol. (91); 1308-1315.

- N.H.Jayadas, K.Prabhakaran Nair.g, and K.mohanan pillaI (2003), “Vegetable oils as a potential cutting fluid—An evolution”, Tribiology International, vol. (43), 1073-1081.

- Chaur-Jeng Wang and Jenq-Yith Pan (2003), “Corrosion of carbon steel with NaCl coating in an atmosphere produced by burning emulsified diesel oil”, Materials chemistry and physics, vol.( 82); 965-973.

- S.S,Abd Rehim Mohammed A. Amin, and Hesham T.M. Abdel-Fatah, (2002), “Electrochemical frequency modulation and inductively coupled plasma atomic emission spectroscopy methods for monitoring corrosion rates and inhibition of low alloy steel corrosion in sulphuric acid solutions and a test for validity of the Tafel extrapolation method”, Corrosion science, vol.(51); 882-889.

- M.A Maleque., H.H.Majuuski and A.M.S.A.Haseeb,(2002), “Effect of mechanical factors on tribiological properties of palm oil methyl ester blended lubricant”, Wear, vol. 239(1); 117-125 .

- J.W.Goodrum, Geller, D.P., T.T. Adams, J. Pendergrass (2001), “Volatility and boiling points of biodiesel from vegetable oil and tallow”, Biomass and Bioenergy, vol.(22); 205-211.

- M.A Maleque. H.H.Majuuski , A.Kuba and T.Nonaka, (2000), “Palm oil and mineral oil based lubricants-their tribiological and emission performance”, Tribiology intermational, vol .132(6); 305-314.

- H.H.Majuuski Maleque. M.A, and A.M.S.A.Haseeb(2000), “Effect of mechanical factors on tribiological properties of palm oil methyl ester blended lubricant”, Wear, vol. 239(1); 117-125

- H.H.Masjuki, M.A.Kalam, (1999), “Biodiesel from palm oil-an analysis of its properties and potential”, Biomass and Bioenergy, vol.23(2002); 471-479.

- Jan Cvengros and Frantisek Povazanec, (1996), “production and Treatment of Rape seed oil Methyl Ester as alternative fuels for Diesel Engines”, Bioresource Technology, vol.( 55);145-152