STRUCTURAL AND OPTICAL CHARACTERIZATION OF TiO2 THIN FILM DEPOSITED BY SILAR METHOD

BY

S.SARANYA

(09PHS10)

A dissertation submitted to the

AVINASHILINGAM DEEMED UNIVERSITY FOR WOMEN

COIMBATORE-641043

In partial fulfilment of the requirements for the degree of

MASTER OF SCIENCE IN PHYSICS

APRIL-2011.

STRUCTURAL AND OPTICAL CHARACTERIZATION OF TiO2 THIN FILM DEPOSITED BY SILAR METHOD

BY

S.SARANYA

(09PHS10)

A dissertation submitted to the

AVINASHILINGAM DEEMED UNIVERSITY FOR WOMEN

COIMBATORE-641043

In partial fulfilment of the requirements for the degree of

MASTER OF SCIENCE IN PHYSICS

APRIL-2011.

Certified as a bonafied research work

Signature of                                                         Signature of the Head of the department                                               Guide

ACKNOWLEDGMENT

Develop an attitude of gratitude, and give thanks for everything that one achieves knowing that every steps forward is a step towards achieving something bigger than you current situation.

First and foremost I acknowledge the abundant grace and presence of “Lord Almighty” through the different phases of my project and its successful completion.

I extent my deep heartfelt attitude and profoundsence of gratitude to Dr. (Thiru) MeenakshisundramM.A, M.Phil., Ph.D., Chancellor,

Avinashilingam Deemed University for Women, Coimbatore, for providing opportunity to expose myself to the world of knowledge.

I express my sincere thanks to Dr. (Tmt) Sheela Ramachandran, M.Sc.,P.G.Dip.,Ph.D.,(Avinashilingam),Vice Chancellor, Avinashilingam Deemed University for Women, Coimbatore, for the timely help rendered to complete the project successfully

I record my special thanks to Dr. (Tmt) Gowri Ramakrishnan, M.Sc., (Madras), M.Phil., Ph.D., (Avinashilingam), Registrar, Avinashilingam Deemed University for Women, Coimbatore, for providing all the administrative support and help required to carry out the project

I render my auspicious gratitude to Dr.(Tmt)R.Parvatham, M.Sc.,Dip.Ed.,M.phil.,(Madras)Ph.D.,(Avinashilingam),Dean, Faculty of science, Avinashilingam Deemed University for Women, Coimbatore, for her valuable support.

I gratefully record my sincere, special and heartfelt sence of thanks to Dr. (Tmt) Saroja Prabhakaran, M.A., Dip. Ed. (Madras), Ph.D., (Mother Teresa) the Director Hall of   Residence, Avinashilingam Deemed University for Women, Coimbatore, for facilities provided and constant encouragement to complete the research work.

I express my heartfelt and reverential sence of gratitude to my guide Dr. (Tmt) RachelOommen, M.Sc. (Kerala), Dip.Ed. (Madras), B.Ed. (Annamalai),M.phi.l,Ph.D.,(Bharathiar),professor and Head of the Department of Physics, Avinashilingam Deemed University for Women, Coimbatore, for her constant encouragement, discussion and guidance. Her keen interest and ever-welcoming attitude towards attending to problems paved way for newer ideas and successful completion of my research work

I owe my sincere thanks to all the staff members of the Department of physics, Avinashilingam Deemed University for Women, Coimbatore, for being supportive and understanding.

I am very much thankful to all my friends for their support, understanding and co-operation for the successful completion of the study.

No words are sufficient to express my deep sence of gratitude to my family for their affection, care and co-operation in all walks of my life.

S.SARANYA

CONTENT

CONTENT

LIST OF TABLES

LIST OF FIGURES

LIST OF PLATES

CHAPTER I

INTRODUCTION

1. THIN FILM

1.1 Properties of thin film………………………………………………. ..1

1.2 THIN FILM DEPOSITION TECHINIQUE

    - Physical method……………………………………………. ……..... 2

1.2.2    Chemical method……………………………………………………. 3

1.2.2.1 Chemical bath deposition……………………………….. ..3

1.3 APPLICATION OF THIN FILM……………………………………………... 4

1.4 TITANIUM DIOXIDE

1.4.1 Properties of titanium dioxide………………………………………...6

1.4.2 Titanium dioxide as photo catalyst…………………………………... 7

1.4.3 Application of titanium dioxide………………………………………. 7

OBJECTIVE………………………………………………………………………. 8

CHAPTER II

REVIEW OF LITERATURE………………………………………………… 9

CHAPTER III

3.1 MATERIALS USED………………………………………………………....   24

3.2 DEPOSITION OF TIO2 THIN FILM

3.2.1 Choice of the substrate………………………………………………….25

3.2.2 Requirements of substrate………………………………………………26

3.2.3 Substrate cleaning……………………………………………………….27

3.2.4 Chemical bath deposition……………………………………………… 26

3.2.5 SILAR…………………………………………………………………   27

3.2.6 Preparation of TiO2 thin film…………………………………………   26

3.3 THICKNESS MEASUREMENT

3.3.1 Gravimetric method……………………………………………………   28

3.4STRUCTURAL CHARACTERIZATION

3.4.1 X-ray diffraction………………………………………………………… 30

3.4.2 Theory of Bragg’s law…………………………………………………    30

3.4.3 Structural parameters……………………………………………………  31

3.5 OPTICAL CHARACTERIZATION

3.5.1 Ultraviolet and visible spectroscopy……………………………………… 32

3.5.2 Optical parameters………………………………………………………… 34

CHAPTER IV

4.1 NATURE OFTHINFILM………………………………………………………...42

4.2 OPTICAL CHARACTERIZATION

4.2.1 Transmittance………………………………………………………………        42

4.2.2 Absorbance…………………………………………………………………        43

4.2.3 Extinction co-efficient…………………………………………………….          43

4.2.4 Absorption co-efficient………………………………………………………      43.

4.2.5 Bandgap………………………………………………………………………     44

CHAPTER V

SUMMARYANDCONCLUSION………………………………… ………………..63

BIBLIOGRAPHY…………………………………………………………………… 64

LIST OF TABLES

| TABLE NO | TITLE | PAGE NO |
| --- | --- | --- |
| 3.1 | #### Deposition Conditions | 37 |
| 4.1 | Deposition Condition With Thickness For Sample1,Sample2, Sample3 | 45 |
| 4.2 | Maximum Absorption Co-Efficient Of Ti2 Film For Sample1, Sample2, And Sample3 | 46 |
| 4.3 | Relationship between Band gap and Thickness | 47 |

LIST OF FIGURES

| FIGURE NO | TITLE | PAGENO |
| --- | --- | --- |
| 3.1 | XRD Experimental Setup | 38 |
| 3.2 | Bragg’s X-Ray Diffraction | 39 |
| 3.3 | UV-Vis Spectrophotometer | 40 |
| 4.1 | Variation Of Transmittance With Wavelength Of TiO2 Thin Film(Sample 1) | 48 |
| 4.2 | Variation Of Transmittance With Wavelength Of TiO2 Thin Film(Sample 2) | 48 |
| 4.3 | Variation Of Transmittance With Wavelength Of TiO2 Thin Film(Sample 3) | 49 |
| 4.4 | Variation Of Absorbance With Wavelength Of TiO2 Thin Film (Sample 1) | 50 |
| 4.5 | Variation Of Absorbance With Wavelength Of TiO2Thin Film (Sample 2) | 50 |
| 4.6 | Variation Of Absorbance With Wavelength Of TiO2 Thin Film (Sample 3) | 51 |
| 4.7 | Variation Of Extinction Coefficient With Wavelength Of TiO2 Thin Film (Sample 1) | 52 |
| 4.8 | Variation Of Extinction Coefficient With Wavelength Of TiO2 Thin Film (Sample 2) | 52 |
| 4.9 | Variation Of Extinction Coefficient With Wavelength Of TiO2 Thin Film (Sample 3) | 53 |
| 4.10 | Variation Of Absorption Coefficient With Wavelength Of TiO2 Thin Film (Sample 1) | 54 |
| 4.11 | Variation Of Absorption Coefficient With Wavelength Of TiO2 Thin Film (Sample 2) | 54 |
| 4.12 | Variation Of Absorption Coefficient With Wavelength Of TiO2 Thin Film (Sample 3) | 55 |
| 4.13 | Variation of (αhv)2 with photon energy hv(ev)of TiO2 thin film of thickness 0.3472μm(sample ) | 56 |
| 4.14 | Variation of (αhv)2 with photon energy hv(ev)of TiO2 thin film of thickness 0.52μm(sample 2 ) | 56 |
| 4.15 | Variation of (αhv)2 with photon energy hv(ev)of TiO2 thin film of thickness 0.80μm (sample 3) | 57 |
| 4.16 | Variation of (αhv)1/2 with photon energy hv(ev) of TiO2 thin film of thickness 0.3472μm (sample 1) | 58 |
| 4.17 | Variation of (αhv)1/2 with photon energy hv(ev) of TiO2 thin film of thickness 0.52μm (sample 2) | 58 |
| 4.18 | Variation of (αhv)1/2 with photon energy hv(ev) of TiO2 thin film of thickness 0.80μm (sample 3) | 59 |
| 4.19 | Variation Of Thickness With Immersion Time Of TiO2 Thin Film (Samples 1, 2, 3) | 60 |
| 4.20 | Variation Of Band Gap With Thickness Of TiO2 Thin Film Direct (Samples 1, 2, 3) | 60 |
| 4.21 | Variation Of Band Gap With Thickness Of TiO2 Thin Film Indirect (Samples 1, 2, 3) | 61 |  |
| 4.22 | X-ray diffraction pattern of TiO2 thin film (without annealing) | 62 |  |

LIST OF PLATES

| PLATES NO | TITLE | PAGE NO |
| --- | --- | --- |
| 3.1 | DEPOSITION OF TiO2 THIN FILM BY SILAR METHOD | 41 |

CHAPTER 1

INTRODUCTION

THIN FILM:

The term “thin film” has often been loosely used in literature to imply not only a layer of a solid material but also of a liquid or a gaseous phase [1].Thin film science and technology is one of a the oldest art and modern science. The need for new and improved opto- electronic devices has stimulated a branch of solid state physics called thin film physics and technology which comprises the study and application of thin film. Thin film technology stretches its hands in all almost all direction. Thin film science and technology play an important role in the high-tech industries and has been developed primarily for the need of integrated circuit industries [2].All basic researchers on thin film are generally confined to a limited range of thickness say between few A₀ to about 5000 A₀depending on the properties [1].The demand for  development of smaller and smaller devices with high speed ,especially in new generation of IC, requires advanced materials and new processing technique suitable for future Giga Scale integration(GIS) technology[2].The technology  of thin film plays an important role to achieve this  goal.

Thin film as a two dimensional system is of great importance to many real world problems. Thin film technology is based on three foundations,

- Fabrication

- Characterization

- Application

1.1 PROPERITIES OF THINFILM:

The properties of thin films are different from the properties of corresponding bulk  materials  because of their small thickness, large surface to volume ratio and unique physical structure[3].

Thin film properties are mainly dependent on,

- Rate of deposition

- Substrate temperature

- Environmental condition

- Residual gas pressure in the system

- Purity of the material to be deposited.

- In homogeneity of the film.

- Structural and compositional variation of the film in localized or wider areas.

1.2. THIN FILM DEPOSITION TECHNIQUE:

Thin film can be prepared from a variety of materials such as Metals, semiconductors, insulators or dielectrics etc, and for this purpose various preparation techniques have been employed [4,5]. The deposition techniques and its associated process parameters have a characteristic effect on the nucleation and growth dominated micro structure of a thin film and thereby on it physical properties [6].

A thin film deposition process involves three steps,

- Creation of atomic/molecular/ionic species

- Transport of these species through a medium

- Condensation of the species on a substrate

Depending on whether the vapour species have been carried by physical, chemical and electro chemical process, the deposition process can be broadly classified into two main groups, namely physical method and chemical method.

1. 2.1 PHYSICAL METHOD:

The most important physical methods for preparation of thin films are as follows.

      - Vacuum evaporation

      - Sputtering technique.

      - Pulsed laser deposition

      - Electro hydrodynamic deposition [6].

1.2.2 CHEMICAL METHOD:

Chemical methods are commonly preferred for obtaining large area thin films. This method depends on the deposition of films from aqueous solutions either by passing a current or by chemical reactions under appropriate conditions and is generally used for the deposition of thick metallic or alloy films. By the very nature of their preparative conditions these films are not generally of high purity. Despite this limitation, this technique is widely used for the fabrication of conducting connectors, magnetic memory elements,etc.with an appropriate control on the deposition parameters such as bath composition,temperature,pH,current density,etc.metallic  deposits and even alloys of definite composition can be obtained. The chemical methods are divided into several types.

      - Chemical vapour deposition

      - Electro- less deposition

      - Anodic oxidation

      - Spray pyrolysis

      - Chemical displacement

      - Cathodic  deposition

      - Chemical bath deposition[6]

1.2.2.1 CHEMICAL BATH DEPOSITION:

Chemical bath deposition is an inexpensive and convenient method for large area preparation of thin films at close to room temperature. Chemical bath deposition is also known as chemical solution deposition. It was first described in 1869 and it has been used since than to deposit films of many different semiconductors.Chemical depositions refers to the deposition of films on a solid substrate from a reaction occurring in a solution. Chemical solution is based on the precipitation or electro- less process in solution. While the application of chemical solution deposition for the growth of electronic materials has been known for a long time and deposition of numerous chaleogenide semiconductors has been demonstrated, its development has remained very limited until recently.

In principle, chemical bath deposition can be used to deposit any compound that            satisfies four basic requirements.

- The compound can be made by simple precipitation. Generally although not exclusively, refers to the formation of a stoichoimetric compound formed by ionic reaction.

- The compound should be relatively insoluble in the solution used.

- The compound should be chemically stable in the solution.

- If the reaction proceeds via the free anion, then this anion should be relatively slowly generated (to prevent sudden precipitation) [7].

1.3. APPLICATIONS OF THIN FILM:

Thin film science now covers a wide span of displine such as solid state physics, surface science, crystallography, crystalgrowthprocess, optics, electronics, material science,etc.These investigation led to numerous invention in the form of active devices and passive components,piezoeletric devices,microminiaturation of power supply, rectification and amplication,sensor elements, storage of solar energy and its conversion to other form, magnetic memories, super conducting films,interferance filters, reflection and antireflection coating and other. In the field of science and techonology.we always require “miniature” of components. Only because of the miniature of components, high technical devices like laptop computer and two dimensional TV screens are possible today.

Thin film application could be clustered into two main groups.

- High –tech

- Medium-tech

The possibility of transferring specific or expensive properties to a nanometer-sized coating makes the list of potential applied almost endless and could have an impact in every industrial sector. As research in nanotechnology develops, new characterization and production tools, new materials and process models as well as more computational power will become available which in turn boosts thin film application future.

There’s a fierce worldwide competition in application related with semiconductor. In earlier days, scientific interest in thin solid films was centered on anti reflection coating for lenses, multilayer interference filters, anti mobile headlights and decorative coatings, ceramics and sun glasses, front surface mirror etc., [4].

Thin film solar cells are a good competitor for the single crystal and poly crystalline silicon solar cells because of the availability of cheaper raw materials as well as processing cost. Thin films have attracted great attention in recent years for their potential use in dynamic RAMS and Multi Chip Module (MCM) due to their high dielectric constant and relatively low leakage current.

Most of the thin film applications deal with the development in the semiconductor industry like transistor, Micro Electro-Mechanical Systems(MEMS) planer wave guides(for optical component integration) Non volatile Memory(M-RAM) and in the other relevant application like Anti-scratch coating(in automotive and optical components),coating for antiglare, anode and cathode materials(batteries,capactiors and superconductors)[8].

The optical industry has been using thin film coatings in components like prisms, filters, lenses, reflectors or mirrors. According to experts the lack of understanding of industrial requirements is considered a bottleneck for all materials being researched. This is especially relevant because thin films are a part of material system and should be integrated with other systems. Thus for all of them, there’s plenty of rooms for improvement and development of thin film device application [4].

1.4. TITANIUM DIOXIDE:

Titanium dioxide is a hard material, chemically resistant and transparent in the visible and infrared region with high refractive index. It occurs in three different crystalline forms –rutile, anatase and brookite of which is a naturally occurring compound. It is widely applied in thin film form as electro chromic devices, gas sensors, and hard coating and high index optical coatings. Titanium dioxide attracts much attentation in its remarkable physical and chemical properties. Today, titanium dioxide pigment is by far the most important material used by the paints and plastics industry for whiteness and opacity.  It gives paint high hiding power, meaning the ability to mask or hide a substrate. It does this more effectively than any other white pigment. These unique properties are derived from the refractive index of titanium dioxide. The refractive index expresses the ability to bend and scatter light. Titanium dioxide has the highest refractive index of any material known to man, greater than even diamond. Thin film of titanium dioxide were prepared using many deposition techniques such as reactive evaporation,DC magnetron sputtering ,RF sputtering chemical bath deposition, chemical vapor deposition, electron beam evaporation, sol-gel process[9].Titanium metal is important for its strength, low density and corrosion resistance. Therefore titanium has been called” the wonder metal “because of its unique and useful properties [10].

1.4.1. PROPERITIES OF TITANIUM DIOXIDE:

    - Titanium dioxide is a semiconductor and optically transparent in the visible region.

    - Films made of loosely packed anatase particle. Particle size range from 10nm   to100nm.

    - Highly porous material that provides strong enhancement of the surface area(100 times)

    - High affinity of titanium dioxide surface too many molecules (e.g.; dyes) leads to easy surface modification.

    - Low cost material, easy to produce in large quantities chemically inert, non-toxic,        biocompatible [11].

1.4.2 TITANIUM DIOXIDE AS PHOTOCATALYST:

The work of semiconductor photo catalysis was started in the year of 1972 by A.Fujishima and K.Honda with the study of the splitting of the water on the titanium electrode under the ultra violet (UV) light.Titaniumdioxide have been extensively investigated as heterogeneous semiconductor photocatalysts.Since titanium dioxide offers several advantages such as the use of oxygen as the only required oxidant and their capability to simultaneously carry out oxidative and reductive reactions. Titanium dioxide is also known as a good photo-catalyst for the degradation of several environmental contaminants due to its high photosensitivity, stability and large band gap. In addition, titanium dioxide is an environmentally friendly material that does not form toxic byproducts [12].

1.4.3 APPLICATIONS OF TITANIUM DIOXIDE:

    - The use of titanium dioxide in self–cleaning glass. Free radicals generated from titanium dioxide oxidize organic matter.

    - Disinfection of water by titanium dioxide photo catalysis.

    - Oxidation of organic contaminations using magnetic particles that are coated with titanium dioxide nanoparticles and agitated using a magnetic field while being exposed to UV light.

    - Conversion of carbon dioxide into gaseous hydrocarbons using titanium dioxide in the presence of water.

    - Sterilized surgical instruments and remove unwanted finger prints from sensitive electrical and optical components.

    - Decomposition of crude oil with titanium dioxide nanoparticles.

    - Titanium dioxide is also used as a material in the memristor, a new electronic circuit element. It can be employed for solar energy conversion based on dye, polymer, or quantum dot sensitized nanocrystalline TiO2 solar cells using conjugated polymers as solid electrolyte.

    - Synthetic single crystals and films of TiO2 are used as a semiconductor, and also in Bragg-stack style dielectric mirrors due to the high refractive index of TiO2.

    - TiO2 offers great potential as an industrial technology for detoxification or remediation.

    - In cosmetic and skin care products, titanium dioxide is used as a pigment, sunscreen and a thickener. It is also used as a tattoo pigment and in styptic pencils. Titanium dioxide is produced in varying particle sizes, oil and water dispersible, and with varying coatings for the cosmetic industry. This pigment is used extensively in plastics and other applications for its UV resistant properties where it acts as a UV absorber, efficiently transforming destructive UV light energy into heat.

OBJECTIVE:

Among the various deposition techniques chemical bath deposition is a simple and large area coating technique, for the preparation of titanium dioxide thin films. In the present study, it has been proposed to probe this material in terms of some of its basic properties such as optical and structural studies.

CHAPTER-II

REVIEW OF LITERATURE

INTRODUCTION:

Review of literature is a comprehensive and extensive examination of several research works done by many researches on a selected field. The survey of past and ongoing research on Tio2 thin films will give better understanding of the preparation of materials and its synthesis and characterization. Many researchers have developed and characterized thin film of Tio2 owing to its wide application in numerous fields. In this chapter, a survey on various preparation techniques and its characterization is carried out.

2.1 STUDY ON TiO2THIN FILMS BY DIFFERENT DEPOSITION TECHINIQUE:

José A. Ayllón et al., (2004) identified MW-CBD as a low-temperature deposition technique that gives transparent and well-adhered TiO2 thin films. TiO2 films on transparent conducting oxide are important for dye-sensitized solar cells, extremely thin absorber solar cells and for electrochromic devices. They studied study how the growth process of TiO2 films using MW-CBD is influenced by substrate type using SnO2:F and ITO substrates. Crystallinity of the films is mainly determined by the precursor solution rather than by the substrates studied, though morphology of the substrate influences the morphology of the films. Using the SnO2:F substrate more texturized TiO2 films grow. All films showed photovoltaic behavior. Current near short-circuit current in the I–V characteristic are within experimental uncertainty for films obtained on different substrate type but with the same precursor solution. Films obtained on SnO2:F with the precursor solution based on fluorine-complexed titanium(IV) exhibit the best results. In this case, open-circuit photovoltage increases appreciably [13].

Roberto Gómez et al.,(2004) have performed a spectro- and photoelectrochemical study of electrodes consisting of oriented rutile TiO2 nanowires with a diameter of 2 nm prepared directly by chemical bath deposition on conducting glass. A significant increase (around 0.25 eV with respect to bulk rutile) of the band gap energy for the nanowire film is observed and attributed to quantum size effects, pointing to the presence of individual monocrystalline nanowires with no significant electronic communication among them. This allows for the investigation of morphologically well defined electrodes in the two dimensional quantum confinement regime, which are characterized by particularly good photoelectrocatalytic and electrochromic properties [14].

Kwang-Leong et al., (2004) have investigated TiO2 as one of the best candidates for gas sensing because of its low cost, stable phase even at high temperature, higher gas sensitivity and comparable thermal expansion coefficient to alumina substrate. Further improvement in the performance can be achieved by addition of trivalent or pentavalent dopants. Recently, a novel electrostatic spray assisted vapour deposition (ESAVD) technique has been developed in our laboratory to prepare thin or thick films of various materials. This method offers many advantages over several conventional deposition techniques including a simple set-up, inexpensive and nontoxic precursor, high deposition efficiency and easy control of the surface morphology of the deposited films and excellent control of stoichiometry. The possibility of morphology control is of particular interest for gas sensor application since the surface is primarily involved in the initial sensor/gas interaction. In this work, the structural and morphological characterization of TiO2-based films incorporated with Cr, Nb metal ions deposited by EASVD have been studied. Scanning electron microscopy (SEM) was used to analyze the microstructural and morphological properties. The X-ray diffraction (XRD) and Energy dispersion X-ray (EDX) analysis of SEM were employed to determine the crystal phase and film composition. X-ray photoelectron spectroscopy (XPS) was used to identify the surface chemical stoichiometry of the deposited films [15].

Jin-Hyo Boo et al., (2005) have grown Titanium dioxide (TiO2) thin films on Si(100) and micro cover glass substrates using radio frequency (RF) magnetron sputtering. Highly oriented, crack-free, stoichiometric polycrystalline rutile TiO2 thin film was obtained after annealing at 1000 °C for 1 h. The maximum UV-visible transmittance and hardness of the film were over 90% and 1700 HK0.025, respectively. Different contact angles and crystal growth directions were observed with the various deposition parameters such as annealing temperature, RF power magnitude, and added O2 amounts. These differences were dependent on a phase transition from anatase to rutile phases, reflecting the changes of the crystal structure. In this study, moreover, we found that the transmittance and hardness of the TiO2 thin films were strongly influenced by both the film thickness and the surface roughness. The growth rate was also increased with increasing RF power up to 150 W, and the maximum growth rate observed at 150 W was 1500 nm/h. The most optimum deposition condition for TiO2 thin film growth was determined to be 80 W of RF power, 1000 °C of annealing temperature, 1 h of deposition time, and 30 sccm of O2[16]

CdSe is homogeneously deposited into nanoporous TiO2 films and used in liquid junction photoelectrochemical solar cells by Shaibal K. Sarkar et al.,(2006).The effect of the deposition parameters on the cell are studied, in particular differences between ion-by-ion and cluster deposition mechanisms. CdSe deposition on a Cd-rich CdS film that was deposited first into the TiO2 film, or selenization of the Cd-rich CdS layer with selenosulphate solution improves the cell parameters. Photocurrent spectral response measurements indicate photocurrent losses due to poor collection efficiencies, as shown by the strong spectral dependence on illumination intensity. Cell efficiencies up to 2.8% under solar conditions have been obtained [17].

Titanium dioxide (TiO2) thin films resembled with TiO2 nanoparticles and oppositely charged polyelectrolytes or titanium (IV) bis(ammonium lactato) dihydroxide (TALH) were successfully fabricated via a layer-by-layer (LBL) self-assembly method at room temperature by Jin-Ho Kim etal.,(2006). Especially, by using the quartz crystal microbalance (QCM) to monitor the in-situ deposition phenomenon of TALH that is saturated and then separated from the film before and after the deposition of 30 s at low pH, the anatase TiO2 multilayer films fabricated with 30 s deposition in TALH adjusted to pH 2.5 showed a higher refractive index (ca. n = 1.75), a denser film growth, and a lower surface roughness (ca. 10.5 nm) than those of the films deposited in different conditions. This film showed a high transmittance in visible range for optical applications and photocatalytic properties by decomposing methyl orange molecules gradually according to UV irradiation time. In addition, as the pH of TALH was decreased from pH 5.5 to 2.0, the thickness of (TiO2 / TALH)30 film was increased from ca. 85 nm to ca. 442 nm[18].

Oh-Shim Joo et al., (2006) have described successive ionic layer adsorption and reaction (SILAR) is a process for depositing uniform, crystalline and conformal thin films by alternating exposures to cations and anions. SILAR has been successfully demonstrated for many metal oxides, but not for titanium dioxide (TiO2). Here we demonstrate process for deposition of TiO2 thin films using SILAR method. Titanium tri-chloride and ammonium hydroxide were used as cationic and anionic sources, respectively. Their surface reactions were found to be complementary and self-limiting, thus providing compact, uniform films with control over thickness of the film. The preparative conditions were optimized to get good-quality TiO2 thin films. The films have been characterized for structural, morphological, compositional, optical and photo-response properties. Growth process, reaction mechanism and annealing effect are also discussed [19].

Thin films of TiO2 doped by Ni non-uniformly were prepared by a modified dip-hoisting process of sol–gel method by Wei Xu et al.,(2006).The transmittance, absorbency, photocurrent and open-circuit potential of the thin films were studied by UV–vis spectrophotometer and electrochemical workstation. The activity of thin films was characterized by photocatalytic degradation of aqueous methyl orange under UV irradiation. The results showed that the photocatalytic activity of TiO2 thin films can be remarkably enhanced by Ni non-uniformly doping compared with the pure ones, while that of the uniformly doped can only be improved a little. The transmittance of the TiO2 thin films doped by Ni uniformly and non-uniformly doping showed “blue shift” and “red shift”, respectively. The absorbency of the non-uniformly doped extended to “red shift”. Under UV irradiation, the non-uniformly doped TiO2 thin films show higher open-circuit potential and photocurrent compared with that of the pure ones, which demonstrated that the photogenerated electron–hole pairs were effectively separated. And the electrode bias influenced the photocurrent of Ni non-uniformly doped TiO2 thin films greatly, which verified the structure of p–n junction. The photocatalytic activity mechanism of the non-uniformly doped TiO2 was discussed by p–n junction theory [20].

M.F. Hossain et al.,(2008) have synthesized CdS–TiO2 thin film heterojunctions on glass and indium tin oxide (ITO) substrates with the aim of improving photocatalytic efficiency both in UV–visible and visible light irradiation. The CdS under-layers were prepared by chemical bath deposition technique and subsequently they were annealed in the high vacuum of 5 × 10− 5 Pa at the temperature of 400 °C. The structural and optical properties of all the CdS–TiO2 thin films were studied with the help of X-ray diffractometer, atomic force microscope and ultraviolet–visible spectrophotometer. The photocatalytic activity of the thin films was evaluated by the decomposition of methanol by the use of fourier transform infrared spectrophotometer. It is revealed that the use of ITO substrate and high-vacuum annealing after deposition significantly enhance photocatalytic activity[21].

Jingdong Zhang et al., (2008) have described the preparation of the Titanium Dioxide (TiO2) Films on Glassy Carbon (GC) Electrode Surface by the Liquid Phase Deposition (LPD) Process for Different Deposition times.The Morphological Structure, Interfacial Property and Electrocatalytic Activity of as-prepared LPD TiO2 Films on GC Surface were studied by field-emission Scanning Electron Microscopy (FE-SEM), Cyclic Voltammetry (CV) and Electrochemical Impedance Spectroscopy (EIS). the FE-SEM Observation Showed that the Deposition Time Controlled the Morphology of Film on GC surface. with Increasing Deposition Time, TiO2 Formed Nanoparticles at the Initial 5-h Stage and Compact Thick Films after 20 h. Due to the Semiconducting Properties of TiO2, the LPD Films Inhibited the Electron Transfer Process of [Fe(CN)6]3-/[Fe(CN)6]4- on GC by Increasing the Redox Reaction Peak Potential Separation of CV Curve and Electron Transfer Resistance of EIS. the Inhibition was Increased with TiO2 Film thickness. Nevertheless, the Onset Reduction Potential of Maleic Acid Decreased with Increasing LPD TiO2 Film Thickness while the Cathodic and Anodic Currents Increased, Demonstrating the Useful Electrocatalytic Activity of LPD TiO2 films [22].

Noor Shahina Begum et al., (2008) have analyzed a transparent, high purity titanium dioxide thin film composed of densely packed nanometer sized grains, successfully deposited on a glass substrate at 30°C from an aqueous solution of TiO2–H with the addition of boric acid as a scavenger by liquid phase deposition technique. From X-ray diffraction measurement, the deposited film was found to be amorphous and turns crystalline at 500°C. The deposited film showed excellent adherence to the substrate and was characterized by homogeneous flat surface. TiO2 thin films can be used as a photocatalyst to clean up organohalides, a class of compound in pesticides that pollute the ground water. Photocatalytic degradation experiments show that indanthrene golden orange dye undergoes degradation efficiently in presence of TiO2 thin films by exposing its aqueous solution to ultraviolet light. The suitable surface structure and porosity increases the photocatalytic activity. It was also observed that hemin doped TiO2 thin films break up organohalides at a surprisingly high rate under visible light [23].

T.P. Gujar et al.,(2008) have fabricated TiO2 nanorods from the simple chemical bath deposition (CBD) method and characterized using X-ray diffraction, scanning electron microscopy (SEM), transmission electron microscopy (TEM), and optical absorption studies. The structural study revealed that TiO2 films retain amorphous structure even after annealing at 723 K. The SEM and TEM studies showed good substrate coverage consisting of TiO2 nanorods. The optical band gap declined from 3.4 to 3.3 eV after annealing, showing no significant change. Both as-deposited and annealed TiO2 films exhibit n-type electrical conductivity. As-deposited and annealed TiO2 films showed hydrophilic behavior as water contact angle [24].

J.A. Ayllón et al., (2009) have described that in traditional solar cells, metal-semiconductor contacts used to extract photogenerated carriers are very important. In dye-sensitized solar cells (DSSC) not much attention has been given to contact between the TiO2 and the transparent conducting glass (TCO), which is used instead of a metal contact to extract electrons. TiO2 layers obtained by microwave-activated chemical-bath deposition (MW-CBD) are proposed to improve TiO2 contact to conducting glass. Spectra of incident photon to current conversion efficiency (IPCE) are obtained for two-photoelectrode TiO2 photoelectrochemical cells. IPCE spectra show higher values when TiO2 double layer photoelectrodes are used. In these, the first layer or contacting layer is made by MW-CBD. Best results are obtained for double layer photoelectrodes on FTO (SnO2:F) as conducting oxide substrate. Modeling of IPCE spectra reveals the importance of electrical contact and electron extraction rate at the TiO2/TCO interface [25].

Funda sayilkan et al., (2009) synthesized Fe3+ ion-doped TiO2 particles by the hydrothermal process at 225 °C. Titanium isopropoxide (Ti(OPri)4) was used as precursor material. Both undoped and doped TiO2 particles were used to coat glass surface. The coated surface was examined with respect to their photocatalytic performance for degradation of Malachite Green (MG) dye in aqueous solution under UV and vis-light irradiation. The particles and the films were characterized by XRD, SEM and UV/vis/NIR techniques. The results showed that crystallite size of the hydrothermally synthesized TiO2 particles are in nanoscale. Anatase was only the crystalline phase. Doping of Fe3+ ion improved the photodegradation performance of TiO2 coated surfaces. Degradation performance of Fe3+ doped TiO2 coated surfaces determined under UV- and vis-irradiation conditions was higher than the undoped TiO2 coated surface. It was concluded that the photodegradation of 2.5 mg L−1 MG under UV-light irradiation with the catalysis of Fe3+-doped TiO2 follows the pseudo-first-order reaction kinetics with the rate constant of 0.0202 min−1[26].

Nanostructured TiO2 thin films were deposited on glass substrates by sol–gel dip coating technique by N.R. Mathews et al.,(2009). The structural, morphological and optical characterizations of the as deposited and annealed films were carried out using X-ray diffraction (XRD), Raman spectroscopy, atomic force microscopy (AFM), and UV–vis transmittance spectroscopy. As-deposited films were amorphous, and the XRD studies showed that the formation of anatase phase was initiated at annealing temperature close to 400 °C. The grain size of the film annealed at 600 °C was about 20 nm. The lattice parameters for the films annealed at 600 °C were a = 3.7862 Ǻ and c = 9.5172 Ǻ, which is close to the reported values of anatase phase. Band gap of the as deposited film was estimated as 3.42 eV and was found to decrease with the annealing temperature. At 550 nm the refractive index of the films annealed at 600 °C was 2.11, which is low compared to a pore free anatase TiO2. The room temperature electrical resistivity in the dark was of the order of 4.45 × 106 ohm-cm. Photocatalytic activity of the TiO2 films were studied by monitoring the degradation of aqueous methylene blue under UV light irradiation and was observed that films annealed above 400 °C had good photocatalytic activity which is explained as due to the structural and morphological properties of the films [27].

J.W.J.Hamilton et al.,(2009) have described Microwave activated chemical bath deposition (MW-CBD) as a simple and novel technique in which the substrate is heated directly by microwaves and very well adhered layers are obtained. It has not been used previously for TiO2 deposition on metals. They show that it is possible to coat stainless steel with TiO2 using MW-CBD. Two different precursor solutions are used for TiO2 deposition on steel grade 316. TiO2 thin films on steel substrates were characterized using SEM and Raman spectroscopy. Raman analysis showed that amorphous TiO2 is obtained using the precursor solution based on TiOSO4; however, films show anatase crystal structure when using the precursor solution based on (NH4)2TiF6. Thermal treatment of the films improved crystallinity and also allowed iron diffusion from the steel substrate into the film. Crystalline phases that appeared due to heat treatment were identified from Raman spectra. MW-CBD allows simple low temperature coating of a metal substrate with TiO2 and this should be useful for a number of different applications [28].

C.D. Lokhande et al., (2009) have deposited nano crystalline TiO2 thin films are deposited by simple successive ionic layer adsorption and reaction (SILAR) method on glass and fluorine-doped tin oxide (FTO)-coated glass substrate from aqueous solution. The as-deposited films are heat treated at 673 K for 2 h in air. The change in structural, morphological and optical properties are studied by means of X-ray diffraction (XRD), selected area electron diffraction (SAED), scanning electron microscopy (SEM), Fourier transform infrared (FTIR), transmission electron microscopy (TEM) and UV–vis–NIR spectrophotometer. The results show that the SILAR method allows the formation of anatase, nanocrystalline, and porous TiO2 thin films. The heat-treated film showed conversion efficiency of 0.047% in photoelectrochemical cell with 1 M NaOH electrolyte [29].

K. Prabakar et al., (2010) have prepared Visible light enhanced nitrogen–sulfur (N–S) doped titanium dioxide (TiO2) thin films by the sol–gel method using thiourea as a dopant. The physical and chemical properties of the TiO2 thin films were greatly influenced by the amount of thiourea added to the sol–gel solution. The greatest shift to longer wavelengths for visible light absorption was observed with 0.6 g of thiourea in the precursor solution, while 0.4 g yielded the largest particle sizes. These single-cycle dip-deposited N–S doped TiO2 thin films were used as visible light harvesters as well as blocking layers in dye sensitized solar cells. When deposited directly on conducting fluorine doped tin oxide electrodes, photo-conversion efficiencies were reduced. However, the opposite configuration, with N–S doped thin films on top of nanoporous TiO2, yielded an increased open-circuit voltage of 0.84 V, a short-circuit current density of 9.86 mA cm−2, and an overall conversion efficiency of 5.88% greater than that of a standard cell. The effectiveness of the blocking layer on the cell efficiencies was analyzed by electrochemical impedance spectroscopy [30].

TiO2 thin films were experimentally coated on glass beads by means of a rotating cylindrical plasma chemical vapor deposition (PCVD) reactor by Kyo-Seon Kim et al.,(2010). The morphologies and growth rates of the TiO2 thin films before and after heat treatment were measured for various process conditions. The precursors for the TiO2 films were generated from TTIP by plasma reactions, and they were deposited on the glass beads to become TiO2 thin films. The TiO2 thin films coated on the glass beads became more uniform by heat treatment. The TiO2 thin films grew more quickly on the glass beads with increasing mass flow rate of TTIP, reactor pressure, or rotation speed of the reactor. As the applied electric power decreases, the thickness of the thin films on the glass beads increases. This experimental study shows that the use of a rotating cylindrical PCVD reactor can be a good method to coat high-quality TiO2 thin films uniformly on particles [31].

Min Wook Pyun et al., (2010) have studied the Optical, Structural and Photocatalytic properties of TiO2 thin films obliquely deposited on quartz glass substrate using an electron-beam evaporation method were investigated. The photocatalytic activity of the films was evaluated by photodecomposition of methylene blue. An increase in incident deposition angle increased the porosity and surface roughness of the TiO2 films. As a result, the photocatalytic activity was enhanced with incident deposition angle up to 60°. However, a further increase in incident deposition angle to 75° reduced the photocatalytic activity due to a lack of the crystalline phase [32].

J. Hu et al., (2010) have investigated nanoporous TiO2 films, fabricated by thermal rapid treatment (TRT) of the TiO2 film which was previously deposited on a substrate by liquid phase deposition. The TiO2 films were characterized by X-ray diffraction (XRD), field emission scanning electron microscopy (FE-SEM), and UV-VIS diffuse reflectance spectroscopy (UV-VIS DRS). Photocatalytic activity of nanoporous TiO2 coating was assessed by the photocatalytic degradation of methylene blue aqueous solution [33].

W.S. Shih et al., (2010) have demonstrated that nanocrystalline TiO2 thin films, deposited on ITO/glass substrate by radio-frequency magnetron sputtering. Field-emission scanning electron microscope (FE-SEM) and atomic force microscopic (AFM) images showed the morphology of TiO2 channel layer with grain size and root-mean-square (RMS) roughness of 15 and 5.39 nm, respectively. TiO2 thin-film transistors (TFTs) with sputter-SiO2 gate dielectric layer were also fabricated. It was found that the devices exhibited enhancement mode characteristics with the threshold voltage of 7.5 V. With 8-μm gate length, it was also found that the Ion/off ratio and off-state current were around 1.45×102 and 10 nA, respectively [34].

Lin Guo et al., (2010) have reported that the oriented single-crystalline TiO2 nanorod or wire array on transparent conductive substrates would be the most desirable nanostructure in preparing photoelectrochemical solar cells because of its efficient charge separation and transport properties as well as superior light harvesting efficiency. In this study, a TiO2 nanorod array film grown directly on transparent conductive glass (FTO) was prepared by a simple hydrothermal method. The formation of CdS quantum dots (QDs) on the vertically aligned TiO2 nanorods photoelectrode was carried out by chemical bath deposition. The as-prepared materials were characterized by scanning electron microscopy, transmission electron microscopy (TEM), high-resolution TEM, and X-ray diffraction. The results indicate that CdS QDs with a diameter smaller than 10 nm are uniformly covered on the surface of the single-crystalline TiO2 nanorods. Under AM 1.5 G illumination, the photoelectrode was found with a photocurrent intensity of 5.778 mA/cm2 at a potential of 0 V versus Ag/AgCl and an open-circuit photovoltage of 1.292 V versus Ag/AgCl. The photocurrent is 28.6 times higher than that of a bare TiO2 nanorod array, and the photoelectrochemical properties are comparable to those of a CdS QDs-sensitized TiO2 nanotube array, suggesting that the CdS QDs-sensitized TiO2 nanorod array on FTO photoelectrodes has a potential application in solar cells [35].

Ana P.L. Batista et al., (2010) have studied the effect of doping concentration and depth profile of Cu atoms on the photocatalytic and surface properties of titanium dioxide films. Titanium dioxide films of about 200 nm thickness were deposited on glass substrates on which a thin Cu layer (5 nm) was deposited. The films were annealed during 1 s to 100 °C and 400 °C, followed by chemical etching of the Cu film. The grazing incidence X-ray fluorescence measurements showed a thermal induced migration of Cu atoms to depths between 7 and 31 nm. The X-ray photoelectron spectroscopy analysis detected the presence of titanium dioxide, Cu2O and Cu0 phases and an increasing Cu content with the annealing temperature. The change of the surface properties was monitored by the increasing red-shift and absorption of the ultraviolet-visible spectra. Contact angle measurements revealed the formation of a highly hydrophilic surface for the film having a medium Cu concentration. For this sample photocatalytic assays, performed by methylene blue discoloration, show the highest activity. The proposed mechanism of the catalytic effect, taking place on Ti/Cu sites, is supported by results obtained by theoretical calculations [36]. Zachary Mark Seeley et al., (2010) fabricated titanium dioxide thin film gas sensors via the sol-gel method from a starting solution of titanium isopropoxide dissolved in methoxyethanol. Spin coating was used to deposit the sol on electroded aluminum oxide substrates forming a film 1 μm thick. The influence of crystallization temperature and operating temperature on crystalline phase, grain size, electronic conduction activation energy, and gas sensing response toward carbon monoxide (CO) and methane was studied. Pure anatase phase was found with crystallization temperatures up to 800 °C, however, rutile began to form by 900 °C. Grain size increased with increasing calcination temperature. Activation energy was dependent on crystallite size and phase. Sensing response toward CO and methane was dependent on both calcination and operating temperatures. Films crystallized at 650 °C and operated at 450 °C showed the best selectivity toward CO [37]. M.C. Liao et al., (2010) deposited a series of TiO2 thin films onto glass substrates without intentional heating or biasing by magnetron sputtering of a titanium target using Ar/O2 reactive mixtures over a broad range of total sputtering pressures from 0.12 Pa to 2.24 Pa. Each of the film types was deposited by the threshold poisoned mode at a specific given oxygen flow rate monitored in-situ by optical emission spectroscopy. Both the sputtering pressure and thermal annealing are the key factors for the TiO2 films to yield fast-response superhydrophilicity with a water contact angle of 5°. The mechanism of superhydrophilicity for the TiO2 films deposited by high-pressure sputtering has been discussed based on empirical studies of X-ray diffractometry, high-resolution scanning microscopy and atomic force spectroscopy [38]. Shuai Chen et al., (2011) have found that the Magnesium alloys widely applied in the field of biomaterials due to their moderate mechanical properties close to human bone and gradual degradation in human physiological environment without second surgeries. But results from clinical studies showed that magnesium implants suffered from too rapid degradation in human physiological environment. To reduce the degradation rate of magnesium alloys, surface modification is essential and effective besides element alloying. In this study, titanium dioxide films were deposited on Mg-Zn alloy by direct current reactive magnetron sputtering. The morphology and structure of the films were characterized by atomic force microscopy (AFM), scanning electron microscope (SEM) and X-ray diffraction (XRD). The corrosion resistance in simulated body fluid (SBF) at 37 °C was evaluated by potentiodynamic polarization and hydrogen evolution tests. The corrosion behavior of the samples was investigated by SEM with energy dispersive spectroscopy (EDS) after immersion for different periods. The results showed that the compact films were composed of particles with the size of about 100 nm and could effectively improve the corrosion resistance in SBF. After immersion for 10 days, the corrosion rates of the substrates and samples with titanium dioxide films were 4.13 mm/y and 1.95 mm/y, respectively. During the immersion, the titanium dioxide films could induce the growth of hydroxyapatite (HAp) to improve the bioactivity of the samples[39]. Fangzhou et al., (2011) successfully prepared Carbon coated titanium dioxide nanotubes (C-TNTs) film by a two-step process of anodization and gas thermal penetration. The morphologies and structures of C-TNTs films were characterized by SEM, XRD, XPS and Raman spectroscopy. The length and the pore diameter of titanium dioxide nanotubes (TNTs) are approximately 300 nm and 60 nm, respectively. The phase compositions of TNTs films were converted from amorphous to crystalline anatase and rutile with increasing heat treatment temperature during the gas thermal penetration. The coated carbon in the C-TNTs films is partly graphitized and the films have a strong photo response in the visible region. The photo catalytic tests show that the C-TNTs films reveal higher photocatalytic activity,compared with the TNTs film[40]. T.T. Guaraldo et l.,(2011) have prepared Photoanodes based on Ti/titanium dioxide thin films by the sol-gel method, using either tetraisopropoxide or modified tetraisopropoxide, producing electrodes with different sized nanoparticle coatings, termed nanoporous (20 nm) or nanoparticulated (10 nm) electrodes. The anatase form dominated the composition of the nanoparticulated electrode, which presented a higher surface area, a flat band potential shift of −160 mV and a 50% improvement in photoactivity, compared to the nanoporous electrode. 100% color removal, and 75% mineralization, of indigo carmine dye were achieved after 15 min of photoelectrocatalytic treatment using a nanoparticulated Ti/titanium dioxide electrode operated at a current density of 0.4 mA cm−2. Our findings indicate that the use of nanoparticulated electrodes, under UV irradiation and with controlled current density, is an efficient alternative for the removal of food dye contaminants during wastewater treatment[41]. Chuan-Pei Lee et al.,(2011) studied various weight percentages of titanium nitride (TiN) and thermally-treated titanium nitride (tt-TiN) are incorporated into the binder-free titanium dioxide films, prepared at low temperature (LT, 120 °C), and the corresponding dye-sensitized solar cells (DSSCs) were made. Effects of their incorporation on the photovoltaics of the DSSCs are studied. With the incorporation of 0.125 wt% of TiN in a titanium dioxide film of only 5.5 μm-thickness, the corresponding solar-to-electricity conversion efficiency (η) has reached to 3.40% from 2.38% of a cell with a bare titanium dioxide film of same thickness; this increase in efficiency is attributed to the higher electron conductivity and longer electron life time in the titanium dioxide film with TiN. Incorporation of 1.0 wt% of tt-TiN into the titanium dioxide film has further improved the conversion efficiency to 3.77%; this further enhancement in the efficiency is attributed to the partial conversion of TiN into titanium dioxide due to the thermal treatment (450 °C). X-ray diffraction (XRD) and scanning electron microscopy (SEM) are used to study the partial conversion of TiN into titanium dioxide. Other explanations are supported by the data of UV-absorption spectra, electrochemical impedance spectroscopy (EIS), and laser-induced photo-voltage transients[42].

Peng Wan et al., (2011)have studied highly ordered macro-mesoporous anatase TiO2 film which  was synthesized by sol–gel method in an acidic medium, using polystyrene (PS) colloidal crystal and triblock copolymer P123 (EO20PO70EO20) as dual templating. The resulting film was characterized by Raman spectroscopy, X-ray diffraction (XRD), N2 adsorption–desorption analysis, scanning electron microscopy (SEM) and transmission electron microscopy (TEM). The photocatalytic activity of the porous TiO2 film was evaluated by characterizing its photocatalytic effect on the photodegradation process of Rhodamine B (RhB). The results reveal that the bimodal porous material is in anatase phase, and the three-dimensionally ordered macroporous walls are composed of highly ordered mesopores. The average size of the mesopores and the BET surface area are 6.70 nm and 143.37 m2 g-1, respectively. The obtained TiO2 film shows a higher photocatalytic activity than commercial photocatalyst Degussa P25[43].

Tianhong Cui et al., (2011) developed a new method for the superhydrophilic surface modification of copper using versatile solution-based fabrication techniques. The high surface area of TiO2 nanoparticles was exploited to create a thin film with increased surface energy that transformed copper materials from relatively hydrophobic to superhydrophilic. Copper exposed to ambient conditions resulting in a thin layer of copper oxide has a water contact angle near 90°, but following TiO2 modification, the contact angle dropped to 0°.The thin film responsible for this drastic improvement in wettability proved durable by retaining its excellent properties throughout an extended application of thermal stress. SEM and Raman Spectroscopic analysis confirmed the structural integrity of the film before and after a durability test [44].

CHAPTER III

MATERIALS AND METHODOLOGY

Thin film properties are sensitive to their structure, crystalline, nature of defects and imperfection as well as their concentration, compositional variation etc., and to some extent also on the thickness, surface topography and asperities. Most of these factors are associated with the growth process of films and can be controlled and their effects minimized by taking precaution. In this chapter, materials used for the preparation of TiO2 thin film and the methods adopted for the deposition, characterizations are discussed.

3.1 MATERIALS USED:

The materials used for the deposition of TiO2 thin film.

- CHEMICALS :

  - Titanium tri chloride (Sigma 12%)

  - Ammonia solution (Loba 91%)

  - Hydrochloric acid (Merck 35%)

  - Nitric acid (Merck 69%)

  - Extran(Merck)

- GLASSWARES:

  - 50 ml beakers

  - 150 ml beakers

  - 250 ml beakers

  - 500 ml beakers

  - Glass rod

  - Measuring jar

  - Desiccators

  - Microscopic slide

(c) PRECURSOR

- Titanium tri chloride

- Ammonia solution

(d) SOLVENT:

- Deionised water.

3.2 DEPOSITION OF TiO2 THIN FILM:

- SUBSTRATE CLEANING.

- FILM DEPOSITION.

3.2.1 CHOICE OF THE SUBSRATE:

The substrates have a pronounced influence on the growth and orientation of the film. In general, the substrate has to be optically plane, transparent, chemically stable, electrically non-interfering and amenable to moderately high temperature before and after deposition of films. Glass, quartz and ceramic substrate are commonly used for polycrystalline films. The choice of such substrate has been considered for the following advantages.

- Compatibility of crystal structure.

- Freedom from surface strain and cleavage steps.

- Compatibility of thermal–expansion co-efficient between the film material and the substrate.

Glazed substrates surface provide good surface finish, low porosity and have a low dielectric constant value and are effective for most thin film deposition techniques with relatively low deposition temperature.

3.2.2 REQUIREMENTS OF SUBSTRATE:

The characteristics of the substrate used for defect- free films are given below.

- Good surface smoothness.

- Good mechanical strength.

- Inertness or chemical stability.

- Low cost.

- Good uniformity.

3.2.3 SUBSTRATE CLEANING:

A clean and contaminant- free substrate is needed for durable and adherent coating. In the growth of films, cleanliness exerts a decisive influence. Thus a thoroughly cleaned substrate is a pre requisite for the preparation of films.

Fingerprints, residues, oil and airborne particles are the usual contaminants. While cleaning, the contaminates are removed from the substrates. The procedure followed in the present study to clean the glass substrate is described below.

Initially the glass substrate of dimension 75mm X 25mm with thickness of 1mm is cleaned with an acidic bath contains hydrochloric acid and nitric acid in the ratio 1:3 by immersing the substrate for an hour. Thereafter, substrate is rinsed with the ordinary water. Followed by ions in 5% extran solutions for 2 hours. Finally the substrates are again rinsed with deionised water and are dried in desiccators.

3.2.4 CHEMICAL BATH DEPOSITION:

Chemical bath deposition referred to as solution deposition method with its advantage such as simplicity, reproducibility, non-hazardous, cost –effectiveness.etc is well suited for producing large area thin film. This method is a low temperature method and it does not require any sophisticated instruments. It involves the deposition of semiconducting thin film on the substrate that is kept in the aqueous solution.

The chemical bath deposition technique is an open bath wet chemical method that has been extensively employed for the formation of thin films. A major limitation of many existing chemical bath deposition methods is the inefficiency of the processing technique used in terms of the conservation of the starting materials to the thin film. It has been shown that a sizable amount of precursor is lost due to undesirable homogeneous precipitation. Due to this reason, modified chemical bath deposition technique is used.

3.2.5 SILAR:

SILAR is a process for depositing uniform, crystalline and conformal thin films by alternating exposures to cation and anions. SILAR has been successfully demonstrated for many metal oxides, but not for TiO2. Here the process for deposition of TiO2 thin film was demonstrated using SILAR method. SILAR method is inexpensive, simple and convenient for large area deposition. Titanium tri chloride and Ammonium hydroxide were used as cationic and anionic sources respectively. Their surface reactions were found to be complementary and self-limiting; thus providing compact, uniform films with control over thickness of the film. The preparative conditions such as concentration of the precursor, nature of complexing agent, pH of the precursor solution and adsorption, reaction and rinsing time duration etc, were optimized to get good quality TiO2 thin films. The films have been characterized for structural and optical property.

3.2.6 PREPARATION OF TiO2 THIN FILM:

TiO2 films are deposited onto the glass substrate by SILAR technique. Titanium tri chloride and ammonium hydroxide are used as the cationic and anionic precursors respectively. Deionised water is used for rinsing the substrates between successive immersion in the cationic and anionic precursors. The precursors are made with deionised water. The solutions are stirred well to obtain homogeneous solution. Suitable volumes of cationic and anionic precursor solutions are taken in beaker, in addition to, the deionized water. The substrate is immersed for a certain time in the cationic precursor and then rinsed with deionised water. Then the substrate is immersed in the anionic precursor for a specified time followed by rinsing. This complete one SILAR cycle. Films are obtained by repeating the SILAR cycle for number of times. Number of samples is obtained by varying the film deposition condition such as precursor concentration; immersion time; number of SILAR cycles and the deposition condition are optimized. To study the effect of immersion time on the properties of the TiO2 films, samples are deposited at different immersion times with constant precursor concentration and number of reaction cycles. (i.e.) 2 % (1ml) of TiCl3 and 3% (1.5ml) of Ammonium hydroxide was taken in the separate beaker. Both the solutions were continuously stirred by means of a magnetic stirrer. The substrate first dipped in 2 % (1ml) of TiCl3 for 30 seconds, after dipping substrate rinsed with deionized water. The substrate again dipped in 3 % (1.5ml) of ammonia solution for 30 seconds. After dipping substrate was subjected to the deionised water for rinsing. Finally substrates were placed in desiccator for drying. The procedure was repeated by varying the immersion time in the precursors and the bath conditions are depicted in table 3.1.

#### Table: 3.1 DEPOSITION CONDITIONS

| Samples | Volume in percent |  | Volume in ml |  | Immersion time in Cation precursor (sec) | Immersion time in Anion precursor (sec) | Rinsing time (sec) | Immersion cycle (min) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | TiCl3 | Ammonium hydroxide | TiCl3 | Ammonium hydroxide |  |  |  |  |
| 1 | 2 | 3 | 1 | 1.5 | 30 | 30 | 15 | 17 |
| 2 | 2 | 3 | 1 | 1.5 | 40 | 40 | 15 | 17 |
| 3 | 2 | 3 | 1 | 1.5 | 50 | 50 | 15 | 17 |

3.3 THICKNESS MEASUREMENT:

Thickness is the most important film parameter, which controls the film properties. Different techniques have been developed for the measurement of thickness of the films.

Thickness measurement technique may be broadly classified into the following categories.

  - Electrical method.

  - Optical method.

  - Magnetic method

  - Gravimetric method.

  - Radiation method.

  - Mechanical method.

Of which Gravimetric method was adopted to find thickness in the present work.

3.3.1GRAVIMETRIC METHOD:

In this technique, mass of the substrate is measured before and after deposition and the difference between the masses gives the mass of the material deposited.

From which thickness is calculated using the formula,

t= m/a×d

Where,

t=film thickness.

a =area of the sample in cm2.

m=mass of the film.

d=density of the material in g/ (cm3).

3.4 STRUCTURAL CHARACTERIZATION:

The microstructure of the film is found to have profound influence on the optical, electrical and mechanical film properties. The physical properties of thin films are known to differ widely from those of bulk materials. This is evidently connected with the small size of the crystallites terming the film and in particular defects, grain boundaries etc. The structural analysis of thin film is often aided by use of different techniques, which can uniquely identify the crystalline nature. A large number of techniques such as high resolution X-ray and neutron diffraction technique, transmission and scanning electron microscopy, scanning probe microscopy, nuclear methods and a variety of surface technique have been used for many years to characterize thin films.

Among these techniques, X-ray diffraction technique plays a vital role in all aspects of semiconductor technology from fundamental research to manufacturing. The microstructure of the films is directly influenced by the type of substrate used and by deposition conditions prevailing during film formation such as substrate temperature, deposition rate, substrate surface etc. X-ray diffraction technique is a very simple and non-destructive technique requiring only very small area of the sample. With the advancement in technology and complete control over the high power X-ray sources, diffractrometer and counters, this method of analysis has become popular and is widely used. This method is used to find whether the given material is crystalline or amorphous. Hence the structural characterization of Tio2 film (various compositions) has been carried out using X-ray diffractrometer (fig3.1) and the various micro structural parameters have been estimated.

3.4.1 X-RAY DIFFRACTION

Diffraction is one of the most powerful methods for the structural study of the materials, which may involve X rays, electron or neutrons. A zero phase shift between two or more waves reflected from the regular pattern of the studied sample gives the maximum intensity, while the wave in opposite phase will cancel each other and yield minimum intensity.

For example, In the case of light reflected from a layered structure with the spacing (d) between the reflecting planes, the Bragg conditions for diffraction maxima can be obtained from the path difference (n = 2d sin ) of the reflected rays from different crystal planes.

The diffraction pattern reflects the distribution in reciprocal space of either the electron density in electron diffraction or atomic density in neutron diffraction. Therefore, the profile of electron or atomic density can be extracted from the respective diffraction pattern. The later method often referred to as -2 configuration, the rotation of the sample for an angle  is linked with rotation of the detector on 2 and very often the experimental data was presented as the intensity versus 2. The interpretation of diffraction pattern obtained from two dimensional and quasi 3d system include calculating the characteristics comparing the obtained values to the data base of the parameters of known crystallography lattice, the parameters of elementary unit cells for particular crystallographic lattice can also be found.

Figure.3.1 (XRD Experimental Setup)

3.4.2 THEORY OF BRAGGS LAW

The basic X- ray diffraction (fig 3.2) is based on Bragg’s equation. Bragg’s law defines that the wave scattered by the successive parallel planes of atoms of interplanar spacing “d” which is equal to an integral number of wavelength, where phase difference is 2/ times the path difference.

If  is the angle of incidence, then the path difference between two waves is “2d sin”. Hence the Braggs law is,

2d sin  = n

Where,

n = Order of reflection.

d = Distance between the atomic planes parallel to the axis of incident beam.

= Wavelength of x rays. (Refer Fig 3.2)

Fig.3.2 (Bragg’s X-ray Diffraction)

3.4.3 STRUCTURAL PARAMETERS

Grain size (D):

The grain size (D) has been calculated using the Scherrer’s formula

D = k/ cos

Where,

K = slope factor 0.94.

= Wavelength of x rays.

= Braggs angle.

= FWHM in radian.

Interplanar spacing (dhkl):

From the XRD profiles, the interplanar spacing dhkl has been calculated using the Braggs relation.

dhkl = n/2 sin

Where,

= Braggs angle.

n = Order of diffraction.

= Wavelength of incident X-rays.

Lattice constant (α):

From the observed and derived d spacing and assumed (hkl) indices, the lattice constant  is evaluated.

Micro strain ():

The micro strain ()is obtained using the relation

=  cos/4

Where,

= FWHM of the peak.

= Diffraction angle.

Dislocation density ():

Dislocation is an imperfection in a crystal associated with mismatch of the lattice exciting in different parts of the crystal. The dislocation density () is evaluated from Williamson and small man’s formula,    = 1/D2 lines/m2

3.5 OPTICAL CHARACTERIZATION:

The knowledge of optical property of solid films has widely contributed to the phenomenal growth of their application. Optical characterization of films is strongly influenced by the process parameters and the deposition method. Thin films are primarily characterized by absorption/transmission and refractive index. The optical study of solid is concerned with the interaction of the photon energy with matter and the consequent changes occurring in the electronic status. From reflection, transmission and absorption process, the optical constants such as Extinction coefficient (Kf) absorption coefficient (α) and band gap are evaluated.

3.5.1 ULTRAVIOLET AND VISIBLE SPECTROSCOPY:

Ultraviolet-visible spectroscopy or ultraviolet-visible spectrophotometry (UV-Vis or UV/Vis) refers to absorption spectroscopy or reflectance spectroscopy in the ultraviolet-visible spectral region. This means it uses light in the visible and adjacent (near-UV and near-infrared (NIR)) ranges. The absorption or reflectance in the visible range directly affects the perceived color of the chemicals involved. In this region of the electromagnetic spectrum, molecules undergo electronic transitions. This technique is complementary to fluorescence spectroscopy, in that fluorescence deals with transitions from the excited state to the ground state, while absorption measures transitions from the ground state to the excited state.

The instrument used in ultraviolet-visible spectroscopy is called a UV/Vis spectrophotometer. It measures the intensity of light passing through a sample (I), and compares it to the intensity of light before it passes through the sample (Io). The ratio I / Io is called the transmittance, and is usually expressed as a percentage (%T). The absorbance, A, is based on the transmittance:

A = − log (T /100)

The UV-visible spectrophotometer can also be configured to measure reflectance. In this case, the spectrophotometer measures the intensity of light reflected from a sample (I), and compares it to the intensity of light reflected from a reference material (Io)(such as a white tile). The ratio I / Io is called the reflectance, and is usually expressed as a percentage (%R).

The basic parts of a spectrophotometer are a light source, a holder for the sample, a diffraction grating in a monochromator or a prism to separate the different wavelengths of light, and a detector. A spectrophotometer can be either single beam or double beam. In a single beam instrument (such as the Spectronic 20), all of the light passes through the sample cell. Io must be measured by removing the sample. This was the earliest design, but is still in common use in both teaching and industrial labs. In a double-beam instrument, the light is split into two beams before it reaches the sample. One beam is used as the reference; the other beam passes through the sample.

Components of a typical spectrometer are shown in the following diagram (fig 3.3). The functioning of this instrument is relatively straightforward. A beam of light from a visible and/or UV light source is separated into its component wavelengths by a prism or diffraction grating. Each monochromatic (single wavelength) beam in turn is split into two equal intensity beams by a half-mirrored device. One beam, the sample beam, passes through a small transparent container (cuvette) containing a solution of the compound being studied in a transparent solvent. The other beam, the reference, passes through an identical cuvette containing only the solvent. The intensities of these light beams are then measured by electronic detectors and compared. The intensity of the reference beam, which should have suffered little or no light absorption, is defined as I0. The intensity of the sample beam is defined as I. Over a short period of time, the spectrometer automatically scans all the component wavelengths in the manner described. The ultraviolet (UV) region scanned is normally from 200 to 400 nm, and the visible portion is from 400 to 800 nm.

If the sample compound does not absorb light of of a given wavelength, I = I0. However, if the sample compound absorbs light then I is less than I0, and this difference is plotted on a graph versus wavelength. Absorption may be presented as transmittance (T = I/I0) or absorbance (A= log I0/I). If no absorption has occurred, T = 1.0 and A= 0. Most spectrometers display absorbance on the vertical axis, and the commonly observed range is from 0 (100% transmittance) to 2 (1% transmittance). The wavelength of maximum absorbance is a characteristic value, designated as λmax

Fig(3.3) UV-VIS Spectrophotometer

3.5.2 Optical parameters

Absorption coefficient

The absorption coefficient is calculated using the relation,

α = 2.303 log (1/T)

t

t=Thickness of the film,

T=Transmittance of the film.

Extinction coefficient:

The extinction coefficient (K) is calculated making use of Lambert’s eqution,

I = I0exp (-4πkt/λ)

Where,

λ = wavelength of light,

t = thickness of the material.

Thus the value of K can be determined from the formula,

K = 2.303xlog (1/T) x λ

4πt

Band gap:

In a material, the energy difference between its non-conductive state and its conductive state is called Band gap. There is virtually no band gap in most metals, but a very large one in an insulator (dielectric). In a semiconductor, the band gap is small. Technically, the band gap is the energy it takes to move electrons from the valence band to the conduction band.

For incident photon energy greater than the band gap and above, the exponential tail and

the optical absorption  follow a power law.

αhν=A(hν-Eg)n

Direct transition:

In a material, which is free of imperfection, there occur direct but allowed transition from valence band to conduction band, in the case, the top of valence band and bottom of conduction will be at same point.

Αhν =A (hν-Eg)1/2

Indirect transition:

When material contain, defect such as impurities, dislocation etc indirect transistion is said to occur. Consider some perturbation in the system and also interaction with photon as quanta of the vibration modes of lattice. This perturbation will give rise to an additional transition, which is known as indirect transition. In this special case the bottom of the valence band and the top of conduction band will be at different points. The condition for the indirect transition.

αhν=A(hν-Eg)2

Chapter 4

RESULTS AND DISSCUSION

In this chapter, structural and optical characterization results of TiO2 thin film deposited by SILAR method by varying adsorbtion and reaction time are discussed.

4.1 NATURE OF THIN FILM:

In thin film, thickness plays an important role and all its properties depend mainly on thickness. There is often a considerable deviation from that of the bulk behavior and sometimes-new phenomena are observed in the thin film states. In the present work, thin films of TiO2 are deposited by varying the adsorption and reaction times. Thickness of the films is found to increase with increase in adsorption and reaction times. Thickness for sample 1, sample 2, and sample 3 are 0.3472m, 0.52m, and 0.800m respectively. These three samples fall under “Thin film” category, because of the range of film thickness [1].

TABLE: 4.1 DEPOSITION CONDITION WITH THICKNESS FOR SAMPLE1,SAMPLE2, SAMPLE3

| samples | Adsorption time | Reaction time | Thickness (µm) |
| --- | --- | --- | --- |
| 1 | 30 | 30 | 0.3472 |
| 2 | 40 | 40 | 0.52 |
| 3 | 50 | 50 | 0.80 |

4.2OPTICAL CHARACTERIZATION:

Optical transmittance data are recorded using UV-Vis spectrophotometer. Optical constants such as absorbance, extinction co-efficient, absorption co-efficient, and band gap are calculated from transmittance data.

4.2.1 TRANSMITTANCE:

Optical transmittance spectra of TiO2 thin films of different thickness are shown in fig.4.1, fig 4.2 and fig 4.3.

Transmittance of the films rises sharply near the UV-Vis boundary. There is a gradual increase in the transmittance of the film in Visible and NIR region. The similar behaviors obtained in all the three graphs. TiO2 film thickness 0.52m exhibited maximum transmittance (70%) at UV-Visible region as shown in fig (4.2).

Tshihiro Miyata et al., (2006) reported an optical transmittance of 85% in 500nm region for the TiO2 films deposited by vacuum arc plasma evaporation method. [2]

Yang feng et al., (2003) have also observed an optical transmittance of 80%in UV region for TiO2 films deposited by chemical bath deposition method. [3]

The optical transmittance of the TiO2 films deposited by SILAR method is lesser than the reported values.

ABSORBANCE:

Absorbance spectra of Tio2 thin films are shown in fig 4.4, fig 4.5 and fig 4.6.

Absorbance falls rapidly in the wavelength range of 500nm.There is gradual decrease in absorbance with increase in wavelength in the Vis-NIR region. Absorbance of the film increases with increase in thickness. The similar behaviors obtained in all the three graphs. The TiO2 film thickness 0.80m exhibited maximum absorbance (3.75) at region in fig (4.6).

TABLE 4.2 MAXIMUM ABSORBTION CO-EFFICIENT OF TIO2 FILM FOR SAMPLE1, SAMPLE2, and SAMPLE3

| THICKNESS(µm) | ABSORBANCE(A) |
| --- | --- |
| 0.3472 | 2 |
| 0.52 | 3.5 |
| 0.80 | 3.75 |

Chung-Han Wua et al., (2011) observed a similar behavior of absorbance for the TiO2 films deposited by spin coating method [4].

EXTINCTION CO-EFFICIENT:

Extinction co-efficient spectra of Tio2 thin films are shown in fig 4.7, fig 4.8 and fig 4.9.

Extinction co-efficient falls rapidly in the wavelength range of 500nm.There is gradual decrease in extinction co-efficient with increase in wavelength in the Vis-NIR region. The similar behaviors obtained in all the three graphs. The TiO2 film thickness 0.3472m exhibited maximum extinction co-efficient (0.3) at UV region in fig (4.7).

M.M Hasan et al., (2008) observed a similar behavior of extinction co-efficient for the TiO2 films deposited by RF magnetron sputtering method [5].

ABSORPTION CO-EFFICIENT:

Absorption co-efficient spectra of TiO2 thin films are shown in fig 4.10, fig 4.11 and fig 4.12.

Absorption co-efficient falls rapidly in the wavelength range of 500nm.There is gradual decrease in absorption co-efficient with increase in wavelength in the Vis-NIR region.  Absorption co-efficient of the film increases with decrease in thickness. The similar behaviors obtained in all the three graphs. The TiO2 film thickness 0.3472m exhibited maximum absorption co-efficient (13x10^6) at UV region in fig (4.10).

M.Gartner et al., (2008) reported an absorption co-efficient which is constantly increases from 400nm-700nm for TiO2 film deposited by sol-gel method [6]. In the present work, absorption co-efficient drastically increases at 500nm for the TiO2 films.

BANDGAP:

The calculated direct and indirect band gap of the TiO2 films of different thickness are 3.65eV-3.75eV and 2.98eV-3.15eV.The direct and indirect band gap values are shown in the table 4.2.

TABLE 4.3 RELATION SHIP BETWEEN BANDGAP AND THICKNESS

| Thickness(µm) | Direct band gap(eV) | Indirect band gap(eV) |
| --- | --- | --- |
| 0.3472 | 3.68 | 3.1 |
| 052 | 3.65 | 2.98 |
| 0.80 | 3.75 | 3.15 |

Optical study confirms existence of separate direct transition with band gap energies 3.67eV	 for TiO2 films by R.S.Mane et al., (2005) [7].

Direct band gap values obtained in the present work agree well with the results of A. Elfanaoui et al., (2011) [8].

In contradictory to the results obtained in the present study,Yanfeng Gao et al.,(2003) and V. Senthilkumar et al.,(2010) have reported an indirect band gap of 3.6eV for the TiO2 thin films by DC reactive magnetron sputtering technique and Chemical bath deposition method [3, 9].

Fig. 4.1 VARIATION OF %T WITH WAVELENGTH OF TiO2 THIN FILM

(Sample 1)

Fig. 4.2 VARIATION OF % T WITH WAVELENGTH OF TiO2 THIN FILM

(Sample 2)

Fig. 4.3 VARIATION OF % T WITH WAVELENGTH OF TiO2 THIN FILM

(Sample 3)

Fig. 4.4 VARIATION OF ABSORBANCE WITH WAVELENGTH OF TiO2 THIN FILM (Sample 1)

Fig. 4.5 VARIATION OF ABSORBANCE WITH WAVELENGTH OF TiO2 THIN FILM (Sample 2)

Fig. 4.6 VARIATION OF ABSORBANCE WITH WAVELENGTH OF TiO2 THIN FILM (Sample 3)

Fig. 4.7 VARIATION OF EXTINCTION COEFFICIENT WITH WAVELENGTH OF TiO2 THIN FILM (Sample 1)

Fig. 4.8 VARIATION OF EXTINCTION COEFFICIENT WITH WAVELENGTH OF TiO2 THIN FILM (Sample 2)

Fig. 4.9 VARIATION OF EXTINCTION COEFFICIENT WITH WAVELENGTH OF TiO2 THIN FILM (Sample 3)

Fig. 4.10 VARIATION OF ABSORPTION COEFFICIENT WITH WAVELENGTH OF TiO2 THIN FILM (Sample 1)

Fig. 4.11 VARIATION OF ABSORPTION COEFFICIENT WITH WAVELENGTH OF TiO2 THIN FILM (Sample 2)

Fig.4.12 VARIATION OF ABSORPTION COEFFICIENT WITH WAVELENGTH OF TiO2 THIN FILM (sample 3)

Fig. 4.13 VARIATION OF (αhv)2 WITH PHOTON ENERGY hv(eV)OF TiO2 THIN FILM OF THICKNESS 0.3472μm (Sample 1 - DIRECT)

Fig. 4.14 VARIATION OF (αhv)2 WITH PHOTON ENERGY hv(eV)OF TiO2 THIN FILM OF THICKNESS 0.52μm (Sample 2 – DIRECT)

Fig. 4.15 VARIATION OF (αhv)2 WITH PHOTON ENERGY hv(eV)OF TiO2 THIN FILM OF THICKNESS 0.80μm (Sample 3 - DIRECT)

Fig. 4.16 VARIATION OF (αhv)1/2 WITH PHOTON ENERGY hv(eV) OF TiO2 THIN FILM OF THICKNESS  0.3472μm (Sample 1 – INDIRECT)

Fig. 4.16 VARIATION OF (αhv)1/2 WITH PHOTONENERGY hv(eV) OF TiO2 THIN FILM OF THICKNESS  0.52μm (Sample 2-INDIRECT)

Fig. 4.18 VARIATION OF (αhv)1/2 WITH PHOTON ENERGY hv(eV) OF TiO2 THIN FILM OF THICKNESS 0.80μm (Sample 3 - INDIRECT)

Fig. 4.19 VARIATION OF THICKNESS WITH IMMERSION TIME OF TiO2 THIN FILM (Samples 1, 2, 3)

Fig. 4.20 VARIATION OF BAND GAP WITH THICKNESS OF TiO2 THIN FILM -DIRECT (Samples 1, 2, 3)

Fig. 4.21 VARIATION OF BAND GAP WITH THICKNESS OF TiO2 THIN FILM INDIRECT (Samples 1, 2, 3)

CHAPTER V

SUMMARY AND CONCLUSION

Thin film science and technology plays an important role in the high –tech industries and has been developed primarily for the need of integrated circuit industries. Amorphous and crystalline thin film is very important in modern technology.

Chemical bath deposition is an inexpensive and convenient method for large area preparation of thin films. But the major limitation of chemical bath deposition methods is that the loss of materials due to undesirable homogeneous precipation.To over come this problem, modified chemical bath deposition technique is used for the deposition of the thin films. SILAR method is an inexpensive, simple and convenient for large area deposition.

TiO2 is an environmentally friendly material that does not form toxic byproducts; the important application of TiO2 is disinfection of water by TiO2 photo catalysis and sterilized surgical instruments and removes unwanted finger prints from sensitive electrical and optical components.TiO2 offers great potential as an industrial technology for detoxification or remediation.

In the present study, various samples of TiO2 thin film were deposited on the glass substrate a room temperature by varying the adsorption and reaction time as 30 sec, 40sec, and 50sec.

A systematic study on the optical and structural properties of the prepared thin film using-VIS-NIR spectrograph was done. This spectrometer is used to record the optical transmittance and absorbance (a).Using this transmittance and absorbance, various optical constants such as extinction co-efficient, absorption co-efficient and band gap energies are calculated. It is found that TiO2 films have 70% transmittance in the UV region. A direct band gap of 3.65-3.75um was obtained for thin film samples, without annealing.

The structural characterization is mainly used to identify the nature of the film. In present study, TiO2 film exhibits amorphous nature. Hence TiO2 thin films are suitable material for photo catalytic application

REFERENCE

1.A.Goswami,Thin film Fundamentals, New age International Publishers, (1996) pg: 1-5.    2.A.Z.Moshfegh,H.V.Kanel,S.C.Kashyap,M.Watting, Physics and Technology of Thinfilms,INFT(2003)pg:1-4

3.L.Chopra, Kasthuri, Thin film Phenomena, Mc- Graw Hill Book Company, Newyork (1996).

4.L.I.MAISSEL, R.GLANG, Hand Book of Thin film Techonology, Mc-Graw Hill Book Company, Newyork (1970), pg: 1-3.

5.L.Holland, Vacuum Deposition Of Thin film, John Wiley, Newyork (1956), pg: 1-5.

6.K.L.Chopra,s.pandya,Thin Solid Film, Mc-Graw Hill Book Company,Newyork(1983).

7.Gray Hodes,Chemical Solution Deposition Of Semiconductor Films,Mareel Dekker Inc.,Newyork(2009).

8.A.Vancalster,F.Vanfleteren.,et.,al,Journal of Applied Physics,64(1998)pg:3282.

9.B.Ravikumar, S.Uthana, B.srinivasulunaidu, P.Sreedharareddy,

Journal Of Indian Institute of Science, 81(2001), pg: 573-577.

10. J.D.Lee, Concise in Organic Chemistry, Black well science Ltd (1996),pg: 684-685.

11. Reg.P.Smestad, Solar Energy Material Solar Cells 55(1998), pg: 157-178

12.T.S.Ko,S.Yng,H.C.Hsu,C.P.Chu,S.C.Liao,T.C.Lu, S.C.Nang Material Science and Engineering B 134(2006).

13.Elena Vigil, Bernardo González, Inti Zumeta Sergilus Docteur, Ana M. Peiró avid


References and further reading may be available for this article. To view references and further reading you must purchase this article. Gutiérrez–Tauste Concepción Domingo, Xavier Domènechand José A. Ayllón,The role of conducting-oxide-substrate type and morphology in TiO2 films grown by microwave chemical bath deposition (MW-CBD) and their photovoltaic characteristics, Journal of Crystal Growth, Volume 262, Issues 1-4, 15 February 2004, Pages 366-374.

14.Thomas BergerTeresa Lana- Villarreal,Damián Monllor-Satoca and Roberto Gómez, The electrochemistry of transparent quantum size rutile nanowire thin films prepared by one-step low temperature chemical bath deposition, Journal of Crystal Growth,Volume 262, Issues 1-4, 15 February 2004, Pages 366-374.

15.Jing Du; Kwang-Leong Choy, Electrostatic Spray Assisted Vapour Deposition of TiO2-Based Films, Solid State Ionics: Diffusion and Reactions.Vol 173; No 1-4; Year 2004. 119-124.

16.


References and further reading may be available for this article. To view references and further reading you must purchase this articleCheol Ho Heo,Soon-Bo Lee and Jin-Hyo Boo, Deposition of TiO2 thin films using RF magnetron sputtering method and study of their surface characteristics,Thin Solid Films,Volume 475, Issues 1-2, 22 March 2005, Pages 183-188.

17.Olivia Niitsoo, Shaibal K. Sarkar, Christophe Pejoux, Sven Rühle, David Cahen and Gary Hodes, Chemical bath deposited CdS/CdSe-sensitized porous TiO2 solar cells,Journal of Photochemistry and Photobiology A: Chemistry, Volume 181, Issues 2-3, 31 July 2006, Pages 306-313.

18.Jin-Ho Kim, , Shiro Fujita and Seimei Shiratori, Fabrication and characterization of TiO2 thin film prepared by a layer-by-layer self-assembly method,Thin Solid Films,Volume 499, Issues 1-2, 21 March 2006, Pages 83-89.

19.U.M. Patil, K.V. Gurav, Oh-Shim Joo and C.D. Lokhande,

Synthesis of photosensitive nanograined TiO2 thin films by SILAR method ,

Journal of Alloys andCompounds,Volume 478, Issues 1-2, 10 June 2009, Pages 711-715.

20.Hua Yu ,Xin-Jun Li , Shao-Jian Zheng and Wei Xu, Photocatalytic activity of TiO2 thin film non-uniformly doped by Ni,Materials Chemistry and Physics,


References and further reading may be available for this article. To view references and further reading you must purchase this article.Volume 97, Issue 1, 10 May 2006, Pages 59-63.

21.S. Biswas , M.F. Hossain, T. Takahashi, Y. Kubota and A. Fujishima, Photocatalytic activity of high-vacuum annealed CdS–TiO2 thin film, Thin Solid Films, Volume 516, Issue 21, 1 September 2008, Pages 7313-7317.

22.Jingdong zhang,munetaka oyama, Tunable Electrochemical Properties of Liquid Phase Deposited TiO2 Films,jourenal of applied electrochemistry,vol 38,no 1-0,year 2008,1421-1426.

23.Noor Shahina Begam;H.M.Farveez Ahmed, Synthesis of Nanocrystalline TiO2 Thin Films by Liquid Phase Deposition Technique and its Application for Photocatalytic Degradation Studies,Bulliten of Material science ,vol 31,no 1,year 2008,43-48.

24.


References and further reading may be available for this article. To view references and further reading you must purchase this article.A.M. More,T.P. Gujar, J.L. Gunjakar, C.D. Lokhande , and Oh-Shim Joo, Growth of TiO2 nanorods by chemical bath deposition method,Applied Surface Science,Volume 255, Issue 5, Part 2, 30 December 2008, Pages 2682-2687.

25. ZumetaJ.A. Ayllón, B. González, X. Domenech and E. Vigil ,TiO2 films obtained by microwave-activated chemical-bath deposition used to    improve TiO2-conducting glass contact , Solar Energy Materials and Solar Cells,Volume 93, Issue 10, October 2009, Pages 1728-1732.

26.Meltem Asiltürk, , Funda Sayılkan and Ertuğrul Arpaç, Effect of Fe3+ ion doping to TiO2 on the photocatalytic degradation of Malachite Green dye under UV and vis-irradiation Journal of Photochemistry and Photobiology A: Chemistry,Volume 203, Issue 1, 5 March 2009, Pages 64-71.

27.N.R. Mathews,Erik R. Morales, M.A. Cortés-Jacome and J.A. Toledo Antonio, TiO2 thin films – Influence of annealing temperature on structural, optical and photocatalytic properties,Solar Energy,Volume 83, Issue 9, September 2009, Pages 1499-1508.

28.E. Vigil, D. Dixon, J.W.J. Hamilton and J.A. Byrne, Deposition of TiO2 thin films on steel using a microwave activated chemical bath, Surface and Coatings Technology,Volume 203, Issue 23, 25 August 2009, Pages 3614-3617.

29.K. Prabakar, Min-kyu Son,Daniel Ludemanand Hee-je Kim,Visible light enhanced TiO2 thin film bilayer dye sensitized solar cells ,Thin Solid Films Volume 519, Issue 2, 1 November 2010, Pages 894-899.

30.U.M. Patil, K.V. Gurav, Oh-Shim Joo and C.D. Lokhande,Synthesis of photosensitive

nanograined TiO2 thin films by SILAR method ,Journal of Alloys andCompounds,
Volume 478, Issues 1-2, 10 June 2009, Pages 711-715.

31.Dong-Joo Kim, Jin-Yi Kang and Kyo-Seon Kim, Coating of TiO2 thin films on particles by a plasma chemical vapor deposition process,Advanced Powder Technology,Volume 21, Issue 2, March 2010, Pages 136-140.

32.Min wook pyun; Eui jung kim; Dae-hwang yoo; SungHong Hahn,Oblique Angle Deposition of TiO2 Thin Films Prepared by electron-beam Evaporation,Applied surface science ,vol 257,no:4,year 2010,1149-1153.

33.J.hu: C.Zhang; S.Guan; l.Wang; S.Zhu; S.Chen; J.Gao; E.Meng; S.Hou Bb.Cui; H.Sun, Nanoporous TiO2 Films Prepared by Thermal Rapid Treatment (TRT),material letters,Vol 64,No;23,Year 2010,2569-2571.

34.W.S. Shih; S.J. Young; L.W. Ji; W. Water; T.H. Meen; K.T. Lam; J. Sheen; W.C. Chu, Thin Film Transistors Based on TiO2 Fabricated by Using radio-frequency Magnetron Sputtering ,Journal of Physics and Chemistry of Solids.Vol 71; No 12; Year 2010. 1760-1762.

35.Yusong Bai;Hao Zhang;Zhonghao Zhang;                                                                                                                                                                                                                          ZhonghaZhang;Jing hong Li;Lin Guo, CdS Quantum Dots-Sensitized TiO2 Nanorod Array on Transparent Conductive Glass Photoelectrodes,journal of physical chemistry C Vol 114,No 39,Yeart 2010,16451-16455.

36.Hudson W.P. Carvalho; Ana P.L. Batista; Peter Hammer; Teodorico C. Ramalho, Photocatalytic Degradation of Methylene Blue by TiO2-Cu Thin Films: Theoretical and Experimental Study, Journal of Hazardous Materials.Vol 184; No 1-3; Year 2010. 273

37.Zachary Mark Seeley; Amit Bandyopadhyay; Susmita Bose, Titanium Dioxide Thin Films for High Temperature Gas Sensors, Thin Solid Films.Vol 519; No 1; Year 2010. 434-438.

38.M.C. Liao, Niu and G.S. Chen,Effect of sputtering pressure and post-annealing on hydrophilicity of TiO2 thin film deposited by reactive magnetron sputtering,Thin Solid Films,Volume 518, Issue 24, 1 October 2010, Pages 7258-7262.

39.Shuai Chen;Shaokang Guan;Bin Chen;Wen Li;Jun Wang;Liguo Wang;Shijie Zhu;Junhua Hu,Corrosion Behavior of TiO2 Films on Mg-Zn Alloy in Simulated Body Fluid,Applied surface science,Vol 257,No 9,Year 2011,4464-4467.

40.Fangzhou Jia; Zhongping Yau,Zhaohu Jiang; Chunxiang Li, Preparation of  Carbon Coated TiO2 Nanotubes Film and its Catalytic Application for H2 Generation, CatalysisCommunication,Vol.:12,  No:6,  February, 10 2011  [Page 497-501.

41.T.T. Guaraldo; S.H. Pulcinelli; M.V.B. Zanoni, Influence of Particle Size on the Photoactivity of Ti/TiO2 Thin Film Electrodes, and Enhanced Photoelectrocatalytic Degradation of Indigo Carmine Dye, Journal of Photochemistry and Photobiology A: Chemistry.Vol 217; No 1; Year 2011. 259-266.

42.Chuan-Pei Lee; Lu-Yin Lin; Keng-Wei Tsai; R. Vittal; Kuo-Chuan Ho;Enhanced Performance ofdyesensitized Solar Cell with thermally-treated TiN in its TiO2 Film Prepared at Low Temperature, Journal of Power Sources   Vol.: 196,  No.: 3,  February, 1 2011  [Page 1632-1638].


References and further reading may be available for this article. To view references and further reading you must purchase this article.

43. Jianquan Zhao; Peng Wan; Jing Xiang; Tong Tong; Lei Dong; Zhinong Gao; Xinyu Shen; Hua Tong; Synthesis of Highly Ordered Macro-mesoporous Anatase TiO2 Film with High Photocatalytic Activity, Microporous and Mesoporous Materials.Vol 138; No 1-3; Year 2011. 200-206.

44.Benjamin T. McDonald; Tianhong Cui ,Super hydrophilic Surface Modification of Copper Surfaces by Layer-by-Layer self-assembly and Liquid Phase Deposition of TiO2 Thin Film, Journal of Colloid and Interface Science.Vol 354; No 1; Year 2011, 1-6.

45. A.Gosami, Thin film fundamentals , New Age International Publishers (1996) 98

46.P.D.More, G.S.Shahan, H.P.Deshmukh, Material Science and Physics 80(2003)48.

47.Ludmila Eckertova, Physics of Thin film, Plenum press, Newyork (1986).

48.K.L.Chopra, Mayer S pandye, Thin solid films, Plenum press,  Newyork (1983).

49.Course,Sze Pessey.Land Castal.E “Thin Solid film”15(1973) 223.

50.A.V.Nabok, thin solid films,327 (1998),pg 510-540.

51.W.I.F.David, K.Shankland, L.P.Cusker, C.H.Baeslochu, Structural determination from power diffraction data.

52.B.D.Culity, Elements of X-ray Diffraction, additional-Wasley Publishing  company Inc., (1967)285.

53.Gilbert L.R, R.Maisser, R.Roy, Thin Solid films 54,(1978), 149

54.Skoog et al. Principles of Instrumental Analysis. 6th ed.Thomson

Brooks/Cole. 2007, 169-173

55.K.Rammamoorthy,R.Sivakumar,k.saravanakumar,m.Jayachandran,

C.Sancheeviraja,Thin film Preparation and Characterization for Energy Conversion,Karaikudi(2002)100.

56.Toshihiro Miyata, Satoshi Tsukada, Tadatsugu Minami,Preparation of anatase TiO2 thin films by vacuum arc plasma evaporation,Thin Solid Films 496 (2006)136–140.

57.Yanfeng Gao, Yoshitake Masuda, Zifei Peng, Tetsu Yonezawa and Kunihito Koumoto,Room temperature deposition of a TiO2 thin film from aqueous

peroxotitanate solution,Journal of material chemistry 14th January 2003.

58.Chung-Han Wua, Hanying Li, Hon Hang Fong , Vladimir A. Pozdin , Lara A. Estroff , George G. Malliaras, Room-temperature preparation of crystalline TiO2 thin films and their applications in polymer/TiO2 hybrid optoelectronic devices Organic Electronics 12 (2011) 1073–1079.

## 59. M. M. Hasan, A. S. M. A. Haseeb, R. Saidur, and H. H. Masjuki, ,Effects of Annealing Treatment on OpticalProperties of Anatase TiO2 Thin Films.International Journal of Chemical and Biological Engineering 1:2 2008

60. M. Gartner, P. Osiceanu a, M. Anastasescu , T. Stoica , T.F. Stoica ,

C. Trapalis, Investigation on the nitrogen doping of multilayered, porous TiO2 thin films, Thin Solid Films 516 (2008) 8184–8189.

61. R.S. Manea, Seung Jae Roha, Oh-Shim Joob, C.D. Lokhandec, Sung-Hwan Hana Improved performance of dense TiO2/CdSe coupled thin films by low temperature process Electrochimica Acta 50 (2005) 2453–2459.

62. A. Elfanaoui , E. Elhamri , L. Boulkaddat , A. Ihlal , K. Bouabid , L. Laanab , Taleb , X. Portier, Optical and structural properties of TiO2 thin films prepared by solgel spin coating International j o u r n a l o f hydrogen energy

( 2 0 1 1 ) 4 1 3 0e4 1 3 3

63. V. Senthilkumar, M. Jayachandran , C. Sanjeeviraja ,Preparation of anatase TiO2 thin films for dye-sensitized solar cells by DC reactive magnetron sputtering technique, Thin Solid Films 519 (2010) 991–994