EFFECT OF GROWTH RATE ON THE OPTICAL AND

STRUCTURAL PROPERTIES OF TiO2 THIN FILMS

DEPOSITED BY SILAR METHOD

BY

SARANYA, R.

(09PHS09)

A Dissertation submitted to the

AVINASHILINGAM DEEMED UNIVERSITY FOR WOMEN

COIMBATORE – 641 043

In partial fulfillment of the requirements for the degree of

MASTER OF SCIENCE IN PHYSICS

APRIL - 2011

EFFECT OF GROWTH RATE ON THE OPTICAL AND

STRUCTURAL PROPERTIES OF TiO2 THIN FILMS

DEPOSITED BY SILAR METHOD

BY

SARANYA, R.

(09PHS09)

A Dissertation submitted to the

AVINASHILINGAM DEEMED UNIVERSITY FOR WOMEN

COIMBATORE – 641 043

In partial fulfillment of the requirements for the degree of

MASTER OF SCIENCE IN PHYSICS

APRIL – 2011

Certified as a Bonafide Research Work

Signature of the                                                         Signature of the

Head of the Department                                                      Guide

acknowledgement

I owe my sincere thanks to Lord Almighty and my parents without whom I would have been nothing and showering their generous blessings upon me in all endeavors.

I am grateful to (Dr.) T.S.K. Meenakshi Sundharam, M.A, M.Phil, Chancellor, Avinashilingam Deemed University for Women, Coimbatore for providing the opportunity to conduct this study.

My sincere thanks to Dr. (Mrs.) Sheela Ramachandran, M.Sc, P.G. Dip., PhD (Avinashilingam), Vice Chancellor, Avinashilingam Deemed University for Women, Coimbatore for providing all the necessary facilities for the study.

My hearty thanks to Dr. (Mrs.) Gowri Ramakrishnan, M.Sc., (Madras), M.Phil, PhD.,(Avinashilingam), Registrar Avinashilingam Deemed University for Women, Coimbatore for providing adequate facilities required to carry out the work.

My thanks to Dr. (Mrs.) R. Parvatham, M.Sc., Dip.Ed, M.Phil., (Madras), PhD.,(Avinashilingam), Dean, Faculty of Science, Avinashilingam Deemed University for Women, Coimbatore, for her support in the completion of my thesis.

I express my humble thanks to our former Vice Chancellor, Hon. Colonel.          HON.COL. Dr. (Mrs.) Saroja Prabhakaran M.A., Dip.Ed., (Madras), PhD., (Mother Teresa), of Avinashilingam Deemed University for Women, Coimbatore, for the moral support, kind blessing and for providing the adequate help required to carry out the study.

I express my heartfelt and reverential sense of gratitude to my guide Dr.(Tmt)Rachel Oommen, M.Sc.(Kerala), Dip.Ed., (Madras), B.Ed.(Annamalai), M.phil, Ph.D.,(Bharathiar),professor and Head of the Department of Physics, Avinashilingam Deemed University for Women, Coimbatore, for her inspiring guidance, meticulous care, patience, help, encouragement,  motivation,  and skillful and expert suggestion throughout this work.

I also wish to thank all the staff members of the Department of physics Avinashilingam Deemed University for women, Coimbatore, for their help and encouragement.

I express special thanks to my senior Ms. Usha Rajalakshmi P, Research scholar Avinashilingam Deemed University for Women, Coimbatore, for her valuable moral support and encouragement throughout the project period.

I owe my gratitude to my friends and all my well wishers for their constant encouragement, support and help in carrying out this work successfully.

I would like to express my special thanks to my dear Brother and my dear Sister R.ASHOK KUMAR and R. SUGANYA.

R.SARANYA

# CHAPTER I

# INTRODUCTION

1.1 THIN FILMS

Thin film is the branch of physics that deals with very thin structured layers of different materials. “Any solid or liquid with one of its dimensions very much less than that of the other may be called as thin film. [1]” Thin film science has received tremendous attention in the recent years especially after the World War II because of numerous applications in diverse fields. The need for new improved optical and electronic devices have stimulated a new branch of solid state physics called “thin film physics” and technology which comprises the study and application of thin films of elements, binary, ternary and as well as quaternary systems with controlled compositions and specific properties.

Thin solid films were probably first obtained by electrolysis in 1838. BUNSAN and GROVE obtained metal films in 1852 by means of a chemical reaction and by low discharge sputtering respectively. Faraday obtained metal films in 1857 by thermal evaporation on explosion of current methods for the deposition of the thin films from a variety of materials such as metals, insulators or dielectrics etc. Since then it has come a longer a subject of some casual academic interest but has become a full-fledged discipline. Thin film science covers a wide span of disciplines such as solid-state physics, surface science, crystallography, crystal growth process, optics, electronics, and material science. The term “THIN FILM” implies not only a layer of solid material but also a liquid or gaseous phase.

Factors determining the proportion of thin films are

- Rate of deposition.

- Substrate temperature.

- Environmental conditions.

- Residual gas pressure in the system.

- Purity of the material to be deposited.

- Inclusion of foreign matter in the deposit in homogeneity of the film.

- Structural and compositional variations of the film in localized or wide areas.

Surface states of a film also play a dominant role in modifying electrical and other properties. In addition, because of a high surface to volume ratio in a film, a freshly formed film surface becomes highly reactive.

1.2 FILM GROWTH

Film formation involves the deposition of material atom-by-atom or molecule-by-molecule and layer by layer and there should be a sufficient time interval between the two successive depositions of atoms and also layers so that these can occupy the minimum potential energy configuration with respect to the substrate and subsequently on previous deposited layers. With the buildup of layers, the effect of the substrate or the initial layers will gradually diminish but the influence of the freshly formed layers will always be present on the incoming atoms or molecules to determine their occupational sites.

1.4 APPLICATIONS OF THIN FILMS

- Many active and passive microminiaturized components such as solar cells, radiation sources, sensors, magnetic devices, bolometer etc., are fabricated by using thin films.

- Metallic and dielectric thin films find applications in metallic mirrors, antireflection coatings, and dielectric high reflecting mirrors, semitransparent, interference filters.

- Optical semi reflectors are used in interferometers, range finders and lasers.

- Thin film as antireflection coatings will reduce the reflectance and increase the transmittance as the energy has to be conserved.

- Widely used band pass filter is the cold mirror having a high reflectance throughout the visible region and a low reflectance to infrared spectrum. These devices are used in ophthalmic industry for various purposes.

- Thin films find applications in microelectronics, which are smaller, less expensive and more reliable in comparison with conventionally, built up circuits.

- In comparison with semiconductor circuits they are flexible and permit the fabrication of components with closer tolerances.

- Passive components like resisters and thin film capacitors can be fabricated in variety of ways by choosing the required conditions and the techniques.

- Thin film selective absorbing coating with high absorbance in the solar spectral region and low emittance in the thermal IR region increases the efficiency of photo thermal conversion.

- Development of photovoltaic conversion is one of the achievements in thin film technology. Materials like amorphous and crystalline silicon, cadmium telluride, cadmium sulfide, gallium arsenide, copper indium, diselenide etc. have been showing enhanced efficiency of solar cells. [2,3]

1.4 DEPOSITION METHODS

Variety of thin film techniques are available offering a great flexibility for thin film preparation. Growth techniques plays a significant role in governing the properties of the thin films, because the same material deposited by two different techniques usually vary with physical properties; this is due to fact that the electrical and optical properties of these films strongly depend on the structure morphology and the impurities present.

In general, the deposition techniques can be broadly classified into two groups namely physical and chemical methods.

1.4.1 PHYSICAL METHOD

Generally this method is called as physical vapor deposition method because it is mainly based on formation of vapor of material, to be deposited. Vapor then condense on the substrate surface thus forming thin films.

Various physical depositions include:

- Pulsed laser deposition.

- Flash evaporation.

- Cathodic arc deposition.

- Sputtering.

- Vacuum evaporation.

1.4.2 CHEMICAL METHOD

Important chemical methods are:

- Electro deposition.

- Anodic oxidation.

- Electro less plating.

- Chemical bath deposition.

- Spray pyrolysis.

1.4.2.1 CHEMICAL BATH DEPOSITION

Chemical bath deposition is solution deposition method first described in 1869 and it has been used since then to deposit films of many different semiconductors. It is probably the simplest method available for this purpose. All that is needed is a vessel to contain the solution (an aqueous solution) and the substrate on which deposition is required.

“The Chemical bath deposition technique is an open bath wet chemical method that has been extensively employed for the formation of thin films. Thin film formation by Chemical bath deposition is described at the surface of the substrate. In Chemical bath deposition, even though the deposition is by reduction of metal salts, the reactions do not go auto-catalytically unlike electroplating.”

This method involves the hydrolysis of metal ions in aqueous solution followed by their controlled heterogeneous precipitation. Two processes can take place during Chemical bath deposition.

1. Ionic species in solution absorb on the substrate and lead to heterogeneous nucleation.

2. Colloidal particle first nucleate in the solution and absorb on the substrate surface.

The reaction rate is controlled by adjusting PH, temperature and relative concentrations of various reactants in the solution. Since these ions are slowly generated, the stoichiometry can be maintained for any cation – anion ratio. As a result homogenous phases of compounds can be obtained. Many sulfides and selenides have been prepared by this technique.

The process that occurs in Chemical bath deposition solution consists of following steps:

- Equilibrium between the complexing agent and water.

- Formation and dissociation of ionic metal ligand complexes.

- Hydrolysis of the chalcogenide source.

- Formation of the solid.

Chemical bath deposition can be used to deposit any compound that satisfies four basic requirements.

- The compound should be relatively insoluble in the solution used.

- The compound should be chemically stable in the solution.

- If the reaction proceeds through the free anion, this anion should be relatively slowly generated.

- If the reaction is of the complex decomposition type, then decomposition of the metal complex should be similarly relatively slow.

1.4.2.2 MECHANISM OF CHEMICAL BATH DEPOSITION

The mechanism of Chemical bath deposition process can be divided into two different processes

- Formation of required compound by ionic reaction involving free atoms.

- Decomposition of metal complexes.

These two categories can be further classified into two

- Formation of isolated simple molecule that cluster and eventually form a crystal or particle.

- Mediation of a solid phase, usually the metal hydroxide. [4]

# 1.5 ADVANTAGES

- Simplicity

- No requirement of sophisticated instruments.

- Minimum natural wastage.

- Economical way of large area deposition.

- No need of handling poisonous gases like hydrogen selenide.

- Leads to most compact well adhered films.

- Films may be deposited at low temperature on variety of substrate.

- Adjusting the chemical composition and deposition time may readily control thickness of the deposited layer.

1.6 DISADVANTAGES

- Precursor loss due to undesirable homogenous precipitation.

- Inefficiency of processing technique used in terms of the conversion of the starting material to thin films. [5,6]

1.7 TITANIUM DIOXIDE THIN FILMS

Titanium Dioxide is one of the extensively studied transition metal oxides because of their interesting chemical, electrical and optical properties. Titanium dioxide has three different structure types; rutile, anatase, and brookite. All of these crystalline forms of Titanium Dioxide occur in nature as mineral, but only rutile and anatase have been able to be synthesized in pure form at low temperature until recent days. Therefore, anatase and rutile phases which belong to the tetragonal crystal system are widely studied on their syntheses, characterizations and photocatalytic properties. So far anatase phase is known to exhibit higher photocatalytic efficiency compared with rutile phase. Only little efforts have been made on the synthesis, characterization and properties of brookite phase which is belonging to the orthorhombic crystal system. The poor result on brookite phase is due to the difficulty in preparing the pure brookite type Titanium Dioxide without mixture of rutile or anatase phase. Recently, the method to synthesize pure brookite phase Titanium Dioxide was reported, which means that versatile studies on the brookite phase can be ignited. [7] Titanium Dioxide is a high band gap semiconductor that is transparent to the visible light and has excellent optical transmittance.

Among the three crystalline polymorphs of the Titanium Dioxide Rutile Titanium Dioxide is the most attractive for electrical applications because it has the highest dielectric constant. Though Titanium Dioxide has been extensively investigated in the past, anatase Titanium Dioxide found to exhibit interesting properties recently, which makes it a promising material for gas sensors, solar cell and dielectrics and memory cell capacitors and semi conducting FETs. [8, 9]

Rutile is high temperature stable phase and has a refractive index of 2.7, while anatase is formed at lower temperature and has a refractive index of 2.5. At higher temperature about 915ºC anatase will automatically revert to the Rutile structure. Rutile is the more common and better known material while anatase is the rarest. Anatase shared many of the properties of Rutile: luster, hardness and density. Anatase and rutile have the same symmetry but different structures.

Titanium Dioxide has a high ability of adsorption of water molecule and its porosity is easily controlled. Its anatase structure transforms into a more stable rutile structure at appropriate annealing temperature. Titanium Dioxide is a large band gap semiconductor with many interesting properties. It is transparent to visible light, has high refractive index and low adsorption and consequently, is widely used as an optical coating material.

Among many known methods to form Titanium Dioxide film, chemical bath deposition has advantages of simple, economic, effective method to produce high quality coatings.

1.7.1 Properties of Titanium Dioxide

- High dielectric constant.

- Strong mechanical stability.

- Strong chemical stability.

- Good insulating property.

1.7.2 Titanium and its characteristics

- Titanium was discovered in 1910 and got its name from "Titan", a giant Greek

Mythology.

- It is strong and highly resistant to corrosion.

### Titanium is bio-compatible because it is non allergenic.

1.8 APPLICATIONS OF TITANIUM DIOXIDE

- Titanium Dioxide films potentially have a number of electronic device applications such as dye sensitized photovoltaic cells, gas sensors, electro chromic displace and planar wave guides.

- Due to its high dielectric constants Titanium Dioxide is also suggested as alternative for ultra thin gate dielectrics to silicon dioxide for memory and logic devices.

- Titanium Dioxide thin films have been studied most extensively for various optical applications like photo catalyst, optoelectronics and ceramic membrane.

- Rutile Titanium Dioxide is the most attractive for electrical applications because it has the highest dielectric constant.

- Titanium Dioxide is also extensively used in optical thin film device application owing to their high thermal and chemical stability in hostile environments. These films present good durability such as anti-reflection coating, multilayer optical coatings and optical wave-guides.

- Titanium Dioxide finds application in all kinds of paint, printing ink, plastics, paper, synthetic fibers, rubbers, condensers, ceramics, electronic components along with food and cosmetics.

- Titanium Dioxide coated tiles in a hospital environment showed the surface bacteria on the wall surfaces are well reduced to zero plus carbon bacteria counts were reduced.

- Titanium Dioxide is used in sunscreens capacitors, general pigments and coatings. [11,12]

- Titanium dioxide, particularly in the anatase form, is a photo catalyst under ultraviolet (UV) light.

1.9 MOTIVATION OF THE PRESENT WORK

Titanium Dioxide being an n-type wide band gap semiconductor, which is transparent to visible light, it is proposed to prepare thin films of titanium dioxide by CBD technique and to investigate its optical and structural properties.

1.10 OBJECTIVES

In the present work an attempt has been made to prepare Titanium Dioxide thin film using low cost technique like chemical bath deposition.

- The formation and characterization of thin films of Titanium Dioxide by chemical bath deposition form the backbone of the present work.

- Investigation of structural and optical properties of the material.

- Effect of annealing on the films.

- Effect of growth rate on optical and structural properties.

CHAPTER II

# REVIEW OF LITERATURE A literature review discusses published information in a particular subject area, and sometimes information in a particular subject area within a certain time period. It can be just a simple summary of the sources, but it usually has an organizational pattern and combines both summary and synthesis.

K. Prabakar et al., (2010) have described the preparation of visible light enhanced nitrogen-sulfur (N-S) doped Titanium Dioxide thin films by the sol-gel method using thiourea as a dopant. The physical and chemical properties of the Titanium Dioxide thin films were greatly influenced by the amount of thiourea added to the sol-gel solution. The greatest shift to longer wavelengths for visible light absorption was observed with 0.6 g of thiourea in the precursor solution, while 0.4 g yielded the largest particle sizes. These single-cycle dip-deposited N-S doped TiO2 thin films were used as visible light harvesters as well as blocking layers in dye sensitized solar cells. When deposited directly on conducting fluorine doped tin oxide electrodes, photo-conversion efficiencies were reduced. However, the opposite configuration, with N-S doped thin films on top of nanoporous TiO2, yielded an increased open-circuit voltage of 0.84 V, a short-circuit current density of 9.86 mA cm−2, and an overall conversion efficiency of 5.88% greater than that of a standard cell. The effectiveness of the blocking layer on the cell efficiencies was analyzed by electrochemical impedance spectroscopy.

Corina Vacaroiu et al., (2009) have described the photocatalytic performances and antibacterial activity of nitrogen doped TiO2 nanosystems with three and five layers obtained by a sol-gel route, followed by thermal treatment in oxygen or ammonia atmosphere at temperatures between 400 and 1000°C. Subsequently, the antibacterial activity of the obtained nanosystems on the Escherichia coli cells are determined and discussed. The obtained results show a significant dependence of the functional performances on the system's composition. In particular, the antimicrobial activity of nitrogen-doped TiO2 films is correlated with the temperature of thermal treatment and illumination time with visible artificial light. Xian-Feng Gao et al., (2010) The photoresponse of TiO2 nanotube-array films in the visible region is shown to have been significantly improved by sensitizing them with CdS and CdSe semiconductor quantum dots using a sequential chemical bath deposition method. These quantum dots served as cosensitizers, and the performance of corresponding photoelectrode was measured in a photoelectrochemical solar cell. A 13.0 mA/cm2 short circuit current density is achieved with the TiO2/CdS/CdSe photoelectrode under AM 1.5G illuminations, which is higher than the direct sum of CdS and CdSe sensitized TiO2. Parvaneh Sangpour et al., (2010) Titania thin film system containing noble metallic nanoparticles such as Au, Ag, and Cu have been prepared by utilizing radio frequency reactive magnetron cosputtering method. The structural and morphological properties of the thin films were characterized by X-ray diffraction (XRD) and atomic force microscopy (AFM). Surface chemical composition of the films was determined by X-ray photoelectron spectroscopy (XPS). Optical properties of the TiO2 annealed films containing Au, Ag, and Cu metallic nanoparticles were investigated by UV−visible spectrophotometry showing surface plasmon resonance of the metals. The photocatalytic activity of all synthesized samples annealed at 600 °C in an Ar + H2(80 + 20%) environment was evaluated by measuring the rate of photodegradation reaction of methylene blue (MB) under similar conditions in the presence of UV and visible light irradiation. The Au:Titanium Di oxide and Cu:Titanium Di oxide thin film systems significantly enhanced photodecomposition of MB resulting in 80 and 90% of its initial concentration after 200 min photoirradiation, respectively. The increase in the surface roughness measured by AFM observation and the presence of the Ti3+ oxygen vacancy in the photoirradiated thin films were found responsible for the enhancement of the MB photodegradation reaction. The complex studies of photoinduced absorption, second harmonic generation and third harmonic generation were performed by Yahia Djaoued et al., (2010) for TiO2 films of different morphology. In particular they have studied the influence of a bicolor laser beam treatment by a 300 mW green cw laser emitting at 532 nm on changes of absorption, birefringence and third harmonic generation on TiO2 films. They have performed the corresponding measurements using as a photoinducing light a glass erbium 10 ns pulsed laser with a fundamental wavelength of about 1540 nm together with its second harmonic generation (SHG) at 770 nm using the method of bicolor laser treatment and a frequency repetition of about 10 Hz. Varying the power density ratios between the fundamental and its SHG they have established the optimal conditions to achieve maximal photoinduced changes of absorption, birefringence and third harmonic generation (THG). They have detected changes of the birefringence and of the THG immediately after the laser treatment. They studied an influence of the nanoparticle's sizes on the observed changes of the optical features. Additionally they have studied the role of different chemical treatment on the structural and optical parameters. Habib M. Pathan et al., (2005) have investigated a lot of methods for the deposition of Titanium Dioxide thin films; however, in each of these methods as-deposited films are amorphous and need further heat treatment at high temperature. A chemical bath deposition (CBD) method was used for the preparation of Titanium Dioxide thin films. They investigated nanocrystalline TiO2 thin films using CBD at room temperature onto glass and ITO coated glass substrate. The films were characterized by X-ray diffraction (XRD), scanning electron microscopy (SEM), and high-resolution transmission electron microscopy (HRTEM) techniques. The chemically synthesized films were nanocrystalline and composed of crystal grains of 2–3 nm. Patterned thin films of titanium dioxide (TiO2), with micrometer-sized features, were prepared by Keith J. Stevenson et al., (2001) on transparent, conductive indium-tin oxide glass platforms via microtransfer molding and electrochemical deposition. The grating pattern produces optical diffraction, where the efficiency of diffraction (g) depends on the degree of contrast in refractive index between the patterned material and the surrounding medium. The refractive index of a representative micropatterned TiO2 film (anatase) was estimated, via solvent index matching experiments, to be 2.72-a value sufficiently large to achieve good contrast with air or water. A new method, based on the measurement of changes in diffraction efficiency, is described for the detection and evaluation of organic chemical adsorption on various titanium dioxide surfaces. The strategy is illustrated for the vapor-phase adsorption of chloroform on high-area amorphous, anatase, and rutile forms of titanium dioxide. The uptake of 2,4,5-trichlorophenol from aqueous solutions by amorphous TiO2 was also examined by the modulated optical-diffraction-grating technique. Millon et al., (2007) have found that sol-gel TiO2 thin films have been loaded with platinum clusters through a photo-platinization method using water/ethanol platinum solutions. The morphological and physico-chemical properties of platinized films as well as the chemical state of platinum clusters have been studied by scanning electron microscopy, Fourier transform infrared spectroscopy, and X-ray photoelectron spectroscopy. These characterizations show that morphological and physico-chemical properties are strongly influenced by the water/ethanol composition of the platinum solution and temperature of the post-platinization heat-treatment, which in turn determines the photocatalytic performances of platinized films. UV-assisted photocatalytic reactions induced by platinized films follow bi-regime kinetics. The first regime is characterized by a rather high rate constant, while long term UV exposition promotes a more or less pronounced deceleration of the photocatalytic reaction. Optimization of the photocatalytic activity requires a platinization in presence of a water excess followed by a heat-treatment in the 250-400 °C thermal range. Films processed in such conditions exhibit rate constants in the first and second photocatalysis regime which are four times and three times greater, respectively, than the rate constant measured for non-platinized films. Vigil et al., (2009) have found that Microwave activated chemical bath deposition (MW-CBD) is a simple and novel technique in which the substrate is heated directly by microwaves and very well adhered layers are obtained. It has not been used previously for TiO2 deposition on metals. They showed that it is possible to coat stainless steel with TiO2 using MW-CBD. Two different precursor solutions are used for TiO2 deposition on steel grade 316.Titanium Dioxide thin films on steel substrates were characterized using SEM and Raman spectroscopy. Raman analysis showed that amorphous TiO2 is obtained using the precursor solution based on TiOSO4; however, films show anatase crystal structure when using the precursor solution based on (NH4)2TiF6. Thermal treatment of the films improved crystallinity and also allowed iron diffusion from the steel substrate into the film. Crystalline phases that appeared due to heat treatment were identified from Raman spectra. MW-CBD allows simple low temperature coating of a metal substrate with Titanium Dioxide and this should be useful for a number of different applications. Kee-Rong Wu et al.,(2009) have elucidated how indium tin oxide (ITO) thin film affects the microstructural andphotocatalytic properties of layered TiO2/ITO films prepared by DC magnetron sputtering.Two ITO substrates, as received ITO (aITO) and in situ sputtered ITO (sITO), are adopted herein. Photocatalytic measurements of methylene blue and dimethyl sulfoxide indicate that the layered TiO2/sITO film has greater photocatalytic oxidation than the TiO2/aITO catalyst. According to photoelectrochemical tests, the latter exhibits a completely opposite activity to that of the former. Secondary ion mass spectrometry elemental depth profiles reveal that tin atoms in the sITO film really permeate into the growing TiO2 film and promote the formation of the crystalline Ti1−xSnxO2 layer. Additionally, cross-sectional transmission electron microscopy images and the selective area diffraction patterns show the difference between the diffusion of tin in the two catalysts. The photocatalytic oxidation capability is further enhanced in the layered TiO2/sITO film because of an increase in the bandgap energy and a positive shift in the Fermi level energy of the Ti1−xSnxO2 layer. Conversely, tin diffusion is limited in the aITO substrate under controlled conditions, in such a manner that a Schottky barrier can form at the TiO2/aITO interface. Therefore, photogenerated electrons can be efficiently transferred from the overlaid TiO2 film to the aITO substrate, producing a remarkable photocurrent density under UV illumination. Microstructural measurements reveal that the growth of the reactive {0 0 1} facets and columnar porous structure are favored by the synergetic effect of ITO substrate and an extended period of deposition. Accordingly, the photocatalytic capabilities are further raised. Transparent thin films were obtained on microscope glass slides by r.f. magnetron reactive sputtering. The samples were investigated using X-ray diffraction (XRD), transmittance electron microscopy (TEM), UV-VIS-NIR spectrophotometer and coatings scratch testing. All the films were anatase phase and the particle size was in nanoscale. The photocatalytic properties of the samples were tested on the degradation of methylene blue dye solution. It was found that the photocatalytic activity increased with decreasing sputtering pressure. At the same time, the results indicate that the band gaps of the films all became larger than the bulk TiO2 and the adhesion strength between the films and the substrates decreased with increasing sputtering pressure T. M. Wang et al., (2002). Series of transparent TiO2 thin films have been obtained on microscope glass slides by means of r.f. Magnetron reactive sputtering using Ar and O2 mixed gases. The photocatalytic activity of the TiO2 thin films was evaluated by the degradation of rhodamine B dye wastewater. The influences of substrate temperatures and total sputtering pressures on the photocatalytic activity of the TiO2 films were investigated. It was observed that substrate temperature had little influences on the photocatalytic activity, but the photocatalytic activity of the TiO2 thin films was improved by decreasing the total sputtering pressure S. K. Zheng et al., (2003). G. Sauthier et al., (2010) have analysed Nitrogen–doped TiO2 thin films grown on (001) SiO2 substrates by reactive pulsed laser deposition. A KrF* excimer laser source (λ = 248 nm, τFWHM 10 ns, ν = 10 Hz) was used for the irradiations of pressed powder targets composed by both anatase and rutile phase TiO2. The experiments were performed in a controlled reactive atmosphere consisting of oxygen or mixtures of oxygen and nitrogen gases. The obtained thin film crystal structure was investigated by X-ray diffraction, while their chemical composition as well as chemical bonding states between the elements were studied by X-ray photoelectron spectroscopy. An interrelation was found between nitrogen concentration, crystalline structure, bonding states between the elements, and the formation of titanium oxinitride compounds. Moreover, as a result of the nitrogen incorporation in the films a continuous red-shift of the optical absorption edge accompanied by absorption in the visible spectral range between 400 and 500 nm wavelength was observed. Peng Sun et al., (2010) have analysed nanostructured TiO2 thin films prepared on metal substrates using a facile layer-by-layer dip-coating method. The phase structure and morphologies of preparing samples were characterized by means of X-ray powder diffraction (XRD) and field-emission scanning electron microscopy (FESEM). The results confirm that films are highly crystalline anatase TiO2 and free from other phases of TiO2. Scanning electron microscopy (SEM) shows that the nanoparticles are sintered together to form a compact structure. The electrical properties of samples were investigated by cutternt–voltage analysis; the result indicates that a rectifying junction between the nanocrystalline Titanium Dioxide film and metal substrate was formed. The photoelectrochemical characteristics recorded under 1.5 AM illumination indicates that the as-fabricated thin film electrode possesses the highest photocurrent density at 450 °C, which is 1.75 mA/cm2 at 0 V vs. Ag/AgCl. Titania thin films were prepared by Rudolf C. Hoffmann et al., (2008) on bare Si and Pt/Ti/SiO2/Si substrates by chemical bath deposition (CBD) from solutions of a titanium peroxo complex and subsequent calcinations at 350 and 700 °C, respectively. The CBD process allotheyd deposition on both uncoated and metal-coated Si substrates with the same deposition rate. Optimization of the annealing process yielded uniform and crack-free nanocrystalline anatase films. The influence of the film thickness, irradiation of visible light, measuring frequency, temperature and substrate on the dielectric properties will be discussed in the paper. Films with a final thickness of about 600 nm showed comparably high relative permittivity of 31.8 on silicon and of 52.7 on Pt/Ti/SiO2/Si substrates, respectively. The present route provides anatase thin films with higher dielectric constants than classical sol–gel routes and is therefore a promising candidate for potential applications in large-scale integration. Titanium Dioxide layers grown by microwave-activated chemical bath deposition (MW) and dip coating (DC), as well as by the combination of both techniques, were studied by Rutherford backscattering spectrometry (RBS), atomic force microscopy (AFM) and scanning electron microscopy (SEM). RBS analysis allows the determination of the stoichiometry and the thickness (in atoms/cm2) of the TiO2 layers. TiO2 layers grown by DC have higher growth rates on aTiO2 film obtained by MW compared to deposition directly onto an indium–tin oxide (ITO) substrate.TiO2 layers grown by MW on a film obtained by DC have higher growth rates when compared to layers deposited onto ITO substrates. In this case, AFM analysis shows that the surface is rough and RBS reveals the presence of holes in TiO2 films. Fernández-Lima et al., (2003) Successive ionic layer adsorption and reaction (SILAR) is a process for depositing uniform, crystalline and conformal thin film by alternating exposures to cations and anions. SILAR has been successfully demonstrated for many metal oxides, but not for TiO2. Here they demonstrate process for deposition of TiO2 thin films using SILAR method. Titanium tri-chloride and ammonium hydroxide were used as cationic and anionic sources, respectively. Their surface reactions were found to be complementary and self-limiting, thus providing compact, uniform films with control over thickness of the film. The preparative conditions were optimized to get good-quality TiO2 thin films. The films have been characterized for structural, morphological, compositional, and optical and photo-response properties. Growth process, reaction mechanism and annealing effect are also discussed. H.M. Pathan et al., (2006) Titanium Dioxide films were fabricated on fluorine doped tin oxide (FTO) coated glass substrate using successive ionic layer adsorption and reaction (SILAR) method A.M. More et al., (2009). The X-ray diffraction, scanning electron microscopy, transmission electron microscopy, optical absorption and contact angle measurement were applied to study the structural, surface morphological, optical and surface wettability properties of the as-deposited and annealed TiO2 films. The X-ray diffraction studies revealed both as-deposited and annealed TiO2 films are amorphous. Irregular shaped spherical grains of random size and well covered to the fluorine doped tin oxide coated glass substrates were observed from SEM studies with some cracks after annealing. The optical band gap values of virgin TiO2, annealed, methyl violet and rose bengal sensitized TiO2 were found to be 3.6, 3.5, 2.87 and 2.95 eV, respectively. Surface wettability studied in contact with liquid interface, showed hydrophobic nature as water contact angles were greater than 90°. The adsorption of dyes, as confirmed by the photographs, is one of the prime requirements for dye sensitized solar cells (DSSC). Nanocrystalline TiO2 thin films were deposited by simple successive ionic layer adsorption and reaction (SILAR) method on glass and fluorine-doped tin oxide (FTO)-coated glass substrate from aqueous solution by U.M. Patil et al., (2009). The as-deposited films are heat treated at 673 K for 2 h in air. The change in structural, morphological and optical properties are studied by means of X-ray diffraction (XRD), selected area electron diffraction (SAED), scanning electron microscopy (SEM), Fourier transform infrared (FTIR), transmission electron microscopy (TEM) and UV–vis–NIR spectrophotometer. The results show that the SILAR method allows the formation of anatase, nanocrystalline, and porous TiO2 thin films. The heat-treated film showed conversion efficiency of 0.047% in photoelectrochemical cell with 1 M NaOH electrolyte. The use of successive ionic layer adsorption and reaction (SILAR) method was preferred for the growth of amorphous TiO2 thin films at ambient temperature. Further, these films were annealed at 673 K for 2 h in air for structural improvement and characterized for structural, surface morphological, optical and electrical properties. An amorphous structure of TiO2 was retained even after annealing as confirmed from XRD studies. The spherical grains of relatively large size were compressed after annealing. A red shift in band gap energy and decrease in electrical resistivity were observed due to annealing treatment. S.S. Kale et al., (2006) Electrochromic TiO2 films were deposited on TiO2 (sputtered)/indium–tin-oxide (ITO)-glass substrates by the chemical solution deposition method (CSD) using a solution mixture of titanium diisopropoxide bis(acetylacetonate) and 2-methoxyethanol by Ying-Chung Chen et al., (2008). The sputtered TiO2 thin film was used as a buffer layer to increase the adhesion between TiO2 film and ITO-glass substrate.TiO2 films were dried in air at 150 °C for 10 min, and coating/drying operations were repeated until the desired thickness was obtained. By changing the heating temperature (150–400 °C), the effects of various processing parameters on the films characteristics are studied. Electrochromic properties of TiO2 films were investigated using cyclic voltammograms (CVs) and in situ transmittance measurements, which were carried out on TiO2 films immersed in an electrolyte of 1 M LiClO4 in propylene carbonate (PC).Titanium Dioxide films were found to show reversible blue coloration upon Li+ ion intercalation in this study. Experimental results reveal that the processing parameters will influence the electrochromic properties of TiO2 films such as transmittance, CVs, inserted charge, optical density change, coloration efficiency and insertion coefficient. Longjie Zhou et al., (2008) have analyzed the preparation on bare Si titania thin films and Pt/Ti/SiO2/Si substrates by chemical bath deposition (CBD) from solutions of a titanium peroxo complex and subsequent calcinations at 350 and 700 °C, respectively. The CBD process allowed deposition on both uncoated and metal-coated Si substrates with the same deposition rate. Optimization of the annealing process yielded uniform and crack-free nanocrystalline anatase films. The influence of the film thickness, irradiation of visible light, measuring frequency, temperature and substrate on the dielectric properties has been discussed. Films with a final thickness of about 600 nm showed comparably high relative permittivity of 31.8 on silicon and of 52.7 on Pt/Ti/SiO2/Si substrates, respectively. The present route provides anatase thin films with higher dielectric constants than classical sol–gel routes and is therefore a promising candidate for potential applications in large scale integration. A.M. More et al., (2008) have analyzed TiO2 nanorods fabricated from the simple chemical bath deposition (CBD) method and characterized using X-ray diffraction, scanning electron microscopy (SEM), transmission electron microscopy (TEM), and optical absorption studies. The structural study revealed that TiO2 films retain amorphous structure even after annealing at 723 K. The SEM and TEM studies showed good substrate coverage consisting of TiO2 nanorods. The optical band gap declined from 3.4 to 3.3 eV after annealing, showing no significant change. Both as-deposited and annealed TiO2 films exhibit n-type electrical conductivity. As-deposited and annealed TiO2 films showed hydrophilic behavior as water contact angles were 10° and 12°, respectively. Atmospheric pressure chemical vapor deposition (APCVD) of TiO2 thin films has been achieved by C. Quiñonez et al., (2010) onto glass and onto ITO-coated glass substrates, from the reaction of TiCl4 with ethyl acetate (EtOAc). The effect of the synthesis temperature on the optical, structural and electrochemical properties was studied through spectral transmittance, X-ray diffraction (XRD) and electrochemical impedance spectroscopy (EIS) measurements. It was established that the TiO2 films deposited onto glass substrate, at temperatures greater than 400 °C grown with rutile type tetragonal structure, whereas the TiO2 films deposited onto ITO-coated glass substrate grown with anatase type structure. EIS was applied as suitable method to determine the charge transfer resistance in the electrolyte/Titanium Di oxide interface, typically found in dye-sensitized solar cells. Titanium Dioxide films were prepared on a silicon or soda-glass substrate using a sol suspension Chiaki Oharaet al., (2008). The TiO2 film on the silicon substrate was composed of pure anatase phase and showed almost no contaminations. In contrast, the TiO2 film on the soda-glass substrate was composed of anatase and brookite phases. The diffusion of Na into the TiO2 film on the soda-glass substrate was observed by XPS, and Na was concentrated on the surface of the film. The yield of the brookite phase increased with decreasing distance from the surface of the film on the soda-glass substrate. Na promoted the formation of the brookite phase, although the preparative procedure was used for anatase synthesis. The photocatalytic activity of TiO2 films deposited on different substrates by the spray-drying method using suspensions of commercially available TiO2 (Degussa P25 or Tronox) as starting material was studied M. Uzunova-Bujnova et al., (2009). The influence of the type of the initial TiO2, preparation conditions (temperature of the substrate during the film deposition, temperature of the post-deposition annealing), substrate material (glass, fused silica, stainless steel and graphite), the presence of additives in the spraying suspension (polyethylene glycol, ethylene glycol and acetylacetone) and its sonication before spraying on the morphology, size of crystallites and phase composition (rutile/anatase ratio) was studied. Optimal conditions for spray deposition of the films are suggested. A.P. Caricato et al., (2007) have reported morphological and optical properties of a colloidal TiO2 nanoparticle film, deposited on a quartz substrate by using the Matrix-Assisted Pulsed Laser Evaporation (MAPLE) technique. Atomic Force Microscopy demonstrated that a good uniformity of the deposition can be obtained. The presence of agglomerates with dimensions of about 1 μm in size was noticed. Form UV–vis transmission spectra, recorded in the 200–800 nm range, the optical constants and the energy gap were determined besides the film thickness. The optical constants resulted in agreement with the values reported in literature for TiO2 nanoparticle thin films. ### Bok-Hee Kim et al., (2004) Synthesized TiO2 thin film on α-Al2O3 (0 0 0 1) substrate by liquid sprayed mist chemical vapor deposition under 1 atm. Tetraethylorthotitanate [TEOT, (C2H5O) 4Ti] was used as starting material. The liquid source to synthesize TiO2 thin film was prepared from dissolving the starting materials in 2-methoxyethanol. The TiO2 thin film was obtained as the amorphous phase at 300 °C and crystalline anatase type TiO2 above 400 °C. The crystal of thin film was mainly oriented to –(1 1 2) plane. The degree of (1 1 2) orientation, the thickness, and the surface roughness of the film were strongly dependent on the substrate temperature and deposition time. By the controlling the substrate temperature and deposition time, TiO2/α-Al2O3 (0 0 0 1) films with preferred orientation were successfully fabricated, and the film deposition rate was about 10 nm/min. Jin-Yi Kang et al., (2010) have experimentally coated the TiO2 thin films on the glass beads by a rotating cylindrical plasma chemical vapor deposition (PCVD) process. The precursors for the thin films were generated by the plasma reactions, and they deposited on the glass beads to become the grains on the films. The TiO2 thin films grow more quickly on the glass beads by increasing the reactor pressure, or the rotation speed of the reactor. As the applied power increases, the thickness of the thin films on the glass beads decreases. As the thickness of the TiO2 thin films increases, the uniformity of the TiO2 thin films decreases due to the deposition of larger grains or due to the increase of crack size. The rotating cylindrical PCVD process can be a good method to prepare the particles coated with metal or organic-doped thin films for highly functionalized materials. Nitrogen doped TiO2 thin films were deposited by RF magnetron sputtering onto various substrates. The films were prepared in plasma of argon, oxygen, and nitrogen, with varying the nitrogen content, from 0% up to 70%. The resulting TiOx-Ny films were found to consist of cubic TiN osbornite and tetragonal TiO2 rutile phases. Using optical spectroscopy with large spectral range from 350 to 1000 nm, the band gap width was determined and a narrowing of the optical gap from 2.76 to 2.32 eV was observed as a function of the N-content. It was found that the optical properties of the TiOx-Ny layers are influenced by the surface morphology, roughness, surface energy and phase content. The chemical composition, the crystalline structure, the surface morphology and the surface energy were thoroughly studied by the Rutherford backscattering spectrometry (RBS), grazing-angle XRD, atomic force microscopy (AFM) and contact angle measurements (wettability), respectively. K.G. Grigorov et al., (2011). Jing Du et al., (2004) have identified Titanium Dioxide as one of the best candidates for gas sensing because of its low cost, stable phase even at high temperature, higher gas sensitivity and comparable thermal expansion coefficient to alumina substrate. Further improvement in the performance can be achieved by addition of trivalent or pentavalent dopants. Recently, a novel electrostatic spray assisted vapour deposition (ESAVD) technique has been developed in our laboratory to prepare thin or thick films of various materials. This method offers many advantages over several conventional deposition techniques including a simple set-up, inexpensive and nontoxic precursor, high deposition efficiency and easy control of the surface morphology of the deposited films and excellent control of stoichiometry. The possibility of morphology control is of particular interest for gas sensor application since the surface is primarily involved in the initial sensor/gas interaction. In their work, the structural and morphological characterization of Titanium Dioxide-based films incorporated with Cr, Nb metal ions deposited by EASVD have been studied. Scanning electron microscopy (SEM) was used to analyze the microstructural and morphological properties. The X-ray diffraction (XRD) and Energy dispersion X-ray (EDX) analysis of SEM were employed to determine the crystal phase and film composition. X-ray photoelectron spectroscopy (XPS) was used to identify the surface chemical stoichiometry of the deposited films. Yahia Djaoued et al.,(2010) have carried out the complex studies of photoinduced absorption, second harmonic generation and third harmonic generation for Titanium Dioxide films of different morphology. In particular they have studied the influence of a bicolor laser beam treatment by a 300 mW green cw laser emitting at 532 nm on changes of absorption, birefringence and third harmonic generation on Titanium Dioxide films. They have performed the corresponding measurements using as a photoinducing light a glass erbium 10 ns pulsed laser with a fundamental wavelength of about 1540 nm together with its second harmonic generation (SHG) at 770 nm using the method of bicolor laser treatment and a frequency repetition of about 10 Hz. Varying the power density ratios between the fundamental and its SHG they have established the optimal conditions to achieve maximal photoinduced changes of absorption, birefringence and third harmonic generation (THG). They have detected changes of the birefringence and of the THG immediately after the laser treatment. They studied the influence of the nanoparticle's sizes on the observed changes of the optical features. Additionally they have studied the role of different chemical treatment on the structural and optical parameters.

CHAPTER III

MATERIALS AND METHODS

This chapter describes the experimental techniques used in the present investigations on thin films. TiO2 thin films are being prepared by various techniques. In the present work, TiO2 thin films were prepared by modified chemical bath deposition technique called SILAR to obtain good quality and homogenous film. The experimental details pertaining to the evaluation of various properties using analytical techniques for film characterization implemented in the present work are also outlined.

3.1 MATERIALS USED

(a)        CHEMICALS:

- Titanium Trichloride (Sigma aldrich 12%)

- Ammonia solution (Loba 9%)

- Nitric acid (Merck 69%)

- Hydrochloric acid (Merck 36%)

- Extran (Merck)

- Deionized water

(b)        GLASS WARES:

- Beakers (50ml,150ml,250ml,500ml)

- Measuring jar

- Glass rod

- Microscopic slides

- Desiccators

  - EXPERIMENTAL STUDY

1. Film deposition

2. Film characterization

3.2.1 FILM DEPOSITION

3.2.1.1 CHOICE OF THE SUBSTRATE

The substrate shows a great influence on the growth and the orientation of the film. The nature and the surface finish of the substrate are important because they influence the properties of the films deposited. Ideally, the substrate should provide mechanical support but not interact with the film except for sufficient adhesion. Therefore glass substrates are used, since they are very economical, can be easily cleaned, and also due to their stability. In the present work microscopic glass slides of dimensions 75mm x 25mm with thickness of 1.34mm were used.

3.2.1.2 CLEANING OF THE SUBSTRATES

For durable and adherent coating, a glass substrate must be adequately cleaned. The proper cleaning technique depends on the nature of the substrate, the nature of the contaminants and the degree of cleanliness required. Expected contaminants include those from manufacturing procedures, human contact, air bone dust and oil particles. Cleaning involves the breaking of adsorption bonds between the substrate and the contaminants without damaging the substrate and the surface itself.

The following procedure is used for cleaning these substrates:

- The glass substrate is first immersed in an acidic bath containing conc. HNO3and conc. HCl in the ratio 1:3 for about 30 minutes.

- The substrates are rinsed well with distilled water and immersed in Extran solution (5%) for two hours.

- After chemical treatment the substrates are washed with deionized water and are dried in desiccators. [45]

3.2.1.3 CHEMICAL BATH DEPOSITION

Chemical bath deposition is also called a liquid phase deposition or chemical solution deposition. The method involves immersion of a substrate in an aqueous solution containing a precursor species, which hydrolysis slowly to produce super saturated solution of the desired oxide, which then precipitates preferentially on the substrate surface producing a conformal coating.

Chemical bath deposition is an inexpensive and convenient method for large area preparation of thin films as close to room temperature where a controllable chemical reaction in an aqueous solution containing the various reactants is involved.

In order to overcome its disadvantage like precipitation in solution, during deposition, it is needed to keep cationic and anionic precursors separate. Hence films are deposited by Successive Ionic Layer Adsorption and Reaction (SILAR) where cationic and anionic precursors are kept separate.

SILAR method has emerged as one of the solution methods to deposit a variety of compound materials in thin film form. The SILAR method is inexpensive simple and convenient for large area deposition. A variety of substrate such as insulators, semiconductors, metals and temperature sensitive substrates can be used since the deposition is carried out at or near to room temperature. As a low temperature process, it also avoids oxidation and corrosion of the substrate. The prime requisite for obtaining good quality thin films is the optimization of preparative provisors i.e. precursors nature of complexing agent, PH of the precursor solution and adsorption reaction and rinsing time duration.

3.2.1.4 DEPOSITION OF TIO2 THIN FILM

Thin film of titanium dioxide is deposited by SILAR technique which involves the successive immersion of the substrate in cationic and anionic precursor solutions followed by rinsing with deionized water after each immersion.  TiCl3 and ammonium hydroxide served as the cationic and anionic precursor respectively. Deionized water is used for rinsing the substrate after immersion in the precursor solution which facilitates the removal of excess cations or anions which are adsorbed onto the substrates. Volume percent solutions of the precursors are prepared with distilled water. Appropriate volumes of the precursor’s solutions and deionized water are taken in separate beakers. To study the effect of growth rate on properties of TiO2 films, samples are deposited at different immersion cycle with constant precursor concentration and immersion time.1% (0.5ml) of TiCl3 and 1.5% (0.75ml) of ammonium hydroxide was taken in the separate beaker. Both the solutions were continuously stirred by means of a magnetic stirrer. The substrate first dipped in 1% (0.5ml) of TiCl3 for 30 seconds, after dipping substrate rinsed with deionized water. The subsrate again dipped in 1.5% (0.75ml) of ammonia solution for 30 seconds. After dipping substrate ws subjected to the deionised water for rinsing. This procedure is repeated for different immersion cyclesof 40, 50, 60.finally the substrate is placed in desiccators for drying. One reaction cycle is defined as the condition of being immersed in the following solvents and solution:

- Immersion in cationic solution.

- Immersion in Deionized water.

- Immersion in anionic solution.

- Immersion in Deionized water.

Various deposition parameters such as immersion time, immersion cycle, and concentration of the precursors are employed and optimized. In the present work, TiO2 films with different growth rate are deposited as the growth rate of the films has greater influence on the film proportion. Since the growth rate of the films has greater influence on the film properties, deposit TiO2 films with different growth rates. Various samples of TiO2 films are deposited by varying the number of SILAR (or) reaction cycles and with optimized time. The deposition parameter adopted in the present study for the deposition of TiO2 films is as shown in table 3.1

3.2.1.5 GROWTH RATE:

Growth rate is defined as the ratio of overall thickness of film to the number of cycles;

3.3 STRUCTURAL ANALYSIS

The term structure encompasses variety of concepts, which describes on various scales, the arrangement of the building blocks of a material. The microcrystalline structure of thin films is found to have profound influence on the optical, electrical, mechanical and other properties of thin films. The physical properties of thin films are known to differ widely from those of bulk materials.

This is evidently connected with the small size of the crystallites forming the film and in particular, with the large number of defects such as dislocations, vacancies, stacking faults, grain boundaries and twists. The method of film deposition also influences the structure of the deposited films. The study of the film structure is particularly important when couples with data; the film formation processes with physico-chemical properties of the film.

X- ray diffraction is a very powerful and suitable technique for characterizing the microstructure of the films. It provides a variety of information such as the presence of elements, grain size and orientation, strain state, interfaces and solute concentration distribution between layers.

X-rays, being electromagnetic waves, are scattered in all directions by electron present in different orbital positions around the atom. This is possible because electrons are charged particles and being so, they receive the energy from the electromagnetic X-ray waves, get excited and subsequently while coming down to ground state, radiate the energy. Electrons present in an atom take part in scattering in this way and their effect taken together, gives the scattering effect due to the atom. If the atoms in the matter are periodically arranged, the scattered radiation also bring certain phase relations particular for that ordering present among the atoms in the matter and on this basis X-ray diffraction relations are developed. It is mentioned that the diffraction can happen only for X-rays, electron beams and neutron beams. So these are only tools for investigations of the inner structural arrangements within solid or liquid. [46]

3.3.1 THEORY OF BRAGG’S LAW

The basic X- ray diffraction is based on Bragg’s equation. Bragg’s law defines that the wave scattered by the successive parallel planes of atoms of interplanar spacing “d” which is equal to an integral number of wavelength, where phase difference is 2/ times the path difference.

If  is the angle of incidence, then the path difference between two waves is “2d sin”. Hence the Braggs law is,

2d sin  = n

Where,

n = Order of reflection.

d = Distance between the atomic planes parallel to the axis of incident beam.

= Wavelength of x rays.

For X-ray diffraction, there are two approaches: kinematical and dynamical. when the back internal reflections from crystal layers in the same direction as that of the incident beam are neglected, the theory developed is called kinematical and when that is into consideration, theory developed is dynamical.

X-ray diffraction has many field applications not only in the field of structural analysis of crystalline and amorphous materials, inorganic or even complex organic materials but also metallurgical fields.

3.3.2 XRD DIFFRACTOMETER

X-ray diffractometer comprises of three parts of basic diffraction unit, counter, goniometer and electronic circuit panel with computer-controlled recorder.

The equipment consist of X-ray generator diffractometer, proportional counter and single channel pulse height analyzer. The specimen is mounted at the center of the diffractometer and rotated by angle around the axis. The counter is attached to arm rotating around the same axis the focusing circle continuously stinks with increasing diffraction angle.

Only (hkl) plane parallel to the film placed contribute to the diffracted intensity. Diffraction angle and intensity of the lines are measured with greater accuracy. Possible directions in which a crystal can diffract a beam of mono chromatic X-rays are simply determined by Bragg's conditions nλ= 2d (sinθ).

Film for analysis was mounted on suitable holders to eliminate substrate thickness effects on the position of the diffraction plane. TiO2 thin film samples coated on glass substrates were used for XRD studies.

Applications of XRD includes,

- Characterization of crystalline materials

- Determination of unit cell dimensions

- Measurement of purity of the sample

- Identification of fine grained materials

3.3.3 DETERMINATION OF STRUCTURAL PARAMETERS:

a. Inter planar spacing:

From the XRD profiles, the inter planar spacing dhkl was calculated using the Bragg’s relation.

dhkl=nλsinθ

Where,

λ = Wavelength of the x-rays used

n = Order of diffraction.

= Angle of diffraction.

b. Grain size:

The grain size (D) of the films was calculated by the Scherrer’s formula.

D=   0.9λβcosθ

Where,

β is the full width at half maximum of the corresponding peak of the XRD pattern.

c. Lattice constant:

From the observed and derived d spacing and assumed (hkl) indices, the lattice constant  is evaluated.

d. Dislocation density and micro chain:

A dislocation is an imperfection in a 	crystal associated with the misregistry of the lattice existing in different parts of the crystal. Unlike vacancies and interstitial atoms, dislocations are not equilibrium imperfections. i.e. thermo dynamic considerations are inadequate to account for their existence in the observed densities. The dislocation density (δ) is calculated from the grain size (D) using the following equation

= 1/D2 lines/m2

δ=1D2lines/m2The origin of micro strain is related to the lattice misfit, which in turn depends upon the deposition conditions. The micro strain (ε)

The crystallographic properties of TiO2 thin films have been investigated by X- ray diffraction technique.

3.3.4 ANNEALING

As deposited thin films may contain many defects such as voids, pinholes etc. Annealing of thin films reduce the defects and increases the crystalline size. In the present work the as deposited TiO2 thin films are annealed in air at 300ºC for one hour.

3.4 OPTICAL ANALYSIS

3.4.1 UV-VISIBLE SPECTROPHOTOMETER

The instrument used in ultraviolet-visible spectroscopy is called an UV/Vis spectrophotometer. It measures the intensity of light passing through a sample (I), and compares it to the intensity of light before it passes through the sample (Io). The ratio I / Io is called the transmittance, and is usually expressed as a percentage (%T). The absorbance, A, is based on the transmittance.

A = − log (T/100)

The UV-visible spectrophotometer can also be configured to measure reflectance. In this case, the spectrophotometer measures the intensity of light reflected from a sample (I), and compares it to the intensity of light reflected from a reference material (Io)(such as a white tile). The ratio I / Io is called the reflectance, and is usually expressed as a percentage (%R).

The basic parts of a spectrophotometer are a light source, a holder for the sample, a diffraction grating in a monochromator or a prism to separate the different wavelengths of light, and a detector. A spectrophotometer can be either single beam or double beam.    (Fig. 3.2)

A beam of light from a visible and/or UV light source is separated into its component wavelengths by a prism or diffraction grating. Each monochromatic (single wavelength) beam in turn is split into two equal intensity beams by a half-mirrored device. One beam, the sample beam, passes through a small transparent container (cuvette) containing a solution of the compound, being studied in a transparent solvent.

The other beam, the reference, passes through an identical cuvette containing only the solvent. The intensities of these light beams are then measured by electronic detectors and compared. The intensity of the reference beam, which should have suffered little or no light absorption, is defined as I0. The intensity of the sample beam is defined as I. Over a short period of time, the spectrometer automatically scans all the component wavelengths in the manner described. The ultraviolet (UV) region scanned is normally from 200 to 400 nm, and the visible portion is from 400 to 800 nm.

If the sample compound does not absorb light of of a given wavelength, I = I0. However, if the sample compound absorbs light then I is less than I0, and this difference is plotted on a graph versus wavelength. [47]

Absorption may be presented as transmittance (T = I/I0) or absorbance (A= log I0/I). If no absorption has occurred, T = 1.0 and A= 0. Most spectrometers display absorbance on the vertical axis, and the commonly observed range is from 0 (100% transmittance) to 2 (1% transmittance). The wavelength of maximum absorbance is a characteristic value, designated as λmax.

3.4.2 CALCULATION OF OPTICAL CONSTANTS

a. Transmittance (T):

Transmittance is the act of transmitting. It is also called transmission factor, a measure of the ability of anything to transmit radiation, equal to the ratio of the transmitted light to the incident light; the reciprocal of the opacity.

In other words, Transmittance T is the fraction of incident light at a specified wavelength that passes through a sample.

Where,

I0 is the intensity of the incident light.

I is the intensity of the light coming out of the sample. [48, 49]

b. Absorbance (A):

The fraction of irradiation, which is absorbed, is known as absorbtivity. The absorbance of a sample is proportional to the thickness of the sample and the concentration of the absorbing species in the sample, in contrast to the transmittance I / I0 of a sample, which varies exponentially with thickness and concentration.

A = -log 10 (I/Io)

A = log (1/T)

Where,

I is the intensity of light at a specified wavelength λ that has passed through a sample.

I0 is the intensity of the light before it enters the sample or incident light intensity

T is the Transmittance.

c. Extinction coefficient (Kf):

The Extinction coefficient of a material is measure of how well it scatters and absorbs electromagnetic radiation. If the electromagnetic radiation can pass through very easily then the material has a low extinction coefficient and conversely if the radiation hardly penetrates the material but rather quickly becomes “extinct” if the extinction coefficient is high.

Where,

= Wavelength

T = Transmittance

d = Thickness of the film

d. Absorption coefficient:

Absorption coefficient (a) is the relative decrease in the intensity of a collimated beam of electromagnetic radiation, as a result of absorption by a sample. Material defines extent of absorption of electromagnetic radiation

e. Direct transition

In a material, which is free of imperfections, these occur direct but allowed transtitions from valance band to conduction band. In this case the top of valance band and bottom of conditions based will be at same point.

αhν = A (hν- Eg)1/2

If power index is 3/2 i.e.

αhν = A (hν - Eg) 3/2

Transition is direct but forbidden.

d. Indirect transition

When material contain, defects such a impurities, dislocations etc. the perturbation is to be considered in the system and also interaction with photons of the vibrational modes of lattice. These perturbations will give rise to an additional transition, which is known as indirect transitions. In this special case the bottom of the valance band and the top of conduction band will be at different points. The condition for the indirect transition is

αhv = A (hv - Eg)2

αhv = A (hv - Eg)3

Since indirect transition is forbidden n becomes three.

f. Band gap

In a material, the energy difference between its non-conductive state and its conductive state is called band gap. There is virtually no band gap in most metals, but a very large one in an insulator (dielectric). In a semiconductor, the band gap is small. Technically, the band gap is the energy it takes to move electrons from the valence band to the conduction band. For incident photon energy greater than the band gap and above, the exponential and the optical absorption follow a power law.

αhν=A(hν-Eg)n

Table 3.1 DEPOSITION CONDITIONS

| Samples | Volume in percent |  | Volume in ml |  | Adsorption time (sec) | Reaction time (sec) | Rinsing time (sec) | Immersion cycle (sec) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | TiCl3 | NH3OH | TiCl3 | NH3OH |  |  |  |  |
| 1 | 1 | 1.5 | 0.5 | 0.75 | 30 | 30 | 15 | 17 |
| 2 | 1 | 1.5 | 0.5 | 0.75 | 40 | 40 | 15 | 17 |
| 3 | 1 | 1.5 | 0.5 | 0.75 | 50 | 50 | 15 | 17 |

CHAPTER IV

RESULTS AND DISCUSSION

The effect of growth rate on the structural and optical characteristics of TiO2 thin films prepared by SILAR method is discussed in this chapter.

4.1 NATURE OF THIN FILM

Thickness plays an important role in thin film properties and almost all film properties are thickness dependent. In the present work, thickness of the sample is estimated by gravimetric method. The films are deposited at different growth rates.

Thickness of the film deposited by SILAR method is in the range of 0.5-0.9m. It is found that thickness of the films is increased with growth rate. (Fig 4.3.25)

# 4.2 STRUCTURAL CHARECTERIZATION

The crystalline phase formation of the TiO2 thin films annealed at 300C is analyzed by X ray diffraction. The XRD pattern of the films annealed at 300C is shown in fig 4.2.1 absence of prominent peaks in the XRD pattern reveals the amorphous nature of the film.

V.Senthil kumar et al., (2008) reported that TiO2 thin film annealed at 400C for 1 hr results in growth of anatase phase of TiO2. TiO2 films deposited at 300C are amorphous in nature. Further increasing the deposition temperature leads to a formation of anatase.

M.M.Hasan et al. (2008) observed that TiO2 films annealed at 300C exhibited characteristics peak of anatase crystal plane and intensities of the peaks of few anatase planes increased slightly with the increase of annealing temperature.

4.3 OPTICAL CHARACTERIZATION

Optical transmittance data are recorded using UV-VIS NIR spectrophotometer, optical constants such as Absorbance (A), Extinction coefficient (kf), Absorption coefficient () and Band gap (Eg) are calculated from transmittance data.

4.3.1 TRANSMITTANCE

The optical transmittance spectra of TiO2 thin film deposited at different growth rate are shown in fig 4.3.1, 4.3.2, and 4.3.3. Transmittance of the films rises sharply near the UV-VIS boundary, there is a gradual increase in the transmittance of the film in VIS and NIR region. Transmittance of the film decreases with increase in thickness.

S.Biswas et al, (2006) reported an optical transmittance of 80% at 500 nm for the TiO2 film deposited by CBD technique. R.Dholam et al, (2008) reported an optical transmittance of 90% at 390 nm for the TiO2 film deposited by R.F Magnetron sputtering.

The value observed in SILAR method is less than the reported values.

A significant decrease in the transmittance below 400 nm can be as assigned to absorption of light caused by the excitation of electrons from the valence band to conduction band of titania.

4.3.2. ABSORBANCE

The absorbance spectra of TiO2 thin film shown in fig 4.3.5, 4.3.6, and 4.3.7. Which reveals that absorbance falls of rapidly in UV -VIS boundary while there is gradual decrease in absorbance with increase in wavelength in VIS –NIR region.

Chung – Han- Wua et al, (2011) reported that absorbance of the tio2 film deposited by spin coating method decreases rapidly in the UV region. The UV/VIS absorption peak spectrum of TiO2 film exhibits an adsorption peak at 257 nm.

4.3.3 EXTINCTION COEFFICIENT

The extinction coefficient spectra of TiO2 thin film are shown in fig 4.3.9, 4.3.10, and 4.3.11. Extinction coefficient falls rapidly near UV VIS boundary and remains constant with increase in wavelength for sample 1 and sample 2 but increases for sample 3. The films have very low extinction coefficient in visible region.

M.M Hasan et al., (2008) reported that extinction coefficient falls rapidly in UV- VIS boundary for TiO2film deposited by R.F Magnetron sputtering agree well with the result obtained in the present work but disagrees with results of Diana Mandare et al., (1999)

4.3.4 ABSORPTION COEFFICIENT

The absorption coefficient spectra for the investigated films are shown in fig 4.3.13, 4.3.14, and 4.3.15 for various samples. Absorption coefficient falls rapidly in wavelength range of 350 nm, while there occurs linear decrease in absorption coefficient with increase in wavelength in NIR and IR region. Maximum absorption coefficient is observed in the UV region

The obtained absorption coefficient for TiO2 thin film deposited by SILAR method agrees well with the results of M. Gartner et al., (2008)

4.3.5 BAND GAP

The direct and indirect band gap value of TiO2 thin films deposited by SILAR method is in the range of 3.7eV, 3.65eV, 3.4eV and 3.09eV, 3.17eV, 2.1eV respectively. The direct and indirect band gap of the film decreases with increasing growth rate. (Refer fig. 4.3.26, 4.3.27 and table 4.1) the obtained values of direct band gap TiO2 thin film are agreeing well with the results of R.S Mane et al., (2005) and M.M. Hasan et al., (2008)

The indirect band gap obtained for TiO2 thin film prepared by SILAR method agrees well with the result of R.S. Mane et al., (2005)

The direct and indirect optical band gap for room temperature and substrate temperature at 400C is found to be 3.50eV, 3.41eVand 3.50eV, and 3.54eV respectively. The transmittance of TiO2 thin film is noted higher than 75% for wavelength between 400 to 700nm. V. Senthilkumar et al., (2010)

# 4.3.6 EFFECT OF ANNEALING

Annealing was applied after the deposition of TiO2 to improve the crystal nature and in order to test the higher absorption behaviour of TiO2. The optical constants such as transmittance (T), absorbance (A), extinction coefficient (kf), absorption coefficient () and band gap (Eg) calculated for TiO2 thin film annealed at 300C is shown in fig. 4.3.4,    4.3.8,  4.3.12, 4.3.16, 4.3.20, 4.3.24 respectively.

# 4.3.6.1 TRANSMITTANCE

Optical transmittance spectra of TiO2 thin film annealed at 300C is shown in       fig 4.3.4. There is a gradual increase in transmittance of TiO2 thin film in VIS and NIR region. TiO2 thin film annealed at 300C shows lower transmittance compared to as deposited TiO2 thin film. Hence it agrees well with the results of M.M. Hasan et al., (2008)

M.M. Hasan et al., (2008) reported that TiO2 films annealed at a higher temperature shows a lower transmittance. Because annealing treatment causes a film surface to be rougher which scatters light.

4.3.6.2 EXTICTION COEFFICIENT

Extinction coefficient spectra of TiO2  thin film annealed at 300C is shown in      fig 4.3.8 obtained value of extinction coefficient is found to increase for TiO2 thin film annealed at 300C than as deposited thin film that appears similar to the results of M.M. Hasan et al., (2008)

M.M. Hasan et al., (2008) reported that extinction coefficient is also found to increase as the treatment temperature is increased.

4.3.6.3 BAND GAP

The direct and indirect band gap value of TiO2 thin film annealed at 300C is found to be 3.72 eV and 2.21 eV is shown in fig 4.3.20 and 4.3.24 respectively. The obtained value increases with temperature compared to as deposited thin film. It agrees well with the results of M.M. Hasan et al., (2008) but differs with the results of Lei Ge et al., (2006) that reveals band gap decreases with calcinations temperature.

M.M. Hasan et al., (2008) reported that direct optical band gap for TiO2 thin film annealed at 300C is 3.67 eV to 3.68 eV. Hence both direct and indirect band gap increases with annealing temperature.

.

# Table 4.1 Effect of Growth Rate with Band Gap

| Samples | Growth rate (nm/cycle) | Thickness (m) | Direct Band Gap (eV) | Indirect Band Gap (eV) |
| --- | --- | --- | --- | --- |
| Sample 1 Sample 2 Sample 3 | 0.01341 0.01383 0.01516 | 0.5367 0.6915 0.9100 | 3.70 3.65 3.40 | 3.09 3.17 2.10 |

## Table 4.2 Effect of Annealing

| # Before Annealing |  | # After Annealing |  |
| --- | --- | --- | --- |
| # Direct Band Gap (eV) | # Indirect Band Gap (eV) | # Direct Band Gap (eV) | # Indirect Band Gap (eV) |
| # 3.4 | # 2.2 | # 3.72 | # 2.21 |

Fig. 4.3.1 VARIATION OF PERCENTAGE OF TRANSMITTANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 1)

Fig. 4.3.2 VARIATION OF PERCENTAGE OF TRANSMITTANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 2)

Fig. 4.3.3 VARIATION OF PERCENTAGE OF TRANSMITTANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3)

Fig. 4.3.4 VARIATION OF PERCENTAGE OF TRANSMITTANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3 - Annealed at 300C)

Fig. 4.3.5 VARIATION OF ABSORBANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 1)

Fig. 4.3.6 VARIATION OF ABSORBANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 2)

Fig. 4.3.7 VARATION OF ABSORBANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3)

Fig. 4.3.8 VARIATION OF ABSORBANCE OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3 - Annealed at 300C)

Fig. 4.3.9 VARIATION OF EXTINCTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 1)

Fig. 4.3.10 VARIATION OF EXTINCTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 2)

Fig. 4.3.11 VARIATION OF EXTINCTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3)

Fig. 4.3.12 VARIATION OF EXTINCTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3 - Annealed at 300C)

Fig.4.3.13 VARIATION OF ABSORPTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 1)

Fig. 4.3.14VARIATION OF ABSORPTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 2)

Fig 4.3.15 VARIATION OF ABSORPTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3)

Fig 4.3.16 VARIATION OF ABSORPTION COEFFICIENT OF TiO2 THIN FILM WITH WAVELENGTH (Sample 3 - Annealed at 300C)

Fig 4.3.17 VARIATION OF  (αhv)2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.5367m (Sample 1)

Fig. 4.3.18 VARIATION OF  (αhv)2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.6915m (Sample 2)

Fig. 4.3.19 VARIATION OF (αhv) 2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.910m (Sample 3)

Fig. 4.3.20 VARIATION OF (αhv) 2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.910m (Sample 3 - Annealed at 300C)

Fig. 4.3.21 VARIATION OF (αhv) 1/2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.5367um (Sample 1)

Fig. 4.3.22 VARIATION OF (αhv) 1/2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.6915um (Sample 2)

Fig. 4.3.23 VARIATION OF (αhv) 1/2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.910um (Sample 3)

Fig. 4.3.24 VARIATION OF (αhv) 1/2 OF TiO2 THIN FILM WITH PHOTON ENERGY hv(eV) OF THICKNESS 0.910um (Sample 3 - Annealed at 300C)

Fig. 4.3.25 VARIATION OF THICKNESS WITH GROWTH RATE

(Samples 1, 2, 3)

Fig. 4.3.26 VARIATION OF DIRECT BAND GAP WITH THICKNESS

(Samples 1, 2, 3)

# Fig. 4.3.27 VARIATION OF INDIRECT BAND GAP WITH THICKNESS

(Samples 1, 2, 3)

CHAPTER V

SUMMARY AND CONCLUSION

TiO2 thin film with potential for photovoltaic application has been grown by SILAR method using TiCl3 as an anionic precursor and ammonia as a cationic precursor.

Modified Chemical Bath Deposition (MOCBD) or SILAR is the easiest way of preparing thin films. Homogenous thin films can be prepared inexpensively using this method. No special equipment is needed for this method. Moreover large area deposition of thin films can be attained. This method is believed to be appropriate for the growth of semiconducting film. In the present work SILAR is employed to deposit TiO2 thin films at room temperature. Various films are deposited at different growth rate while concentration and deposition time are maintained constant. Thickness of the film is calculated by weight difference method and the film is found to be comparatively thicker thin film. Good quality thin films of thickness of 0.5, 0.6 and 0.91µm have been obtained.

Films have been characterized by UV-VIS-NIR spectrophotometer. The deposited TiO2 films exhibit improved optical properties. Optical constants such as Absorbance (A), Transmittance have been recorded from which Absorption coefficient (α) Extinction coefficient (kf) and Energy Band gap have been calculated.

The TiO2 thin films have high transmittance in the UV-VIS region and it varies with corresponding growth rate. The analysis of the result reveals that direct band gap of the deposited material is found to be 3.7ev in UV region.

As the growth rate increases band gap decreases. The optical properties of TiO2 thin film depend on growth rate too with respect to deposition cycle.

A direct band gap value of as deposited TiO2 thin films are in the range of        3.4-3.7 eV. The TiO2 films were annealed in air at 300˚C. The TiO2 films have high transmittance in the visible /NIR region of EM spectrum and hence it is a very good material for antireflection coating, photocatalyst, and optoelectronics.

Deposited TiO2 thin film is analysed to X- ray diffraction to confirm the structure of the synthesized sample. Intensity of X-ray diffraction peaks reveals ultimate description of the TiO2 structure that requires identification of position coordinates of each atom. TiO2 films fabricated by SILAR method onto glass substrate annealed at 300˚C for 3 hours were amorphous structure or poor crystalline as noticed from X ray diffraction studies. The optical direct and indirect band gap of TiO2 thin film increases with temperature.

REFERENCES

- A.Goswami., (1996), Thin Film Fundamentals, New Age International Limited Publishers, New Delhi,

- M.K.K. Aranjari and D. Dasgupta, (1987), Thin Solid Films, 155 - 309

- H.R. Kaufman, J.J. Cuomo, J.M.E. Harper, (1982), Journal Of Vacuum, Science Technology, 21 - 725.

- Jorden .E.L.,  (1981), J.E. Electrochem Society ,108 - 478

- Maissel .L.I. And Clang, (1970), Handbook of Thin Film Technology, Mc Graw Hill New York.

- Ludmela Ec Kertova, (1986), Physics of Thin Films, Plenum Press, New York.

- Zhongchun Wang, Ulf Helmerson, Per-Olov Kall, (2002), Thin Solid Films, 405  50-54.

- Silvia Gelover, Pedromondragon, Antoniojimenez, (2004), Journal Of Photochemistry And Photobiology 165, 241 - 246

- C.Pepe, R. Amadelli, M.Pimpinilli, L. Cassae, Koriyama, (2004), 6-7 September.

- www.wikipedia.org.

- B. Karunagaran, R.T. Rajendra Kumar, C.Viswanathan, D.Mangalaraj, Sa.K. Narayandass, G. Mohan Rao, (2003) Crystal Research Technology 38, 773-778.

- Zhongchun Wang, Xingjang Hu, (1999), Thin Solid Films 352, 62-65.

- K. Prabakar; Min-kyu Son; Daniel Ludeman; Hee-je Kim, (2010), Visible Light Enhanced TiO2 Thin Film Bilayer Dye Sensitized Solar Cells, Thin Solid Films,  Vol 519; No 2;  894-899.

- Corina Vacaroiu, Madalin Enache, Mariuca Gartner, Gabriela Popescu;Mihai Anastasescu, Aurelia Brezeanu,  N. Todorova, Tatiana Giannakopoulou,  Christos Trapalis,  Lucia Dumitru, (2009) The Effect of Thermal Treatment on Antibacterial Properties of Nanostructured TiO2(N) Films Illuminated with Visible Light, World Journal of Microbiology and Biotechnology. Vol 25; No 1; 27-31.

- Xian-Feng Gao,  Wen-Tao Sun, Guo Ai, Lian-Mao Peng, (2010), Photoelectric Performance of TiO2 Nanotube Array Photoelectrodes Cosensitized with CdS/CdSe Quantum dots Applied Physics Letters.Vol 96; No 15.

- Parvaneh Sangpour; Fatemeh Hashemi; Alireza Z. Moshfegh, (2010), Photoenhanced Degradation of Methylene Blue on Cosputtered M:TiO2 (M = Au, Ag, Cu) Nanocomposite Systems: A Comparative Study Journal of Physical Chemistry C.Vol 114; No 33; 13955-13961.

- Yahia Djaoued; K. Ozga; A. Wojciechowski; A.H. Reshak; J. Robichaud; I.V. Kityk, (2010), Photoinduced Effects in TiO2 Nanocrystalline Films with Different Morphology Journal of Alloys and Compounds.Vol 508; No 2; 599-605.

- Habib M. Pathan; Woo Young Kim; Kwang-Deog Jung; Oh-Shim Joo, (2005), A Chemical Route to Room-temperature Synthesis of Nanocrystalline TiO2 Thin Films Applied Surface Science.Vol 246; No 1-3; 72-76.

- Xiaojun Dang; Keith J. Stevenson; Joseph T. Hupp, (2001), Monitoring Molecular Adsorption on High-Area Titanium Dioxide via Modulated Diffraction of Visible Light Langmuir.Vol 17; No 11; 3109-3112.

- C. Millon , D. Riassetto, G. Berthome, F. Roussel, M. Langlet, (2007), The photocatalytic activity of sol- gel derived photo- plantinized TiO2 films, journal of photochemistry and photobiology A: chemistry vol 189; No 2-3; 334-348.

- E.Vigil, D. Dixon, J.W. J Hamilton and J. A. Byme, (2009), Deposition of TiO2 thin films on steel using a microwave activated chemical bath, surface and coatings technology volume 203, issue 23, pages 3614- 3617.

- Kee- Rong Wu, chung- hsuang hung and Meng- Hsiu Tsai, (2009), Effects of ITO thin films on microstructural and photocatalytic  properties  of layered Tio2 / ITO films prepared via an extended deposition period, Applied catalysis B: Environmental volume 92, issues 3-4, Pages 357- 366.

- T.M.Wang , S.K. zheng, W.C. Hao  and C. Wang, (2002), Studies on photocatalytic activity and transmittance  spectra of TiO2  thin films prepared by r.f. magnetron sputtering method, Surface and coatings Technology volume 155, issues 2-3, Pages 141-145.

- S.K. Zheng, G. Xiang, T.M. Wang, F. Pan,  C. Wang and W.C. Hao,  (2003), photocatalytic activity studies of TIo2 thin films prepared by r.f. magnetron sputtering, Vaccum Volume 72, Issue 1, Pages 79 – 84.

- G. Sauthier, F.J. Ferrer, A. Figueras and E. György, (2010), Growth and characterization of nitrogen–doped TiO2 thin films prepared by reactive pulsed laser deposition, Thin Solid FilmsVolume 519, Issue 4, Pages 1464-1469.

- Peng Sun, Haibo Liu, Haibin Yang, Wuyou Fu, Shikai Liu, Minghui Li, Yongming Sui, Yanyan Zhang and Yixi, (2010), Synthesis and characterization of TiO2 thin films coated on metal substrate, Science Volume, Pages 3170-3173.

- Longjie Zhou, Rudolf C. Hoffmann , Zhe Zhao, Joachim Bill and Fritz Aldinger, (2008), Chemical bath deposition of thin TiO2 anatase films for dielectric applications, Thin Solid Films Volume 516, Issue 21, Pages 7661-7666.

- F. Fernández-Lima, E. Vigil, I. Zumeta, F. L. Freire, R. Prioli and E. Pedrero, (2003), Rutherford back scattering spectrometry analysis of TiO2 thin films, Materials Characterization, Volume 50, Issues 2-3, Pages 155-160.

- H.M. Pathan, Sun-Ki Min, J.D. Desai, Kwang-Deog Jung and Oh-Shim Joo, (2006), Preparation and   characterization of titanium dioxide thin films by SILAR method, Materials Chemistry and Physics Volume 97, Issue 1, Pages 5-9


References and further reading may be available for this article. To view references and further reading you must .

purchase this article.

- A.M. More, J.L. Gunjakar, C.D. Lokhande and Oh Shim Joo, (2009) Fabrication of hydrophobic surface of titanium dioxide films by successive ionic layer adsorption and reaction (SILAR) method, Applied Surface Science Volume 255, Issue 12, Pages 6067-6072.

- U.M. Patil, K.V. Gurav, Oh-Shim Joo and C.D. Lokhande, (2009), Synthesis of photosensitive  nanograined TiO2 thin films by SILAR method


References and further reading may be available for this article. To view references and further reading you must ,purchase this article. Journal of Alloys and Compounds Volume 478, Issues 1-2, , Pages 711-715.

- S.S. Kale, R.S. Mane, Hoeil Chung, Moon-Young Yoon, C.D. Lokhande and Sung-Hwan Han,(2006), Use of successive ionic layer adsorption and reaction (SILAR) method for amorphous titanium dioxide thin films growth, Applied Surface Science Volume 253, Issue 2,  Pages 421-424.

- Chih-Ming Wang Shih-Yuan Lin and Ying-Chung Chen, (2008), Electrochromic properties of TiO2 thin  films prepared by chemical solution deposition method, Journal of Physics and Chemistry of Solids  Volume 69, Issues 2-3, Pages 451-455.

- Longjie Zhou, Rudolf C. Hoffmann, Zhe Zhao, Joachim Bill and Fritz Aldinger,(2008), Chemical bath deposition of thin TiO2-anatase films for dielectric applications, Thin Solid FilmsVolume 516, Issue 21, Pages 7661-7666.

- A.M. More, T.P. Gujar, J.L. Gunjakar, C.D. Lokhande and Oh-Shim Joo, (2008), Growth of TiO2 nanorods by chemical bath deposition method, Applied Surface ScienceVolume 255, Issue 5, Part 2, Pages 2682-2687

- C. Quiñonez, W. Vallejo and G. Gordillo, (2010), Structural, optical and electrochemical properties of TiO2 thin films grown by APCVD method, Applied Surface Science Volume 256, Issue 13,  Pages 4065-4071

- Chiaki Ohara, Teruhisa Hongo, Atsushi Yamazaki and Toshio Nagoya, (2008) Synthesis and characterization of brookite/anatase complex thin film Applied Surface Science Volume 254, Issue 20,  Pages 6619-6622.

- M. Uzunova-Bujnova, R. Todorovska, M. Milanova, R. Kralchevska and D. Todorovsky, (2009) On the spray-drying deposition of TiO2 photocatalytic films Applied Surface ScienceVolume 256, Issue 3, Pages 830-837.

- A.P. Caricato, M.G. Manera, M. Martino, R. Rella, F. Romano, J. Spadavecchia, T. Tunno and D. Valerini, (2007), Uniform thin films of TiO2 nanoparticles deposited by matrix-assisted pulsed laser evaporation Applied Surface Science Volume 253, Issue 15, Pages 6471-6475.

- Bok-Hee Kim, Jo-Young Lee, Yong-Ho Choa, M. Higuchi and N. Mizutani, (2004), Preparation of TiO2 thin film by liquid sprayed mist CVD method


References and further reading may be available for this article. To view references and further reading you must purchase this article. Materials Science and Engineering Volume 107, Issue 3, Pages 289-294.

- Dong-Joo Kim, Jin-Yi Kang and Kyo-Seon Kim, (2010), Preparation of TiO2 thin films on glass beads by a rotating plasma reactor 


References and further reading may be available for this article. To view references and further reading you must purchase this article.Journal of Industrial and Engineering Chemistry Volume 16, Issue 6, Pages 997-1000.

- K.G. Grigorov,  I.C. Oliveira; H.S. Maciel, M. Massi; M.S. Oliveira Jr., J. Amorim; C.A. Cunha, (2011), Optical and Morphological Properties of N-doped TiO2 Thin Films Surface Science.Vol 605; No 7-8; 775-782.

- Jing Du; Kwang-Leong Choy, (2004), Electrostatic Spray Assisted Vapour Deposition of TiO2-Based Films Solid State Ionics: Diffusion and Reactions.Vol 173; No 1-4; 119-124.

- Yahia Djaoued; K. Ozga; A. Wojciechowski; A.H. Reshak; J. Robichaud; I.V. Kityk, (2010), Photoinduced Effects in TiO2 Nanocrystalline Films with Different Morphology Journal of Alloys and Compounds.Vol 508; No 2; 599-605.

- Joy george, (1992), preparation of thin films, Marcel Dekker Newyork.

- Sanath kumar Shafferjee, (1999), X-ray diffraction its theory and application, prentice-hall of India (1999) page no: 152.

- Skoog, et al., (2007), Principles of Instrumental Analysis. 6th ed. Thomson Brooks/Cole. 169-173.

- ^ "IUPAC handbook definition". http://www.iupac.org/goldbook/A00035.pdf. Retrieved 2009-07-02.

- ^ "CRC Dictionary of pure and applied physics, CRC Press, Editor: Dipak Basu (2001)". http://www.crcpress.com/product/isbn/9780849328909.

- S. Biswas , M.F. Hossain , T. Takahashi , Y. Kubota , A. Fujishima, (2008),  Photocatalytic activity of high-vacuum annealed CdS–TiO2 thin film.Thin Solid Films 516 7313–7317.

- R. Dholam, N. Patel, M. Adami and A. Miotello, (2008), Physically and chemically synthesized TiO2 composite thin films for hydrogen production by photocatalytic water splitting


References and further reading may be available for this article. To view references and further reading you must purchase this article. International Journal of Hydrogen Energy Volume 33, Issue 23,  Pages 6896-6903

- Lei Ge , Mingxia Xu, Haibo Fang, Ming Sun, (2006),  Preparation of TiO2 thin films from autoclaved sol containing needle-like anatase crystals Applied Surface Science 253 720–725

- Chung-Han Wu, Hanying Li , Hon Hang Fong , Vladimir A. Pozdin , Lara A. Estroff , George G. Malliaras, (2011), Room-temperature preparation of crystalline TiO2 thin films and their applications in polymer/TiO2 hybrid optoelectronic devices, Organic Electronics 12 1073–1079.

- M. Gartner, P. Osiceanu, M. Anastasescu, T. Stoica, T.F. Stoica, C. Trapalis, T. Giannakopoulou, N. Todorova and A. Lagoyannis, (2008), Investigation on the nitrogen doping of multilayered, porous TiO2 thin films, 


References and further reading may be available for this article. To view references and further reading you must purchase this article.Thin Solid Films Volume 516, Issue 22, Pages 8184-8189

- M. M. Hasan, A. S. M. A. Haseeb, R. Saidur, and H. H. Masjuki, (2008), Effects of Annealing Treatment on Optical Properties of Anatase TiO2 Thin Films,  International Journal of Chemical and Biological Engineering.

- Diana Mardare and Peter Hones, (1999), Optical dispersion analysis of TiO2 thin films based on variable-angle spectroscopic ellipsometry measurements 


References and further reading may be available for this article. To view references and further reading you must , purchase this article.Materials Science and Engineering B Volume 68, Issue 1, Pages 42-47

- R.S. Mane, Seung Jae Roh, Oh-Shim Joo, C.D. Lokhande, Sung-Hwan Han, (2005), Improved performance of dense TiO2/CdSe coupled thin films by low temperature process, Electrochimica Acta 50 2453–2459,

- V. Senthilkumar , M. Jayachandran, C. Sanjeeviraja, (2010), Preparation of anatase TiO2 thin films for dye-sensitized solar cells by DC reactive magnetron sputtering technique, Thin Solid Films 519 991–994